## Slide 1: PRECOS ISTC project proposal #3813: Phase relation in corium systems
ISTC
A.P. Alexandrov Research Institute of Technology
Presented by Sevostian V. Bechta
12th CEG-SAM Meeting

## Slide 2: Contents
  General information
  Project focus
  Methodology
  Links with CORPHAD project
  PRECOS test matrix
  Conclusions

## Slide 3: PRECOS project general information
Project participants and coordination
Areva NP, Germany
ISTC, Moscow
FZK, Germany
IRSN,
France
ITU,
EK
CEA,
France
Collaborators
Steering committee
Operation Agent: A.P. Alexandrov RIT, Russia
Coordinator
ISC RAS,
Russia
IHT RAS,
Russia
SPb Electrotechnical State University, Russia

## Slide 4: PRECOS project focus
Project objective: Experimental study of phase diagrams of corium mixtures
Data application
  Liquidus and solidus temperatures versus components concentration
  Temperature-concentration regions of the miscibility gap
  Coordinates of eutectic, dystectic and other characteristic points
  Final solubility in solid solution
Experimental data
  Thermodynamic database optimisation
  Thermodynamic code validation
  Corium behaviour modelling

## Slide 5: Methods of phase diagram experimental study
Visual polythermal analysis in the cold crucible (VPA IMCC)
Differential thermal analysis (DTA) and differential scanning calorimetry (DSC)
Visual polythermal analysis in the Galakhov microfurnace (GM)
High-temperature microscopy (HTM)
Laser pulse heating (LP)
These methods have been applied in the projects: COLOSS, METCOR, CIRMAT, CIT, ENTHALPY, ECOSTAR, OECD/MASCA and CORPHAD

## Slide 6: Methods of posttest analysis
Elemental analysis
 X-ray fluorescence analysis (XRF)
 Chemical analysis (СhA)
Phase analysis
 X-ray diffraction analysis (XRD)
 Energy-dispersive X-ray spectrometry (EDX)
Microstructure analysis
 Optical microscopy
 Scanning electron microscopy (SEM)
Oxygen determination
 Carbothermic reduction

## Slide 7: CORPHAD.2 project test matrix
Composition | Atmosphere | Experimental data
UO2 – FeO | Argon/Helium | liquidus, solidus, solubility limits, eutectic points
ZrO2 – FeO |  | 
SiO2 – Fe2O3/Fe3O4 | Helium/Air/ Oxygen | liquidus, solidus, miscibility gap, eutectic points
UO2 – SiO2 | Argon | miscibility gap
UO2 – ZrO2 – FeO/Fe2O3 | Argon/Air | ternary eutectic points
U – O | Argon | liquidus, solidus, miscibility gap
U – Zr – O |  | 
Zr – Fe – O |  | 
U – Fe – O |  | 
Complex corium mixture UO2 – SiO2 – ZrO2 – Al2O3 – CaO – FeO – Cr2O3 | Nitrogen | liquidus, solidus
Links with CORPHAD projects

## Slide 8
3 tests for 1 point on the average
5 tests for 1 point on the average
Additional number of reference specimens: 48
Scope of experimental work in CORPHAD

## Slide 9
CORPHAD Papers
Bechta S.V., Krushinov E.V., Almjashev V.I., Vitol S.A., Mezentseva L.P., Petrov Yu.B., Lopukh D.B., Khabensky V.B., Barrachin M., Hellmann S., Froment K., Fischer M., Tromm W., Bottomley D., Defoort F., Gusarov V.V. Phase diagram of the ZrO2–FeO system // J. Nucl. Mater. Vol. 348, pp. 114-121 (2006)
Bechta S.V., Krushinov E.V., Almjashev V.I., Vitol S.A., Mezentseva L.P., Petrov Yu.B., Lopukh D.B., Khabensky V.B., Barrachin M., Hellmann S., Gusarov V.V. Phase relations in the ZrO2-FeO system // Russian J. Inorg. Chem. 2006. V. 51. N 2. P. 325-331.
Mezentseva L.P., Popova V.F., Almjashev V.I., Lomanova N.A., Ugolkov V.L., Beshta S.V., Khabensky V.B., Gusarov V.V. Phase and chemical transformations in the SiO2–Fe2O3(Fe3O4) systems at various oxygen partial pressure // Russian J. Inorg. Chem. 2006. V. 51. N 1. P. 125-133.
Bechta S.V., Krushinov E.V., Almjashev V.I., Vitol S.A., Mezentseva L.P., Petrov Yu.B., Lopukh D.B., Lomanova N.A., Khabensky V.B., Barrachin M., Hellmann S., Froment K., Fischer M., Tromm W., Bottomley D., Gusarov V.V. Phase Transformation in the Binary Section of the UO2–FeO–Fe System // Russian J. Radiochemistry. 2007. V. 49. N 1. P. 20-24.
Bechta S.V., Krushinov E.V., Almjashev V.I., Vitol S.A., Mezentseva L.P., Petrov Yu.B., Lopukh D.B., Khabensky V.B., Barrachin M., Hellmann S., Froment K., Fischer M., Tromm W., Bottomley D., Gusarov V.V. UO2–FeO phase diagram // J. Nucl. Mater., 362 (2007) 46-52
Mezentseva L.P., Popova V.F., Almjashev V.I., Lomanova N.A., Ugolkov V.L., Bechta S.V., Khabensky V.B., Barrachin M., Hellmann S., Gusarov V.V. Phase diagrams of the SiO2–Fe2O3(Fe3O4) systems in different gas atmosphere // J. Europ. Ceram. Soc., in press

## Slide 10
CORPHAD Papers in preparation
Draft titles:
Eutectic compositions in the UO2–ZrO2–FeO/Fe2O3 systems
(under discussion with collaborators)
Miscibility gap in the UO2–SiO2 system
Miscibility gap in the U–O system

## Slide 11
Results application: Database optimisation
Version 2004
Version 2005
with CORPHAD points in the optimisation
NUCLEA database (PY. Chevalier et al., 2004)

## Slide 12
Version 2004
Version 2005
with CORPHAD points in the optimisation
NUCLEA database (PY. Chevalier et al., 2004)
Results application: Database optimisation (2)

## Slide 13: PRECOS test matrix
Task | Composition | Atmosphere | Experimental data | Priority level | Pt N
1 | Different compositions in the U-Zr-Fe-O system | Argon | Selected points (liquidus, solidus, tie-lines in the miscibility gap) | 1 | 6
2 | ZrO2 - FeOy | Air and pO2 contol | liquidus, solidus, solubility limits | 2 | 3
 | UO2 - SiO2 | Argon | liquidus, solidus, solubility limits, eutectic point | 1 | 7
 | CaO - UO2 |  |  | 1 | 7
3 | UO2 – FeO – SiO2 |  | liquidus, solidus solubility limits, tie-lines in the miscibility gap, ternary eutectic point | 1 | 10
 | UO2 – FeO – CaO |  | liquidus, solidus solubility limits, ternary eutectic point | 1 | 10
 | ZrO2 - FeO - SiO2 |  | ternary eutectic point | 2 | 2
 | ZrO2 - FeO - CaO |  | ternary eutectic point | 2 | 2
4 | Eutectic composition measurement of a realistic complex corium mixture | Argon or Air | System (atmosphere) proposed by French partners (1 system), System (atmosphere) proposed by German partners (1 system), System (atmosphere) proposed by Russian partners (1 system) | 2 | 3
The matrix has been discussed and updated at the 5th, 6th and 7th CORPHAD Project meetings

## Slide 14: Conclusions
Preparation phase of PRECOS project has been finished
Positive CORPHAD experience instills confidence in PRECOS feasibility
PRECOS project has high chance for starting in early 2008, if the proposal is supported by CEG-SAM and EU