## Slide 1: Progress Report on the ISTC project #3592 “Investigation of Corium Melt Interaction with NPP Reactor Vessel Steel” (METCOR-P)
Presented by S. Bechta
13th CEG-SAM meeting
A.P. Alexandrov Research Institute of Technology

## Slide 2: Contents
Essential information
Objectives
Experimental matrix
Test results:
  MCP-1
  MC12, MCP-2
Planning test:
  MCP-3
Organizational problem

## Slide 3: Essential information
IRSN,
France
Project participants and coordination
ISTC, Moscow
FZK, Germany
JRC ITU,
EK
CEA,
France
Collaborators
Steering committee
Operation Agent: A.P. Alexandrov RIT, Russia
Coordinator
AREVA NP, Germany
ISC RAS,
Russia
SPb Electrotechnical State University, Russia
FZD, Germany
FORTUM, Finland

## Slide 4: Objectives of METCOR-P project
Interaction characteristics at the vertically positioned interface
Peculiarities of interaction with European vessel steel
Corium melt oxidation transients
Qualification and quantification of physicochemical phenomena of corium melt interaction with reactor vessel steel with particular interest to:

## Slide 5
Experimental matrix for the METCOR-P project
*) In accordance with the 1st project meeting decision it is replaced by MCP-2 test with UO2+x– ZrO2 corium in air and horizontal position of interface

## Slide 6: Interaction at vertically positioned interface: MCP-1 test
Objectives of the test
Comparison with results of MC6 test with horizontally positioned interface
Test parameters are similar to MC6 test of METCOR-2:
C-30 corium charge
15Kh2NMFA vessel steel
Pure argon above the melt
10 h exposition

## Slide 7: Furnace design
1 – Water-cooled
screen
2 – Lid
3 – Water in
4 – Quartz tube
5 – Crucible sections
6 – Specimen
7 – Inductor
8 – Bottom calorimeter
9 – Welded crucible
sections
10 – SS support 11 – Water out
12 – Electromagnetic
screen
13 – Crucible collector

## Slide 8: TC locations in the specimen
Coordinates of TC hot junctions
Majority of TC were installed at H=50 mm elevation, where the maximum depth of specimen corrosion was expected according to the pretest calculations

## Slide 9: Test procedure
Time, s | Operation mode
0-963 | Furnace deoxygenation by argon flow
963-3550 | Formation and homogenization of the molten pool. Increase of power in the melt to get 1400 oC on the specimen surface
3550-39874 | Surface temperature and specimen - water power kept constant by inductor voltage control
39875-42000 | Heating disconnection, melt solidification and ingot cooling in argon

## Slide 10: Test results: TC readings (1)
Wrong readings of several thermocouples due to corrosion of wires below the hot junctions

## Slide 11: Test results: TC readings (2)
Estimation of IZ progression from TC readings
Different lifetime of TCs in the mushy interaction zone
Not possible to estimate interaction kinetics
Short incubation period (or no incubation)

## Slide 12: Posttest examination (1)
Axial sections of ingot
Example of TC location
Corium upper crust is removed
Metal inclusions in corium ingot
Axial sections of ingot
Axial sections of ingot
The maximum depth of corrosion is in the middle section of the specimen (Н  30 mm) due to formation of a thick corium upper crust and decrease in the melt depth

## Slide 13: Posttest examination (2)
Axial sections of specimen
MCP-1 (90º rotated)
MC 6
Corium
1st layer
2nd layer
Zone of thermal influence
Steel of initial structure
IZ
Steel

## Slide 14: Posttest examination (3)
Temperature profile of the specimen
A – boundary of the thermal influence zone (lamellar pearlite structure indicating eutectic composition formation at 727 C)
B – boundary of the 2nd layer (1000-1090 C)
C – boundary of the 1st layer (1240-1300 C)
1 – 700 C 5 – 1100 C
2 – 800 C 6 – 1200 C
3 – 900 C 7 – 1300 C
4 – 1000 C 8 – 1400 C
T, oC
90° rotated
Upper surface
bottom

## Slide 15
Reduction of Cn up to ≈17% (instead of 30) at the interaction start is explained by a high oxygen content in the upper crust
Higher content of U and Zr in IZ (40-50 and 13-14 mass %) in comparison with МС6 IZ (24 and 5 mass %)
High content of U and Zr in metal inclusion (58 and 24 mass %)
Posttest examination (4)
XRF and chemical analysis
XRF,mass.%
ChA,mass.%
U=66.1
Zr=20.1
Fe=1.7
Cr=0.06
Ni=0.02
U=65.6
Zr=22.1
Fe=1.0
Cr=0.02
Ni=0.03
U=66.6
Zr=23.2
Fe=1.0
U=64.4
Zr=21.7
Fe=3.5
Cr=0.04
Ni=0.08
U=66.7
Zr=22.3
Fe=5.7
XRF
ChA
U=57.5
Zr=24.2
Fe=17.8
Cr=0.2
Ni=0.3
1st layer:
U=52.4
Zr=13.7
Fe=30.9
Cr=0.6
Ni=0.3
U=66.8
Zr=22.3
Fe=2.1
Average
sample of ingot upper part Cn≈40
Average
sample of
crust
Cn≈48
2nd layer:
U=36.4
Zr=14.3
Fe=47.8
Cr=0.8
Ni=0.5
Average
sample of ingot lower part Cn≈32
29-31mm
23mm
25mm

## Slide 16: Posttest examination (5)
SEM/EDX analysis
Steel
Crust
__________
U(Zr)O2
intermetalics
1st layer
__________
U(Zr)O2
Zr(U)Fe2
U6Fe
U(Zr)- Fe
eutectic
1 mm
Corium
____________
U(Zr)O2
-Zr(O)
2nd layer
_________
U(Zr)Fe2
Fe- U(Zr)
eutectic
UFe3
U(Zr)Fe3
No liquid in the crust
Small solid fraction in the 1st layer
Small liquid fraction in the 2nd layer (only in a thin layer contacted with steel)

## Slide 17: Comparison of MCP-1 and MC6 data
Conditions Results
Different conditions not only in the interface orientation, but also in corium oxidation index and heat flux
Reason of result differences ?

## Slide 18: Discussion of results
Possible reason of sorter incubation period in МСР-1 in comparison with МС6:
- thinning of crust between melt and IZ caused by increased heat flux and surface temperature
Lower temperature of MCP-1 IZ final boundary in comparison with MC6 is explained by a significantly increased U/Zr concentrations in МСР-1 IZ
The latter concentrations are probably influenced by decreased Cn, i.e. increased content of Zr-free in the melt

## Slide 19: Planning for the 1st item of the test matrix
Additional test is recommended with:
С-30 melt composition
On-line measurements of specimen corrosion depth
Thermometry of the zone of maximum heat flux
Technical preparation is in progress (higher furnace power, selection of ultrasonic sensors, …)
Test matrix will be updated at the next project meeting

## Slide 20: Interaction of molten corium and vessel steel in the oxidizing atmosphere. Tests MC12, MCP-2

## Slide 21: Test MC12 (1)
(not funded by ISTC)
Corium UO2+x-ZrO2-FeOу
Atmosphere: air, steam
New data on steel corrosion rate, which confirms corrosion intensification at Ts > 1050 0C
SEM/EDX data explain the intensification as a result of liquid-phase diffusion of steel and corium components

## Slide 22: Test MC12 (2)
SEM/EDX analysis
On corrosion layer/corium crust interface a liquid eutectic mixture is formed which is a multi-component system of corium and steel oxides. It produces channels trough the corium crust.
SEM- image IZ corium/steel
SEM- image of corrosion layer and
corium crust interface

## Slide 23: Test MCP-2 (1)
Corium UO2+x – ZrO2
Atmosphere : Air
New corrosion rate data extend the relevant temperature range. No corrosion intensification is observed until the temperature reaches Ts = 1370 0C
SEM/EDX analysis shows liquid phase in corrosion layer and its absence in corium crust during interaction

## Slide 24: Test MCP-2 (2)
IZ microstructure on the
specimen periphery
IZ microstructure in the
specimen center
Presence of liquid phase in corrosion layer
Absence of liquid phase in corium crust

## Slide 25: Corrosion model
W – corrosion rate, m/s
A – pre-exponential factor;
Ea – activation energy, J/mol;
R = 8.314 J/(molК) – universal gas constant;
d – thickness of corium crust, m;
 – thermal conductivity, MW/(m К);
Tsol , TS – solidus temperature of crust composition and temperature
on the steel surface, К;
q – heat flux, MW/m2.
- Tamman equation;
Assumptions:
corrosion layer thickness is neglected;
l = const;
T = Ts

## Slide 26: Summary of experiment data
Mean-square deviations:
Corium UO2+x-ZrO2 – 25 %
Corium UO2+x-ZrO2-FeOу – 35 %

## Slide 27: Correlations for corrosion rate
Corium UO2+x- ZrO2
Corium UO2+x- ZrO2- FeOy
.
(U/Zr)at 1.1 ; Ts = 870…1370C; q = 0.74…1.19 MW/m2; CFeOy = 0…5 %mass
(U/Zr)at = 0.11... 1.05; Ts = 720…1200C; q = 0.3…1.3 MW/m2; CFeOy = 20…30 %mass
Units: W – m/s; q – MW/m2; T - K

## Slide 28
Discussion (1)
Liquid phase diffusion causes corrosion intensification at steel interaction with fusible UO2+x – ZrO2 – FeOy corium after reaching 1050C on the steel surface
Corrosion rate depends on corium composition. It is 2…3 times higher for UO2+x – ZrO2 than for UO2+x – ZrO2 – FeOy at Ts<1050C, in absence of a liquid phase in the corium crust. The higher is Fe concentration in melt, the faster is diffusion of Fe ions through the corium crust.
Corrosion rate is insensitive the above melt atmosphere (steam, air)

## Slide 29: Discussion (2)
Corrosion model and correlations for corrosion rates have been developed for reactor application (e.g. IVR analysis) Further corrosion intensification at Ts→Tsol for fusible corium require to consider heat generated during chemical reaction of RPV steel components oxidation in IVR analysis
Further corrosion intensification at Ts→Tsol for fusible corium require to consider heat generated during chemical reaction of RPV steel components oxidation in IVR analysis
Papers are being prepared for publications (ICAPP’08, NED, …) using the outputs of vessel steel corrosion studies in oxidizing condition

## Slide 30: Planning for the 2nd item of the test matrix: Interactions during corium oxidation.
The test should be carried out before the next test with vertical interface orientation
Procedure (according to test matrix – item 2, line 4):
- repetition of MC6 test with С-30 corium until corrosion saturation
- oxidation of corium (and IZ) by atmosphere replacement
MCP-3 test objectives: Determination of
Thermal response of the specimen caused by IZ oxidation and chemical heat deposition (will be measured by TC)
Oxidation kinetics (will be derived from in- and off-gas composition and flow rates)
Structure and composition of IZ after oxidation (will be determined by the standard set of post test analysis)

## Slide 31: Organizational problem
No ROSATOM Export Control approval of the project
Export licensing is required. A partner - recipient of the project results should be nominated. Information confidentiality and nonproliferation should be confirmed
Possible solution: The funding party (EC) will authorize e.g. one of its Joint Research Centers as the Partner
The project is suspended until ROSATOM and ISTC decision