## Slide 1: Progress Report on the ISTC project #3592 “Investigation of Corium Melt Interaction with NPP Reactor Vessel Steel” (METCOR-P)
A.P. Alexandrov Research Institute of Technology (Russia)
Presented by S. Bechta
14th CEG-SAM meeting
September 9-11, 2008, Kiev

## Slide 2: Contents
General information
Objectives of METCOR-P project
Experimental matrix for METCOR-P project
Steam oxidation effect on the zone of C-32 corium interaction with vessel steel: MCP-3 test
Thermal and mechanical analyses of the VVER-1000 RPV in an IVR scenario considering corrosion effects
Publications
Organizational problem

## Slide 3: General information
IRSN,
France
Project participants and coordination
ISTC, Moscow
FZK, Germany
JRC ITU,
EK
CEA,
France
Collaborators
Steering committee
Operation Agent: A.P. Alexandrov RIT, Russia
Coordinator
AREVA NP, Germany
ISC RAS,
Russia
SPb Electrotechnical State University, Russia
FZD, Germany
FORTUM, Finland

## Slide 4: Objectives of METCOR-P project
Interaction characteristics at the vertically positioned interface
Peculiarities of interaction with European vessel steel
Corium melt oxidation transients
Qualification and quantification of physicochemical phenomena of corium melt interaction with reactor vessel steel with particular interest to:

## Slide 5
Experimental matrix for METCOR-P project
*) In accordance with a decision of the 1st project meeting, it is replaced by MCP-2 test with UO2+x– ZrO2 corium in air and horizontally positioned interface

## Slide 6
Steam Oxidation Effect on Zone of Interaction of C-32 Corium with Vessel Steel: MCP-3 Test

## Slide 7: Objectives of MCP-3 Test
Qualification and quantification of steam oxidation effect on the interaction zone

## Slide 8: Experimental Setup
1 – steam vent from the furnace, 2 – steam supply line, 3 – lid, 4 – water-cooled cover, 5 – quartz tube, 6 – water-cooled electromagnetic screen, 7 – crucible sections, 8 – inductor, 9 – melt, 10 – acoustic defect, 11 – thermal insulation of the specimen, 12 – top specimen calorimeter,
13 – bottom specimen calorimeter, 14 – US sensor
RASPLAV-3 Furnace
Component | Mass, g
UO2 | 1385.7
ZrO2 | 164.1
Zr | 272.5
Total | 1822.3
Furnace Charge
Cn = 30.8
U/Zr = 1.188 at.

## Slide 9
Experimental Setup (2)
Gas-Aerosol Sampling System
1 – tanks with N2 and Ar
2 – water controller
3 – steam generator
4 – quartz tube for
steam supply into
the furnace
5 – steam condenser
6 – condensate
collector
7 – condensate drop
catcher
8 – ejector
9 – large-area filter
(LAF - steam)
10 – silica gel drier
11 – analytical filter
(AF)
12 – electrochemical
sensors of oxygen
and hydrogen
13 – vacuum receiver
14 – large-area filter
(LAF - Argon)
15 – weight sensor
16 – water lock

## Slide 10
Experimental Procedure
Phase | Time interval, s | Description
A | 0…38300 (≈ 11 h) | Molten pool and interaction zone (IZ) formation
B | 38300…42500 | Vessel steel temperature is decreased, crust above the IZ is formed
C | 42500…44300 | Molten pool is oxidized by steam
D | 44300…49200 | Specimen temperature is increased, crust above the IZ dissolves
E | 49200…50490 | Interaction zone and specimen are oxidized

## Slide 11
Experimental Results
Thermocouple Readings and Anode Voltage
During all experiment
Fragment: Oxidation period
A B C D E
A B C D E

## Slide 12
Experimental Results (2)
Corrosion kinetics
A
D
E
References:
[1] S.V. Bechta, V.B. Khabensky,
V.S. Granovsky etc. EXPERIMENTAL
STUDY OF INTERACTIONS BETWEEN
SUBOXIDIZED CORIUM AND REACTOR VESSEL STEEL. Proc. of ICAPP’06, Reno, NV USA, June 4-8, 2006, Paper 6054
Melt
IZ
Specimen

## Slide 13
Posttest Analysis
Ingot and Specimen Section
Mass of steel that migrated into the melt ≈ 190 g
1 – undamaged specimen surface
2 – posttest specimen boundary
3 – boundary of the decarbonized steel zone
4 – zone of the melt thermal impact on the
steel macro- and microstructure
(boundary – isotherm 727ºС ?)
Specimen Section Scheme

## Slide 14
Posttest Analysis (2)
Sample | Concentration, mass % |  |  |  |  | 
 | Fe0 | Fe2+ | Fe3+ | U4+ | U6+ | Zr4+
Ingot | 1.7 | 4.3 | 1.5 | 54.0 | 3.8 | 21.7
Crust above ingot | – | 3.0 | 1.2 | 59.6 | – | 20.0
Corium splashes | – | 3.5 | 1.7 | 56.6 | – | 23.0
Rod | – | 0.8 | – | 63.7 | – | 24.6
Aerosols on quartz tube | – | 8.4 | 1.3 | 53.0 | 4.8 | 17.3
Aerosols on crucible | – | 3.7 | 2.5 | 34.0 | 28.5 | 2.0
Aerosols on LAF (Ar) | 8.7 | 15.3 | 2.3 | 51.4 | 9.3 | –
Aerosols on LAF (steam) | 19.8 | 28.1 | 2.5 | 29.5 | 6.4 | –
Aerosols in condenser | – | 2.5 | 1.8 | 34.8 | 19.6 | 24.0
Chemical Analysis of Samples
Total mass of aerosols – 88.9 g
Mass of evaporated iron – 3.2 g

## Slide 15
Posttest Analysis (3)
Specimen temperatures during its interaction with suboxidized corium
T, oC
Final position of the interaction
zone (IZ)
1 cm
US sensor
sighting spot
Parameter | Test | 
 | MC6 | MCP-3
Final Corrosion Depth, mm | 6.2 | 7.6
The IZ lower boundary temperature at its final position (TB), ºC | 1180 | 1160
Comparison of MC6 and MCP-3 Test Results
End of phase A: ~4000 s

## Slide 16
Corium and IZ/specimen oxidation
Hydrogen Generation
Average rates of hydrogen release:
6.9 mg/s – at phase C
3.6 mg/s – at phase E
Hydrogen release rates at the steady states:
9.7 mg/s – at phase C
5.0 mg/s – at phase E

## Slide 17
Interaction zone oxidation
Heat Generation during IZ and specimen oxidation (Stage E)
Reactions in the interaction zone:
Zr + O2 = ZrO2 + 1090 kJ
U + O2 = UO2 + 1060 kJ
2U + O2 = 2UO3 + 2360 kJ
Fe + O2 = FeO + 500 kJ
4Fe + 3O2 = 2Fe2O3 +1440 kJ
Heat of chemical reactions generated at stage E:
≈ 888 kJ
Corresponding average power of chemical reactions :
≈ 0.505 kW
Integral heat power to the specimen surface both from the melt and generated by chemical reactions ≈ 2.5 kW (0.76 MW/m2)
( 2 kW or 0.61 MW/m2 – from the melt,
0.5 kW or 0.15 MW/m2 – chemical reactions)
The IZ composition was determined using the MC6 test results

## Slide 18
Preliminary Conclusions
Posttest analysis is still underway, however the following notes can be made:
Under the conditions similar to those of molten suboxidized С-30 corium interaction with steel in MC6 test, the interaction zone depth in the USS sighting spot was deeper by approx. 1.4 mm and the incubation period shorter by approx. 6000 s before oxidation started in MCP-3
The oxidation rate and hydrogen generation rate measured during the pool oxidation regime were close to MA-9 test (MASCA program). The oxidation is controlled by steam supply to the molten pool surface
The interaction zone oxidation was realized In the most conservative regime (after complete oxidation of molten corium),
A partial melting of the steel surface layer in the end of the oxidation regime was caused by the increase in heat transfer from the melt (facility-specific factor) and additional heat generated by chemical reactions. The respective heat fluxes have been evaluated as 0.61 and 0.15 MW/m2

## Slide 19
Thermal and mechanical analyses of the VVER-1000 RPV in an IVR scenario considering corrosion effects

## Slide 20
Objectives
Evaluation of the influence of corrosion on the vessel integrity under the IVR conditions

## Slide 21
Corium pool configurations
Configuration 1: suboxidized pool
  segregated pool (metal and oxide layer)
  oxide mass: 64 t, metal mass: 116 t
  pool height 2.2 m (1 m + 1.2 m)
Configuration 2: fully oxidized pool
  homogeneous pool
  mass: 210 t
  pool height: 3.1 m

## Slide 22
Temperature fields and heat fluxes
segregated pool
homogeneous pool

## Slide 23
Analysis of four scenarios
A: segregated pool without corrosion
B: segregated pool with corrosion
C: homogeneous pool without corrosion
D: homogeneous pool with corrosion

## Slide 24
Final ablation
B
A
C
D
The effect of corrosion for the homogeneous pool is higher than for the segregated one

## Slide 25
Ablation kinetics
Abrupt changes are due to the computational grid discreteness

## Slide 26
Mechanical calculations
Elastic-plastic material behaviour
Material configuration: final ablation state
Temperature field from t = 300 s
Weight of vessel and melt pool
Increasing internal pressure until vessel failure
Failure criterion: allowable stress max (T)

## Slide 27
Stress at failure pressure (segregated pool)
A
B
Pa
Pa

## Slide 28
Stress at failure pressure (homogeneous pool)
C
D
Pa
Pa

## Slide 29
Main results - overview
Scenario | A | B | C | D
Pool configuration | segregated | segregated | homogeneous | homogeneous
Corrosion | no | yes (suboxidized corium) | no | yes (oxidized corium)
Ablated steel mass, t | 32.3 | 36.5 | 25.5 | 35.5
Min. wall thickness, mm | 60 | 50 | 100 | 70
Failure pressure, MPa | 13.81 | 13.80 | 19.33 | 19.11

## Slide 30
Allowable stress and characteristic temperatures
Tallow,cr
TB
Tliq

## Slide 31
Preliminary conclusions
Corrosion leads to a significantly higher vessel ablation
The effect of corrosion is more pronounced in the homogeneous (oxidized) pool
The segregated pool configuration is more critical due to the higher peak heat flux
The vessel strength is almost not influenced by corrosion
  load is borne by the cold outer region of the vessel wall

## Slide 32: Publications
  S.V. Bechta, V.S. Granovsky, V.B. Khabensky, E.V. Krushinov,
  S.A. Vitol, A.A. Sulatsky, V.V. Gusarov, V.I. Almiashev,
  D.B. Lopukh, D. Bottomley, M. Fischer, P. Piluso, A. Miassoedov,
  W. Tromm, E. Altstadt, F. Fichot, O. Kymalainen “Interaction
  between Molten Corium UO2+X - ZrO2- FeOy and VVER Vessel
  Steel” Proceedings of ICAPP ’08, Anaheim, CA USA, June 8-12,
  2008, Paper 8052
  S.V. Bechta, V.S. Granovsky, V.B. Khabensky, V.V. Gusarov,
  V.I. Almiashev, L.P. Mezentseva, E.V. Krushinov, S.Yu. Kotova,
  R.A. Kosarevsky, M. Barrachin, D. Bottomley, F. Fichot,
  M. Fischer “Corium Phase Equilibria based on MASCA,
  METCOR and CORPHAD Results”, Nuclear Engineering and Design 238 (2008), pp. 2761-2771

## Slide 33: Publications (2)
  S.V. Bechta, V.S. Granovsky, V.B. Khabensky, E.V. Krushinov,
  S.A. Vitol, V.F. Strizhov, D. Bottomley, M. Fischer, P. Piluso,
  A. Miassoedov, W. Tromm, E. Altstadt, H. G. Willschutz, F. Fichot,
  O. Kymalainen “VVER Steel Corrosion During In-Vessel
  Retention of Corium Melt” ERMSAR 2008 Conference Paper (In press)
  S.V. Bechta, V.S. Granovsky, V.B. Khabensky, E.V. Krushinov,
  S.A. Vitol, A.A. Sulatsky, V.V. Gusarov, V.I. Almiashev,
  D.B. Lopukh, D. Bottomley, M. Fischer, P. Piluso, A. Miassoedov,
  W. Tromm, E. Altstadt, F. Fichot, O. Kymalainen “VVER Vessel
  Steel Corrosion at Interaction with Molten Corium in Oxidizing
  Atmosphere” (in preparation)

## Slide 34
Organizational problem
Restrictions imposed by the Rosatom Export Control:
Export license is necessary
Partner should be found and results confidentiality should be confirmed
JRS ITU is ready to be the partner
An agreement on the conditions of providing project deliverables to the ISTC is currently negotiated between Rosatom and the ISTC