## Slide 1: Examination of the VVER fuel behavior under the severe accident conditions
A. Goryachev, I. Kuzmin, A. Leshchenko, V. Serebryakov
RIAR, Dimitrovgrad, Russia
Topical ISTC meeting July 02-04, 2007 Podolsk 1

## Slide 2
Flood temperature, °С Oxide film thickness, m | 1400 | 1600 | 1700
0 | 2 tests | 1 test | 1 test
100 | 2 tests |  | 
300 |  |  | 
tests performed in the frame of stage A Spent ROD-QUENCH Project “Examination of the VVER fuel behavior under the severe accidents. Reflooding stage "
Topical ISTC meeting July 02-04, 2007 Podolsk 2

## Slide 3: Tests with irradiated simulators quenched without pre-oxidation
Simulator #42 (65 MW·d/kgU)
Simulator was broken during post-test examinations
Topical ISTC meeting July 02-04, 2007 Podolsk 3

## Slide 4: Tests with irradiated simulators quenched without pre-oxidation
Simulator #46 (65 MW·d/kgU)
Simulator kept intact during post-test examinations
Simulator #45 (65 MW·d/kgU)
Simulator was broken during post-test examinations
Topical ISTC meeting July 02-04, 2007 Podolsk 4

## Slide 5: Tests with irradiated simulators quenched without pre-oxidation Gaseous Fission Product release
Simulator #46 (65 MW·d/kgU)
Simulator #45 (65 MW·d/kgU)
Topical ISTC meeting July 02-04, 2007 Podolsk 5

## Slide 6: Results of the irradiated simulator tests
Test # | 36 | 37 | 39 | 40 | 45 | 46
Fuel Burnup, MW·d/kgU | 54 | 54 | 65 | 65 | 65 | 65
Pre-oxidation (annealing) time at 1400 °C, s | 240 | 0 | 240 | 0 | 240 | 240
Simulator environment | steam-Ar | Ar | steam-Ar | Ar | Ar | Ar
Quench temperature, °C | 1400 | 1700 | 1400 | 1400 | 1600 | 1400
Maximum temperature during the quench, °C | 1407 | 1703 | 1428 | 1411 | 1604 | 1422
Oxide film thickness, μm | 111 | 19 | 92 | 9 | * | *
Outer  - Zr(O) layer thickness, μm | 186 | 31 | 126 | 23 | * | *
Inner  - Zr(O) layer thickness, μm | 170 | 337 | 122 | 90 | * | *
Metal layer thickness, μm | 607 | 648 | 614 | 674 | * | *
Total hydrogen production, mg | 164 ± 13 | 16.3 ± 1.3 | 173 ± 14 | 13.6 ± 1.1 | 20.6 ± 1.6 | 9.4 ± 0.6
Hydrogen production during the quench, mg | 6.7 ± 0.5 | 14.7 ± 1.2 | 7.0 ± 0.6 | 13.6 ± 1.1 | 20.6 ± 1.6 | 9.4 ± 0.6
* - to be measured
Topical ISTC meeting July 02-04, 2007 Podolsk 6

## Slide 7
Determination of FP release
Quench
tank
Ar carrier gas
Ar, 85Kr, Xe
g - detector
MFM
mass-spectrometer
Ar carrier gas
Gamma - spectrum
Gas flow rate
Xe concentration
85Kr and Xe release rate
85Kr activity
Topical ISTC meeting July 02-04, 2007 Podolsk 7

## Slide 8
(3)
 i – acquisition time of spectrum i, s;
Ii – average intensity
of 85Kr -line 514 keV, s-1;
Gi – average gas flow rate, cm3/s;
V – volume of the gas tube
on the -detector, cm3;
 – registration effectiveness;
 – 85Kr decay constant;
 – gamma yield per decay;
m – fuel mass in specimen, g.
Determination of 85Kr and Xe release during a test
(4)
J(t) – registered current, rel.un;
G(t) – registered gas flow rate, sccm/s;
K – calibration factor.
P 2
V 4
V 2
G 2
P 3
V 1
V 3
GPS 1
P 4
Ar + steam
V 7
V 6
R
R
G 1
P 1
G 7
V 8
C1
MFC 2
C2
GA
G 4
G 6
GPS 2
P 5
V 5
G 5
GFS
Ar
GFU
Quench tank
Steam generator

MS
dump
dump
MFM
gas mass flow meter
mass-spectrometer
Ge(Li) detector
dump
Gas lines system of test rig
Topical ISTC meeting July 02-04, 2007 Podolsk 8

## Slide 9
Determination of relative release of volatile FP
Relative method.
Test 36 (Burnup 54 MWd/kg U;
isothermal annealing: 1400°C, 240 s; quenching temperature 1400 °C)
Topical ISTC meeting July 02-04, 2007 Podolsk 9

## Slide 10
Determination of relative release of 85Kr and Cs
F85Kr - relative release of 85Kr;
 i – acquisition time of spectrum i, s;
Ii – average intensity of 85Kr -line 514 keV, s-1;
Gi – average gas flow rate, cm3/s;
FCs - relative release of Cs;
Si – photopeak area at the i coordinate.
Topical ISTC meeting July 02-04, 2007 Podolsk 10

## Slide 11
Determination of 85Kr and Xe content in the fuel
The content of 85Kr and Xe in the reference sample is assumed as the initial 85Kr specific activity Аref and initial specific volume of the xenon VXe ref and calculated on the basis of the results of the experiment on dissolution of the fuel reference sample.
fuel sample at moving bowl
mass flow meter
bubblers
mass spectrometer
Ar
TC
heater
dissolution device
filter
Ge(Li) - detector
mass flow controller
Hot cell
Rig for determination of FP content by fuel dissolution
MS

P 1
Ar
MS
MFM
MFC
dump
filter
Topical ISTC meeting July 02-04, 2007 Podolsk 11

## Slide 12
Determination of Cs relative release
The parameters determined :
volumetric activity and radionuclide composition in quench tank water;
- specific activity and radionuclide composition of the acid solution (reference fuel specimen or tested sample);
Relative error of activity determination is 9% (Р=0,95).
Test
solution
Volume measurement
Remote probe sampling
g - spectrometry
Probe
dilution
g - detector
134Cs, 137Cs activity
Topical ISTC meeting July 02-04, 2007 Podolsk 12

## Slide 13
Determination of Cs relative release
Relative method.
Assuming that 154Eu does not release from the fuel during the test it can be considered
that the areas of 154Eu photopeaks are proportional to the specimen masses
where Fi - relative release of Cs calculated by the i gamma line;
Si , SEu – photopeak area of the i gamma line and the one of 1274 keV 154Eu.
if Fi  9% then  Fi  100%
Cs relative release error
Topical ISTC meeting July 02-04, 2007 Podolsk 13

## Slide 14
FP release calculated using the dissolution results
Test | 36 |  | 37 | 39 |  |  | 40 |  | 
Burnup, МWd/kg U | 54 |  | 54 | 65 |  |  | 65 |  | 
Holding time at 1400°С, s | 240 |  | 240 | 240 |  |  | 0 |  | 
Maximal temperature, °C | 1400 |  | 1700 | 1400 |  |  | 1400 |  | 
85Kr release (on-line measurement), % | 18.1±4.0 |  | 31.8±3.2 | 8.4±4.5 |  |  | 4.1±4.5 |  | 
137Cs release calculated using -scanning data, % | 5 |  | - | 9 |  |  | 3 |  | 
Sample position along the simulator, mm | 90 | 22 | 96 | 131 | 95 | 11 | 136 | 84 | 19
85Kr release calculated by dissolution data, % | 18.8 ± 4.0 | 2,0 ± 5.0 | 42,3 ± 2.7 | 16,9 ± 4.1 | 12,7 ± 4.3 | 8,2 ± 4.5 | 9,9 ± 4.5 | 2,2 ± 4.8 | 2,3 ± 4.8
137Cs release calculated by dissolution data, % | 8,2 ± 9,2 | <2 | 37,8 ± 6,2 | 6.0 ± 9,4 | 5,4 ± 9,5 | 3,0 ± 9,7 | 7,5 ± 9,3 | <2 | <2
Measured 85Kr concentration in the reference samples: 54 МWd/kg U– 3.5 μl/g
65 МWd/kg U– 6.6 μl/g
Topical ISTC meeting July 02-04, 2007 Podolsk 14

## Slide 15
Test |  | 36 | 37 | 39 | 40 | 42* | 43** | 45 | 46
Burnup, МWd/kg U |  | 54 | 54 | 65 | 65 | 65 | 65 | 65 | 65
Holding time at 1400°С, s |  | 240 | 240 | 240 | 0 | 0 | 340 | 240 | 240
Maximal temperature, °C |  | 1400 | 1700 | 1400 | 1400 | 1600* | 1400 | 1600 | 1400
Total 85Kr release, μl STP |  | 37 ± 4 | 65 ± 8 | 33 ± 4 | 16 ± 2 | 29 ± 4 | - | 18 ± 2 | 11 ± 1
Total Xe release, ml STP |  | 12.9 ±1.3 | 34 ± 3.4 | 9.9 ± 1.0 | 4.9 ± 0.5 | 15.4 ±1.6 | - | in the progress | in the progress
Relative 85Kr release, % |  | 18.1 ±4.0 | 31.8 ±3.2 | 8.4 ±4.5 | 4.1 ±4.5 | 7.4 ±4.5 | - | 5.1 ±4.5 | 3.1 ±4.6
Relative 85Kr release from simulator central part (dissolution data), % |  | 18.8 ±4.0 | 42,3 ±2.7 | 12,7 ±4.3 | 2,2 ±4.8 |  |  |  | 
Cs release to the cooling tank water, % | 137Cs | 0.6 ±0.2 | 1.2 ±0.3 | 1.3 ±0.3 | 0.6 ±0.2 | 0.8 ±0.2 | 1.2 ±0.3 | 0.9 ±0.2 | in the progress
 | 134Cs | 0.5 ±0.2 | 1.0 ±0.2 | 1.2 ±0.3 | 0.6 ±0.2 | 0.9 ±0.2 | 1.2 ±0.3 | 0.9 ±0.2 | in the progress
Simulator test parameters and FP release
Topical ISTC meeting July 02-04, 2007 Podolsk 15

## Slide 16
Conclusions
Topical ISTC meeting July 02-04, 2007 Podolsk 16
Small progress in tests performance have been achieved after repair of installation.
Data on volatile FP content in samples of initial fuel are obtained
Tests with dissolution of the initial and tested samples have shown that the used method can be applied to the simulators tested at temperatures of 1700 оС. At lower temperatures (1400 оС) the error exceeds the result