Final results of the ISTC project #3831 Development and experiments at large-scale installation for heating and retention of corium

# 1. The preparation of the medium scale MCCI experiment

1.1 Concrete tank

Depth of the walls and bottom of the tank – 100 mm;

inner diameter – 400 mm;

depth – 480 mm.

Concrete tank was located in the steel cylindrical container (diameter – 800 mm) and was surrounded by the sand layer (Fig. 1).

Figure 1 – Concrete tank for corium

1.2  Pyrotechnic compound and PTC briquettes

50 kg of poured PTC;

432 single briquettes (d=50 mm, h=20mm, m=120g, ρ=3.05g/cm3) with the 	total mass of 52 kg;

72 operational briquettes (consisted of 6 single briquettes, wrapped into aluminum foil, Fig. 2);

mass of an operational briquette – 720 g;

length of an operational briquette – 120 mm;

energy release of each operational briquette ~2MJ.

Figure 2 – Operational PTC briquettes

1.3   Initiation of PTC

Initiation of PTC by means of electric igniter and the system of 4 gas burners;

the system of 4 gas burners were used for additional heating of corium during the medium scale experiment;

thermal protection of the burners was achieved by means of asbestos (Fig. 3).

Figure 3 – Concrete tank for corium, filled up with poured PTC

1.4 System of dumping PTC briquettes and experimental installation overview

For dumping operational PTC briquettes into corium we used a steel chute:

inner diameter – 80 mm;

length – 520 m;

located an angle of ~600 to horizon.

The upper end of the chute was 610 mm above the installation with corium. The chute was pointed into the bottom center of the tank. The experimental scheme and experimental installation overview are shown in the Fig. 4, 4a and 4b.

Figure 4 – The experimental scheme

Camera 1 disposition

Figure 4a – Medium scale experimental installation overview

Camera 2 disposition

Figure 4b – Medium scale experimental installation top view

1.5 Temperature measurement system

The system for the diagnosis of temperature was developed and installed (34 thermocouples) into the concrete tank for the medium scale experiment. The scheme of the disposition of thermocouples in the bottom and in the sidewalls of the concrete tank is shown in Fig. 5.

22 thermocouples (Type-K) were disposed into the bottom of the concrete tank at the depths of:

5 mm – 3 units;

10 mm – 5 units;

15 mm – 3 units;

20 mm – 5 units;

30 mm – 4 units.

2 thermocouples (W-Re) were disposed at the bottom surface (0 mm).

12 thermocouples (Type-K) were disposed into the walls of the concrete tank at the depths of:

5 mm – 6 units;

15 mm – 2 units;

20 mm – 2 units;

25 mm – 2 units.

Briquette landing zone

Beam 3

Beam 2

Beam 1

Figure 5 – The disposition of 34 thermocouples in the middle scale experiment.

The coordinates of the thermocouples are shown in Tab. 1. The radial reference point is the axis of symmetry of the cylindrical concrete tank, the altitudinal reference point is the initial position of the bottom of the cylindrical concrete tank.

Table 1 – The coordinates of the thermocouples

| № | Radius | Height | Color | Walls |
| --- | --- | --- | --- | --- |
| 1 | (200)+5 | +55 | red | 1 Beam |
| 2 | (200)+15 | +55 | green | 1 Beam |
| 3 | (200)+5 | +40 | red | 1 Beam |
| 4 | (200)+15 | +40 | green | 1 Beam |
| 5 | (200)+5 | +55 | red | 2 Beam |
| 6 | (200)+25 | +55 | blue | 2 Beam |
| 7 | (200)+5 | +40 | red | 2 Beam |
| 8 | (200)+25 | +40 | blue | 2 Beam |
| 9 | (200)+5 | +55 | red | 3 Beam |
| 10 | (200)+20 | +55 | cyan | 3 Beam |
| 11 | (200)+5 | +40 | red | 3 Beam |
| 12 | (200)+20 | +40 | cyan | 3 Beam |
|  | Radius | Depth | Color | Bottom |
| 13 | 180 | -30 | violet | 1 Beam |
| 14 | 140 | -20 | cyan | 1 Beam |
| 15 | 135 | -10 | orange | 1 Beam |
| 16 | 100 | -15 | green | 1 Beam |
| 17 | 65 | -20 | cyan | 1 Beam |
| 18 | 60 | -10 | orange | 1 Beam |
| 19 | 20 | 0 | black | W-Re 1 Beam |
| 20 | 0 | 0 | black | W-Re |
| 21 | 20 | -15 | green | 2 Beam |
| 22 | 60 | -30 | violet | 2 Beam |
| 23 | 65 | -10 | orange | 2 Beam |
| 24 | 100 | -5 | red | 2 Beam |
| 25 | 135 | -30 | violet | 2 Beam |
| 26 | 140 | -10 | orange | 2 Beam |
| 27 | 180 | -20 | cyan | 2 Beam |
| 28 | 20 | -10 | orange | 3 Beam |
| 29 | 60 | -20 | cyan | 3 Beam |
| 30 | 65 | -5 | red | 3 Beam |
| 31 | 100 | -30 | violet | 3 Beam |
| 32 | 135 | -20 | cyan | 3 Beam |
| 33 | 140 | -5 | red | 3 Beam |
| 34 | 180 | -15 | green | 3 Beam |
| 35 | 100 | 0 |  | Light guide |
| 36 | 100 | 0 |  | Light guide |
| 37 | 100 | 0 |  | Light guide |

To measure the corium-concrete surface temperature 3 quartz light guides (of 400 mkm in diameter put into the steel pipes of 4 mm in diameter) were mounted into the concrete tank (Fig. 6). To register corium surface thermal radiation a four-channel pyrometer was developed. As photodetectors photoelectronic multipliers (PEM) Hamamatsu R1925A were used. PEM load resister output current flows to the input of a registrator (oscilloscope, analog-digital converter).

Figure 6 – Ends of the light guides at the bottom of the concrete tank

1. The medium scale MCCI experiment

1. To ignite and create the initial molten pool 50 kg of poured PTC were put into the concrete tank. The volume of poured PTC ≈ 55 l.

2. The experiment started with the initiation of poured PTC by means of electric igniter. Four propane-oxygen burners started operating simultaneously with the igniter. The temperature of the gaseous burning products above corium surface is ~2000 C. These products create thermal isolation “cap” above corium.

3. After ignition of poured PTC inside the tank a combustion took place during 30 s. In 40 s after the ignition briquette dumping with time space 5÷30 s was started. The last two briquettes were dumped into corium with time spaces of 10 and 30 s respectively.

4. The average PTC drop rate was ~7 s. Total time from ignition till last briquette dumping was about 520 s.

5. The average energy release power inside the melt during the briquette dumping was about 280 kW that equals to the combustion of 100 g/s of PTC.

6. The velocity of the briquettes while impacting with the corium surface was ~8 m/s. The briquettes fully penetrated the corium surface and moved into the center of the melt, where the energy release took place and provided good melt mixing. It’s needed to mention that the briquettes didn’t fall accurately into the center of the melt but impacted with the offset to the sidewall (in the area of the light guide №35 in Fig. 5).

7. During the experiment (while the briquettes were dumped) no solid crust (or its fragments) formation was noticed.

8. Carried out medium scale MCCI experiment was recorded by 2 video cameras (Fig. 4). Camera 1 was located at the same height with the concrete tank at the distance of ~8 m (Fig. 4b). Camera 2 was located at 3.5 above the concrete tank put 1 m aside its axis; the recording was made with the help of a mirror (disposed at an angle of 45 deg to the horizon above the tank, Fig.4 and 4a).

3. Medium scale MCCI experimental results

3.1 Frozen corium ingot

After the medium scale experiment molten corium froze and formed a cylindrical “tablet” with the following parameters (Fig. 7-10):

- tablet diameter ~450 mm;

- tablet thickness ~160 mm;

- tablet volume ~ 25 l;

- tablet mass ~ 105 kg;

- tablet density ~4.2 g/cm3.

At the bottom and around the tablet a stuck concrete crust can be clearly seen. The tablet is of grey color and consists mainly of ZrO2 and Fe and possibly of partially unreacted Fe2O3 reactant. Iron seems to be well distributed in the volume of tablet since a magnet was attracted by all sides of the tablet. Components of thermal decomposition of SiO2 and CaO are supposed to be inside too.

Figure 7 – Frozen tablet. Bottom view

Figure 8 – Frozen tablet. Top view. Tablet diameter is ~450 mm.

Figure 9 – Frozen tablet. Side view. Tablet thickness ~160 mm.

Figure 10 – Tablet mass ~105 kg

3.2 Concrete and frozen tablet fragments

In ~20 hours after the medium scale MCCI experiment the steel container, preserved the concrete tank with the frozen tablet of corium and corium crust at the concrete sidewalls was cut with the help of a gas burner.

The concrete tank immediately crumbled into fragments with characteristic size of ~5–30 cm (Figures 11 and 12). Corium (localized as crust at the inner walls of the concrete tank) also crumbled.

The thickness of corium, localized due to the splashes at the inner sidewalls of the concrete tank is ~10–30 mm, its mass ≈23kg, volume ≈8 L.

Moreover, during the experiment some part of corium in a form of liquid droplets flew out of the tank and fell onto the ground near the installation, its mass is ≈2 kg, volume ≈1 L.

Thus, the total corium mass away from the tablet is ~25 kg, volume ≈9 L.. Its compound is apparently close to that of the tablet.

Figure 11 – Fragments of the bottom and the sidewalls of the concrete tank

Figure 12 – “Tablet” of corium with the remains of corium crust on it (localized at the inner sidewalls of the concrete tank). Fragments of the sidewalls in the upper part of concrete tank.

Figure 13 – The final state of corium and concrete tank

The process of crumbling the concrete walls in radial direction was ~25 mm, in axial direction – 20-30 mm. The area of the bottom where the briquettes fell down was more ablated (Fig. 5). The fragment of the area of maximum ablation is shown in Fig. 14.

It’s needed to mention a red color ring shaped zone that borders with the tablet of corium (Fig. 11). The inner diameter of this zone is ~450 mm, its width ~30 mm. Apparently it is a result of corium-concrete interaction.

Figure 14 – Bottom thickness after the experiment in the area of PTC combustion ~70 mm

3.3 Mass balance of PTC constituents and concrete

The mass of initial reactants for PTC reaction was 102 kg. Another ~1 kg was formed by aluminum used for PTC cylinder wrapping. Thus, the total mass of the reactants was ~103 kg.

The products of PTC reaction were the tablet of corium, which mass was 105 kg and the fragments of corium (with mass ~25 kg) that was found outside the tablet. Thus, the total mass of reaction products was ~130 kg.

As follows from above the mass of concrete, crumbled during the experiment was ~27 kg (here we neglect the mass of gaseous products of thermal destruction of concrete).

In Fig. 15a top view of a fragment of corium tablet is shown where a piece of tablet was mechanically removed to carry out the investigation of vertical cut. In Fig. 15b is shown a zoomed in view of the removal zone.

/a/							   /b/

Figure 15 – Corium tablet with removal zone

In Fig. 16a and 16b are shown the zoomed in fragments of the tablet vertical cut. From these figures it can be seen that the tablet inside is a grey porous mass with specks of white and yellow color. Apparently, the yellow fragments are iron oxides and the white ones – the products of concrete thermal destruction (SiO2 и CaO). Observing the cut surface profile we can make a conclusion that the distribution of iron, Zr oxide and concrete thermal destruction products inside the tablet is quite uniform. The bottom zone of the tablet is evidently the iron layer of 2-3 mm thickness.

Figure 16a – Tablet vertical cut

Figure 16b – Zoomed in view of the vertical cut in the upper tablet surface zone

4. Temperature registration and thermal flux estimation

4.1. A method of temperature registration by means of thermocouples

In the experiment we used 34 thermocouples, placed in three rays at 120 deg. to each other. The disposition scheme is shown in Fig. 5.

Two thermocouples №№ 19 & 20 were of W-Re and the junction was mounted at the corium-concrete contact surface. Other thermocouples – Type K – were mounted at different distances from corium-concrete surface in the bottom (№№ 13-34) and inside the concrete sidewalls (№№1-12).

Type K thermocouples used in a measurement system along with the special 4-channel temperature detectors “CENTER-309”, calibrated up to 13700 C. Such detector was used with W-Re thermocouple №20. In this case to convert data from detector to temperature we used well known calibration functions of thermal EMF versus Temperature for W-Re and Type-K thermocouples.

The other W-Re thermocouple (№19) used to directly measure thermal EMF using an oscilloscope Agilent. To interpret the measurements to temperature we used the well known data.

The results of corium temperature measurements by means of thermocouples are shown in Fig. 17.

Figure 17 – Bottom temperature (depth 0 mm) (W-Re thermocouples №№19-20)

Thermocouple № 20 provided 1 measurement in 3 seconds;

Thermocouple №19 provided 4 measurements in 1 second;

ТAV = 2440 С was calculated by averaging data recorded by t/c №19.

It should be mentioned that both W-Re thermocouples №№ 19 and 20 survived not only in concrete but also in the molten corium.

4.2 A method of temperature measuring by means of pyrometry

The pyrometric detector is made up by a tube  (stainless steel,  6х1), with a quartz lightguide located inside ( 400 mkm). The upper end of a tube, located at a corium-concrete surface, is covered with a cap of foil (Mo, Ta) - 50 mkm thick. Due to the fragility of a W foil we used a plate instead (100 mkm thick). The distance from the end of a light guide to the foil is chosen so that the radius of sight of a light guide equals to the whole foil surface. The scheme of optical detectors is shown in Fig. 5 (№№ 37-39).

The results of temperature measurements by means of optical method are shown in Fig. 18-18b. The lifetime of optical detectors was ~60 s. Apparently, it is connected with the destruction of steel tubes (Tmelt=1700 C), forming the basis of detectors.

Temperature (K)

Time (s)

W (100 mkm)

Figure 18 – Corium temperature, measured my means of the optical 	method

Temperature (K)

Time (s)

Mo (50 mkm)

Figure 18a – Corium temperature, measured my means of the optical method

Temperature (K)

Time (s)

Ta (50 mkm)

Figure 18b – Corium temperature measured by means of the optical method

The magnitudes of temperatures, measured by means of the optical method satisfactorily agree with the data, obtained by means of W-Re thermocouples.

4.3 Experimental results, obtained by means of Type K thermocouples

Of 34 thermocouples mounted into the concrete tank only 28 provided reliable measurements: 2 W-Re and 26 of Type K. The duration of measurement interval was ~30 min (except thermocouple №19).

In Fig. 19–23 are shown temperatures, measured by Type K thermocouples, disposed in the bottom of concrete tank at different depths and radiuses (Fig. 5 and Table 1).

Figure 19 – Bottom temperature (depth 5 mm)

When the temperature to be measured exceeded 1370 C (maximum Type K detector calibrated temperature) the measuring temperature remained 1370 C. It is clearly seen that since the moment of the thermal (ablation ?) wave arrival (40-50 s) and until the final moment of measuring the temperature at the depth of 5 mm in the whole bottom area exceeded 13700 C.

Figure 20 – Bottom temperature (depth 10 mm)

It is to be mentioned that Type K thermocouples №№26, 23 and 28 as corium (in which they were since the arrival of the thermal (ablation ?) wave) cooled down to the temperature lower than 13700 C started working.

It can be seen that since the moment of arrival of the thermal (ablation ?) wave (50-60 s) and until the final moment of measurement the temperature of thermocouple №18 (it is the closest to the area where the briquettes arrived) exceeded 13700 C. The temperature of the thermocouples №№ 26, 23, 28, disposed farther from that area, at different moments of time (~12, ~17 and ~22 min respectively) became lower than 13700 C. Moreover the process of cooling down started in the most distant areas from the briquette landing zone.

№34

Figure 21 – Bottom temperature (depth 15 mm)

It is clearly seen that since the moment of arrival of the thermal (ablation ?) wave (60-80 s) and up to ~7 min the temperature of thermocouples № 21 and 34 exceeded 13700 C. Further process of cooling down was more intensive in the most distant areas from the briquette landing zone.

The temperature of t/c №16 that was the closest to the landing zone became ~12000 C by the moment of ~25 min. The temperature of this t/c decreased considerably slower and by the moment of ~30 min its temperature reached the magnitude of 12000 C.

Figure 22 – Bottom temperature (depth 20 mm)

It is to be mentioned that Type K thermocouples №№ 27, 29 and 32 were operating during the whole experiment and their temperature never exceeded 1370 C.

It is seen that since the moment of arrival of ablation wave and the temperature growth (~80-120 s) the cooling down of thermocouples №№ 27, 29 and 32 was the slower the farther was the t/c from the center of the bottom.

Figure 23 – Bottom temperature (depth 30 mm)

It is to be mentioned that Type K thermocouples №№ 13, 22, 25 and 31 (as the thermocouples at the depth of 20 mm) were operating during the whole experiment.

It is seen that since the moment of arrival of ablation wave and the temperature growth (~120 s) the growth of the temperature, measured by thermocouples №№ 13, 22, 25 and 31 was the faster the closer was the t/c from the briquette landing zone.

In Fig. 24 are shown the temperatures, measured in the concrete sidewalls at the depth of 5 mm and at the height of 40 mm above the bottom (Fig. 5 and Table 1).

Figure 24 – Wall temperature (depth 5 mm; height 40 mm)

It is obvious that since the moment of arrival of the thermal (ablation ?) wave (~60 s) and up to the beginning of the cooling down (10-12 min) the temperature of thermocouples № 3, 7 and 11 exceeded 13700 C. Further process of cooling down of these thermocouples was slow and acted as a weak function of distance from the landing zone.

In Fig. 25 are shown the temperatures, measured in the concrete sidewalls at the depth of 5 mm and at the height of 55 mm above the bottom.

Figure 25 – Wall temperature (depth 5 mm; height 55 mm)

It is clearly seen that since the moment of arrival of ablation wave (~50-70 s) and up to the beginning of the cooling down (~10, ~13 and ~18 min respectively) the temperature of thermocouples №№ 5, 9 and 1 exceeded 13700 C. Further process of cooling down was the slowest at the area of disposition of t/c № 1 that was the closest to the landing zone (Fig. 5).

In Fig. 26 are shown the temperatures, measured in the concrete sidewalls at the depths of 15, 20 and 25 mm and at the height of 40 mm above the bottom.

Figure 26 – Wall temperature (depths 15 mm, 20 mm, 25 mm; height 40 mm)

It is seen that since the moment of temperature growth (~60-70 s) t/c №4 was heated faster than the others (it was the closest to the landing zone). The temperature growth of the t/c № 12 (until the moment of ~12 min) was the slowest because the thermocouple was the farthermost from the landing zone.

In Fig. 27 are shown the temperatures, measured in the concrete sidewalls at the depths of 15, 20, 25 mm and at the height of 55 mm above the bottom.

Figure 27 – Wall temperature (depths 15 mm, 20 mm, 25 mm; height 55 mm)

It can be seen that since the moment of temperature growth (~60-70 s) t/c №2 was heated faster than the others (it was the closest to the landing zone). After the moment of ~15 min the cooling of thermocouples №№ 2, 10 and 6 was slow and acted as a weak function of distance from the briquette landing zone.

4.4 Estimation of heat fluxes into the concrete crucible

4.4.1 Heat fluxes into the crucible bottom

To estimate the heat fluxes into the bottom of concrete crucible t/c pairs №23-№22 (∆r=5 mm, ∆z=20 mm), №26-№25 (∆r=5 mm, ∆z=20 mm), №20-№21 (∆r=20 mm, ∆z=15 mm). These t/c pairs are closely similar to each other at the radius of disposition thus the temperature difference between them allows to make the most precise estimation of the temperature gradient by the depth (z-Axis) among the number of available thermocouples.

It is to be mentioned that between the points using which we calculate the temperature gradients is found an area of complicated foliated structure: corium+buffer zone+uncrumbled concrete. The state and structure of the buffer zone is hard to estimate due to the lack of information about its temperature (insufficient amount of W-Re thermocouples!). Thus, summarizing the information of carried out medium-scale experiment, it is hard to calculate the thermal conductivity of the buffer zone and, as a consequence, to precisely calculate heat fluxes along the whole foliated area. Thus we made not an accurate calculation but a rather rough estimate from below of heat fluxes into the bottom of concrete crucible. “From below” means that the real magnitudes of the heat fluxes are higher (probably sufficiently higher) than the carried out estimate.

Apparently, among the contents of the foliated area (corium+buffer zone+uncrumbled concrete) it is uncrumbled concrete that has the lowest coefficient of heat conductivity. While making an estimate of heat fluxes from below we use for the whole foliated area the magnitude of that of uncrumbled concrete. We will use the formula for the coefficient of heat conductivity λ(T) provided in a courteous manner by Dr. Christophe Journeau that can be written as:

For     T ≤ 470 K:                           λ = 2,352 – 2,75.10-3 × T    (W.m-1.K-1),

For     470K ≤ T:                           λ = 0,7352 + 6,9.10-4 × T    (W.m-1.K-1).	(1)

To estimate heat fluxes between thermocouples №23 (z=10 mm)-№22 (z=30 mm) we will take the magnitude of λ(T) that corresponds to the average bottom temperature at the depth of z=20 mm (in the middle by the depth between the thermocouples). As can be seen from Fig 22 since the moment of ~200 s as the average temperature of Т≈8500С (≈11000К) can be taken with good accuracy. According to (1) the magnitude of λ23-22(T) ≈ λ26-25(T)  for this temperature is λ (1100) ≈1.49 (W.m-1.K-1).	To estimate heat fluxes between the thermocouples №20 (z=0 mm)-№21(z=15 mm) we’ll take the magnitude of λ(T), corresponding to the temperature of t/c №21, since the moment of ~7 min (the beginning of reliable temperature measurements by t/c №21, Fig. 21). With good accuracy the average temperature of Т≈12500С (≈15000К) can be taken, Fig. 21. According to (1), the magnitude of λ20-21(T) for this temperature is λ(1500) ≈1.77 (W.m-1.K-1).

In Figure 28 are shown the estimates from below of heat fluxes q [kW·m-2] into the crucible bottom.

Figure 28 – Estimated magnitudes of heat fluxes into the crucible bottom [kW·m-2]

It is seen that the magnitude of heat flux q, calculated by means of thermocouples №№20-21, is 150-180 kW·m-2 during the time interval of 100–1500 s.

It is seen that the magnitude of heat flux q, calculated by means of thermocouples №№23–22 and №№26–25, is 70-100 kW·m-2 during the time interval of 100–1000 s.

We need to underline once more that the shown in Fig. 28 magnitudes of the heat fluxes into the crucible bottom are not precise but estimated. And the estimation made from below thus the real magnitudes of the heat fluxes are higher that the estimated.

4.4.2 Heat fluxes into the sidewalls

To estimate the heat fluxes into the crucible sidewalls we use pairs of thermocouples, located (Fig. 5 and Table 1):

- on Beam 1: №1-№2   (∆r=10 mm, z=55 mm), №3-№4 (∆r=10 mm, z=40 mm),

- on Beam 2: №5-№6   (∆r=20 mm, z=55 mm), №7-№8 (∆r=20 mm, z=40 mm),

- on Beam 3: №9-№10 (∆r=15 mm, z=55 mm), №11-№12 (∆r=15 mm, z=40 mm).

These t/c pairs are disposed along the radius r and at the same height z, thus the temperature difference between them allows to rather precisely estimate the temperature gradient into the depth of the sidewalls (by r).

In Fig 29-31 are shown magnitudes of thermal fluxes in the crucible sidewalls. The magnitude of thermal conductivity coefficient for thermal flux calculation was taken by averaging those coefficients for every t/c in pair.

(=1.87 W·m-1·K-1)

(=1.87 W·m-1·K-1)

Figure 29 – Estimated values of thermal fluxes into the concrete sidewalls between the depths of 5 mm and 15 mm [kW∙m-2]

(=1.74 W·m-1·K-1)

(=1.53 W·m-1·K-1)

Figure 30 – Estimated values of thermal fluxes into the concrete sidewalls between the depths of 5 mm and 20 mm [kW∙m-2]

(=1.53 W·m-1·K-1)

(=1.74 W·m-1·K-1)

Figure 31 – Estimated values of thermal fluxes into the concrete sidewalls between the depths of 5 mm and 25 mm [kW∙m-2]

Conclusions

#### 1. The middle-scale experiment with characteristics: corium volume ≈34 kg (tablet volume ≈25 L), corium mass ≈130 kg (tablet mass ≈105 kg), corium temperature ~2500-3000C, heat fluxes towards walls and a bottom of a tank ~100-200 kw/m2, melt retention time ~15 min was made.

#### 2. Designed during the Project pyrotechnic technology of receiving and retention of corium can be used to carry out the large-scale experiment with the following characteristics: corium volume ~100-150 L, corium mass ~1000-1200 kg, corium temperature ~2500-3000C, heat fluxes towards walls and a bottom of a tank ~100-150 kw/m2, corium internal energy release time 1-2 hours.