## Slide 1: Status of METCOR-P ISTC project #3592
Presented by V. Khabensky
4th METCOR-P project meeting
June 1, 2010, St. Petersburg, Russia
International Science and Technology Center
A.P. Alexandrov Research Institute of Technology

## Slide 2: METCOR-P project general information
Project participants and coordination
ISTC, Moscow
FZK, Germany
JRC ITU,
EU
CEA,
France
Collaborators
Steering committee
Operation Agent: A.P. Alexandrov RIT, Russia
Coordinator
AREVA NP, Germany
SPb Technological University, Russia
SPb Electrotechnical State University, Russia
FORTUM, Finland
Investigation of Corium Melt Interaction with NPP Reactor Vessel Steel (#3592 METCOR-P)

## Slide 3
Objectives of METCOR-P project
Qualification and quantification of physicochemical phenomena of corium melt interaction with reactor vessel steel with particular interest to:
Interaction at the vertical position of vessel steel specimen surface
European vessel steel specimen behavior
Oxidation effects

## Slide 4: Experimental matrix for the METCOR-P project

## Slide 5: Revisions of experimental matrix and test sequences in accordance with decisions of the 1st , 2nd and 3rd project meetings and later discussions
Task 1.2: First test is MCP-1«Interaction of molten corium with vertically positioned vessel steel specimen in the neutral atmosphere»
Task 1.1: Replace a reference test with MCP-2 «Interaction of molten corium UO2+x-ZrO2 with horizontally positioned vessel steel specimen in the steam atmosphere»
Task 1.3: Conduct experiment «Interaction of molten corium Fe-U-Zr-Gr-Ni-O with vertically positioned vessel steel specimen in the Ar atmosphere» after improving the system of on-line measurements of corrosion kinetics, МСР-1 posttest analysis and RASPLAV generator capacity increase
Task 2.1: After МСР-2 conduct MCP-3«Interaction of suboxidized corium melt with steel at the replacement of neutral atmosphere with steel»

## Slide 6: Update of experimental matrix and experimental sequence in accordance with decisions of the 1st , 2nd and 3rd project meetings and later discussions (2)
Task 3.2: In MCP-4 «Interaction of molten corium with European vessel steel in oxidizing atmosphere (air)» combine two studies in one experimental procedure: steel corrosion kinetics at its interaction with two corium compositions - UO2-ZrO2 and UO2+x-ZrO2 -FeOy in the 9001200ºС temperature range
Task 3.1: Conduct MCP-5 «Interaction of suboxidized corium melt with European vessel steel» after МСР-4, as planned in the initial Work plan matrix
Task 2.3: Conduct МСР-6 «Oxidation kinetics of metallic melt containing U and Zr, when Ar atmosphere is replaced by steam» with a metallic melt corresponding to the С 30 + 40% system of stainless steel in a one-layer pool
Tasks 2.2 and 1.2: Prepare detailed procedures of two remaining tests for the 4th project meeting

## Slide 7: METCOR-P experimental matrix (2)
- tests carried out before 3rd meeting; - tests carried out after 3rd meeting

## Slide 8: Tests and reporting
Test | Name | Stage | Deliverables
МСР-1 | Interaction of molten corium with vertically positioned vessel steel specimen in the neutral atmosphere | Completed | Report Sent to ITU
МСР-2 | Interaction of molten corium UO2+x-ZrO2 with horizontally positioned vessel steel specimen in the steam atmosphere (Instead of reference test) | Completed | Report Sent to ITU
МСР-3 | Interaction of suboxidized corium melt with steel at the replacement of neutral atmosphere with steam | Completed | Report Sent to ITU

## Slide 9: Tests completed within METCOR-P (2)
Test | Name | Stage | Deliverables/status
МСР-4 | Interaction of molten corium with European vessel steel in oxidizing atmosphere (air) | Completed | Report (ready in Russian version)
МСР-5 | Interaction of suboxidized molten corium with European vessel steel | Completed | Posttest analysis in progress
МСР-6 | Oxidation kinetics of metallic melt containing U and Zr, when Ar atmosphere is replaced by steam | In preparation | -

## Slide 10: METCOR publications
Bechta S.V., Khabensky V.B., Vitol S.A. et al. Experimental Study of Oxides Corium Interaction with Reactor Vessel Steel Samples // RASPLAV Seminar 2000, Munich, Germany, 14-15 Nov., 2000.
Bechta S.V., Khabensky V.B., Vitol S.A. et al. Experimental studies of oxidic molten corium – vessel steel interaction / Nucl. Eng. Design 210, (2001) 193-224.
Bechta S.V., Khabensky V.B., Granovsky V.S., Krushinov E.V., Vitol S.A., Gusarov V.V., Almjashev V.I., Lopukh D.B., Tromm W., Bottomley D., Fischer M., Gornet G., Kymalainen O. New Experimental Results on the Interaction of Molten Corium with Reactor Vessel Steel // Proceeding of ICAPP’04, Pittsburgh, P.A. USA, June 13-17, 2004, Paper 4114.
Bechta S.V., Khabensky V.B., Granovsky V.S., Krushinov E.V., Vitol S.A., Gusarov V.V., Almjashev V.I., Mezentseva L.P., Petrov Yu.B., Lopukh D.B., Fischer M., Bottomley D., Tromm W., Barrachin M., Altstadt E., Piluso P., Fichot F., Hellmann S., Defoort F. CORPHAD and METCOR ISTC projects // The first European Review Meeting on Severe Accident Research (ERMSAR-2005), Aix-en-Provence, France, 14-16 November, 2005.

## Slide 11: METCOR publications (2)
Bechta S.V., Khabensky V.B., Vitol S.A., Krushinov E.V., Granovsky V.S., Lopukh D.B., Gusarov V.V., Martinov A.P., Martinov V.V., Fieg G., Tromm W., Bottomley D., Tuomisto H. Corrosion of vessel steel during its interaction with molten corium. – Part 1: Experimental // Nucl. Eng. Des., 236 (2006) 1810-1829.
Bechta S.V., Khabensky V.B., Vitol S.A., Krushinov E.V., Granovsky V.S., Lopukh D.B., Gusarov V.V., Martinov A.P., Martinov V.V., Fieg G., Tromm W., Bottomley D., Tuomisto H. Corrosion of vessel steel during its interaction with molten corium. – Part 2: Model development // Nucl. Eng. Des., 236 (2006) 1362-1370.
Bechta S.V., Khabensky V.B., Granovsky V.S., Krushinov E.V., Vitol S.A., Gusarov V.V., Almjashev V.I., Lopukh D.B., Tromm W., Bottomley D., Fischer M., Piluso P., Miassoedov A., Altstadt E., Willschufz H.G., Fichot F. Experimental Study of Interaction Between Suboxidized Corium and Reactor Vessel Steel // Proceeding of ICAPP’06, Reno, P.A. USA, June 4-6, 2006, Paper 6054.

## Slide 12: Publications during METCOR-P
Bechta S.V., Granovsky V.S., Khabensky V.B., Krushinov E.V., Vitol S.A., Sulatsky A.A., Gusarov V.V., Almjashev V.I., Lopukh D.B., Bottomley D., Fischer M., Piluso P., Miassoedov A., Tromm W., Altstadt E., Fichot F., Kymalainen O. Interaction between Molten Corium UO2+x-ZrO2-FeOy and VVER Vessel Steel // Proceeding of ICAPP’08, Anaheim, CA USA, June 8-12, 2008, Paper 8052.
Bechta S.V., Granovsky V.S., Khabensky V.B., Krushinov E.V., Vitol S.A., Sulatsky A.A., Gusarov V.V., Almjashev V.I., Mezentseva L.P., Krushinov E.V., Kotova S.Yu., Kosarevsky R.A., Barrachin M., Bottomley D., Fischer M., Fichot F. Corium Phase Equilibria from MASCA, METCOR and CORPHAD Results // Nucl. Eng. and Design, 238, p. 2761-2771 (2008).
3. Bechta S.V., Granovsky V.S., Khabensky V.B., Krushinov E.V., Vitol S.A., Strizhov V.F., D.B., Bottomley D., Fischer M., Piluso P., Miassoedov A., Tromm W., Altstadt E., Willschutz H.G., Fichot F., Kymalainen O. VVR Steel Corrosion during In-Vessel Retention of Corium Melt // Proceeding of the 3rd European Review Meeting on Severe Accident Research (ERMSAR 2008), Paper 2.7, Nesseber, Bulgaria, September 23-25 (2008).

## Slide 13: Publications during METCOR-P (2)
4. Bechta S.V., Granovsky V.S., Khabensky V.B., Krushinov E.V., Vitol S.A., Sulatsky A.A., Gusarov V.V., Almjashev V.I., Lopukh D.B., Bottomley D., Fischer M., Piluso P., Miassoedov A., Tromm W., Altstadt E., Fichot F., Kymalainen O. VVER Vessel Steel Corrosion at Interaction with Molten Corium in Oxidizing Atmosphere // Nucl. Eng. and Design, 239 (2009), p. 1103-1112
5. Bechta S.V., Granovsky V.S., Khabensky V.B., Krushinov E.V., Vitol S.A., Sulatsky A.A., Gusarov V.V., Almjashev V.I., Lopukh D.B., Bottomley D., Fischer M., Piluso P., Miassoedov A., Tromm W., Altstadt E., Fichot F., Kymalainen O. Interaction between Molten Corium UO2+x-ZrO2-FeOy and VVER Vessel Steel // J. Nucl. Technology , vol. 170, APR 2010, p. 210-218.

## Slide 14: Publications during METCOR-P (3)
6. Granovsky V.S., Khabensky V.B., Bechta S.V., Vitol S.A., Krushinov E.V., Kotova S.Yu., Sulatsky A.A., Gusarov V.V., Almjashev V.I., Barrachin M., Bottomley D., Fischer M., Piluso P., Miassoedov A., Tromm W., Fichot F., Kymalainen O. Influence of thermal gradient conditions on the physicochemical interaction between suboxidized corium melt and steel during in-vessel retention // First version in Russian.
Sulatsky A.A., Bechta S.V., Granovsky V.S., Khabensky V.B., S.A., Krushinov E.V., Vitol S.A., Kotova S.Yu., Strizhov V.F., Fischer M., Hellmann S., Tromm W., Miassoedov A., Bottomley D., Piluso P., Kymalainen O., Barrachin M. Molten corium oxidation kinetics at a severe accident with VVER, PWR, BWR // First version in Russian.

## Slide 15: Current situation with METCOR-P
The original date of METCOR-P completion was 01 April 2010. The project time has been extended until 30 September 2010.
During the year after the 3rd meeting (27 May, 2009, St. Petersburg) 2 experiments have been made (МСР-4, МСР-5). MCP-6 test is at a preparation stage.
The 2 remaining experiments will be made before the new Project completion date (30 September 2010).
The analysis of experimental data, delivery of technical reports and final report with be made within 6 months after the official Project completion date.
As the time before Project completion is running short, it is highly desirable to agree about the procedure of МСР-7 and МСР-8, the two remaining tests, as soon as possible.