## Slide 1: Status of PRECOS ISTC project 3813: Phase relation in corium systems
Presented by E. Krushinov
5th PRECOS Project Meeting
May 22, 2012, St. Petersburg
ETU
Saint-Petersburg
A.P. Alexandrov RIT
International Science
and Technology Center
SPbSIT (TU)

## Slide 2: PRECOS project general information
Project participants and coordination
Areva NP, Germany
ISTC, Moscow
FZK, Germany
IRSN,
France
ITU,
EU
CEA,
France
Collaborators
Steering committee
Operation Agent: A.P. Alexandrov RIT, Russia
Coordinator
IVTAN,
Russia
SPb State Electrotechnical University,
Russia
SPb State
Technological University, Russia

## Slide 3: Project objectives
Experimental determination of:
liquidus – solidus temperatures
coordinates of reference points (eutectics, etc.)
solubility limits of solid solutions
compositions of liquids coexisting in the miscibility gap

## Slide 4: PRECOS test matrix
Task | Composition | Atm | Experimental data | Number of tests
1 | U-Zr-Fe-O | Argon | Selected points (liquidus, solidus, tie-lines in the miscibility gap) | 81
2 | ZrO2 - FeOy | Air and pO2 control | liquidus, solidus, solubility limits | 32
 | UO2 - SiO2 | Neutral | liquidus, solidus, solubility limits, eutectic point | 53+154+405
 | CaO - UO2 |  |  | 11+73+214
3 | UO2 – FeO – SiO2 |  | liquidus, solidus, solubility limits, tie-lines in the miscibility gap, ternary eutectic point | 53+154+305+46
 | UO2 – FeO – CaO |  | liquidus, solidus, solubility limits, ternary eutectic point | 73+214+35+36
 | ZrO2 - FeO - SiO2 |  | ternary eutectic point | 0
 | ZrO2 - FeO - CaO |  | ternary eutectic point | 0
4 | Multicomponent prototypic corium | Argon or Air | System (atmosphere) proposed by: - French partners (1 system) German partners (1 system) - Russian partners (1 system) | 22+33+94+26
Notes: 1-LPH (Zr-O), 2- HTM, 3- VPA IMCC, 4- VPA in the Galakhov microfurnace, 5- annealing in the Galakhov microfurnace, 6 - DTA
  It was decided at the 3rd Project meeting to exclude these systems from the test matrix and subject to a more detailed study as higher priority ones

## Slide 5: PRECOS reporting (1) Annual and final reports

## Slide 6: PRECOS reporting (2) Thematic reports

## Slide 7: Publications
Almjashev V.I., Barrachin M., Bechta S.V., Bottomley D., Defoort F., Fischer M., Gusarov V.V., Hellmann S., Khabensky V.B., Krushinov E.V., Lopukh D.B., Lysenko A.V., Martinov A.P., Mezentseva L.P., Miassoedov A., Petrov Yu.B., Vitol S.A.
Ternary eutectics in the FeO–UO2–ZrO2 and Fe2O3–U3O8–ZrO2 systems
// Radiochemistry. 2011. V. 53, N 1. P. 13-18.
Almjashev V.I., Barrachin M., Bechta S.V., Bottomley D., Defoort F., Fischer M., Gusarov V.V., Hellmann S.,Khabensky V.B., Krushinov E.V., Lopukh D.B., Mezentseva L.P., Miassoedov A., Petrov Yu.B., Vitol S.A. Phase equilibria in the FeO1+x–UO2–ZrO2 system in the FeO1+x-enriched domain // JNM. 2010. V. 400. N. 2. P. 119–126

## Slide 8: Planned papers
Phase diagrams of the SiO2–Fe2O3(Fe3O4) system in different gas atmosphere // J. Europ. Ceram. Soc.
Phase diagram of the UO2–SiO2 system // JNM
The manuscript needs refinement:
- thermodynamic (GEMINI2/NUCLEA) optimization