## Slide 1: Progress report on the ISTC project #3813: Phase relation in corium systems (PRECOS)
A.P. Alexandrov Research Institute of Technology
Presented by S. Bechta
18th CEG-SAM meeting
St. Petersburg, Russia
September 28-30, 2010
ETU
Saint-Petersburg
SPbSIT (TU)

## Slide 2: Contents
  General information
  Project objectives
  PRECOS test matrix
  Scope of work in quarters 8 - 9
  Test results:
  UO2-CaO system
  UO2-SiO2- FeO system
  UO2-CaO- FeO system
  Concluding remarks

## Slide 3: PRECOS project general information
Project participants and coordination
Areva NP, Germany
ISTC, Moscow
FZK, Germany
IRSN,
France
ITU,
EU
CEA,
France
Collaborators
Steering committee
Operation Agent: A.P. Alexandrov RIT, Russia
Coordinator
IVTAN,
Russia
SPb State Electrotechnical University,
Russia
SPb State
Technological University, Russia

## Slide 4: Project objectives
Experimental determination of:
liquidus – solidus temperatures
coordinates of reference points (eutectics, etc.)
solubility limits of solid solutions
compositions of liquids coexisting in the miscibility gap

## Slide 5: PRECOS test matrix
Task | Composition | Atm | Experimental data | Priority level | Number of tests scheduled /carried out
1 | U-Zr-Fe-O | Argon | Selected points (liquidus, solidus, tie-lines in the miscibility gap) | 1 | 6/81
2 | ZrO2 - FeOy | Air and pO2 control | liquidus, solidus, solubility limits | 2 | 3/32
 | UO2 - SiO2 | Neutral | liquidus, solidus, solubility limits, eutectic point | 1 | 7/(53+404)
 | CaO - UO2 |  |  | 1 | 7/73
3 | UO2 – FeO – SiO2 |  | liquidus, solidus, solubility limits, tie-lines in the miscibility gap, ternary eutectic point | 1 | 10/(13+44)
 | UO2 – FeO – CaO |  | liquidus, solidus, solubility limits, ternary eutectic point | 1 | 10/13
 | ZrO2 - FeO - SiO2 |  | ternary eutectic point | 2 | 2/0
 | ZrO2 - FeO - CaO |  | ternary eutectic point | 2 | 2/0
4 | Eutectic composition measurement of a realistic complex corium mixture | Argon or Air | System (atmosphere) proposed by: - French partners (1 system) German partners (1 system) - Russian partners (1 system) | 2 | 3/0
Notes: 1-LPH (Zr-O), 2- HTM, 3- VPA IMCC, 4- VPA in Galahov microfurnace

## Slide 6: Scope of work in quarters 8-9
Experiments in the UO2-CaO, UO2-FeO-CaO, UO2-FeO-SiO2 systems have been conducted. Post-test analysis of samples is in progress
IVT RAN setup with laser heating has been additionally equipped with 300 mW diode laser for specimen lighting
IVT RAN setup with laser heating has been used for the verification experiments on previously studied Zr-O and ZrO2-FeO systems
Construction work necessary for getting a license on uranium handling has been completed. The license is expected to be issued in December 2010; after that the U-Zr-Fe-O studies will be started

## Slide 7: Scope of work in quarters 8-9 (2)

## Slide 8
Experimental objectives
Tliq determination
Determination of the components final solubility in the formed solid solutions
Charge composition
mol.% 30UO2 + 70CaO
Tliq was measured 3 times by VPA IMCC with melt sampling
From 4829 s, the pool was pulled out from inductor at 8.5 mm/h for 2.4 hours. This has ensured close to equilibrium crystallization and the eutectic liquid displacement into the ingot upper part
Samples
Tliq
UO2 - CaO system: PRS 11 test results

## Slide 9
VPA IMCC: Example of thermogram 3 from the test showing melt surface
    Results of Tliq measurements: 1912, 1910, 1907oC
Sample | Cha | XRF
 | UO2 mol.% | 
#1 | 30.5 | 32.0
#2 | 30.1 | 32.9
#3 | 30.8 | 34.5
Melt samples
composition
UO2 - CaO system: PRS 11 test results (2)
SEM/EDX in progress

## Slide 10
1
5
mm
2
3
4
5
6
7
8
9
10
1
1
1
2
3.3µm
10µm
12.5µm
UO2 - CaO system: PRS 11 test results (3)
SEM/EDX analysis of the ingot
Eutectic |  | UO2 | CaO
EDX | mass % | 69.7 | 30.3
 | mol% | 32.4 | 67.6
Ca2UO4
Ingot practically consists of Ca2UO4 and small eutectic regions
Eutectic composition is close to the chemical compound, and during the long-term exposure the crystallized eutectic regions undergo recrystallization
Notes: Eutectics for UO2 from 34.8 to 32.4mol.% on PRS10 and 11 respectively. In chemical compound UO2-33.3 mol%
The polished section of the ingot specimen top is presented, there the eutectics was driven/activated/started, куда отгоняли эвтектику.
The charge composition was close to the assumed eutectics, therefore extensive eutectics was expected. But eutectics was formed only in region 9. All other regions practically showed monophase layer of Ca2UO4, which is shown in the bottom images. As some publications mention the existence of this compound in the suboxidized region, we believe that here the eutectics is recrystallized in the suboxidized region into the chemical compound.Agreed with Almyashev.

## Slide 11
Experimental objectives
Tliq determination at high UO2 content
Two melt compositions have been
realized within one melting cycle
6 melt samples were taken and Tliq was
measured 6 times by VPA IMCC
Charge composition
mol.% 60UO2 + 40CaO
Samples
Tliq
Samples
Tliq
UO2 - CaO system: PRS 12 test results

## Slide 12
VPA IMCC: Fragment of the experiment thermogram 3 showing melt surface
    Tliq was measured 3 times: 2440, 2420 and 2432oC
Melt samples composition
Sample | Cha | XRF
 | UO2 mol.% | 
№1 | 57.3 | 55.03
№2 | 52.3 | 56.3
№3 | 59.3 | 55.1
UO2 - CaO system: PRS 12 test results (2)
Charge composition, mol.% 60UO2 + 40CaO
SEM/EDX in progress

## Slide 13
VPA IMCC: Fragment of the experimental thermogram 4 showing melt surface
    Tliq was measured 3 times: 2589, 2620 and 2595oC
Charge composition (after CaO addition in to the melt)
mol.% 70UO2 + 30CaO
Melt samples composition
Sample | Cha | XRF
 | UO2 mol.% | 
№4 | 71.6 | 70.3
№5 | 64.8 | 70.1
№6 | 64.0 | 68.6
SEM/EDX in progress
UO2 - CaO system: PRS 12 test results (3)

## Slide 14
Test results on the UO2 - CaO system
Compositions of the final solid solutions and the eutectics will be refined after SEM/EDX has been performed for PRS12
The posttest analysis of samples from the corium ingot from VULCANO VP-U1, an ECOSTAR test, has detected CaO solubility in UO2 (aproximately 47.9 мол.%) in one of the samples

## Slide 15
UO2 – FeO – SiO2 system: PRS 13 test results
Experimental objectives
Charge composition
mol.% 30.00 UO2 + 46.67 FeO +23.33 SiO2
Tliq was measured 4 times by VPA IMCC and accompanied by melt sampling
From 3276 s, the pool was pulled out from inductor at 9 mm/h for 3.6 hours. This has ensured close to equilibrium crystallization and the eutectic liquid displacement into the ingot upper part
Tliq determination by VPA IMCC.
Determination of the ternary eutectic composition
Samples
Tliq

## Slide 16
# 3
# 4
# 2
UO2–FeO–SiO2 system: PRS 13 test results (2)
VPA IMCC: Example of thermogram 1 from the test showing melt surface
    Results of Tliq measurements: 2055, 2083, 2092, 2079oC

## Slide 17
Chemical analysis of melt samples
UO2–FeO–SiO2 system: PRS 13 test results (3)
In progress:
- SEM/EDX analysis of melt samples;
- chemical analysis of other fused products (ingot, crusts, dry spillages and aerosols) for composing the elemental material balance

## Slide 18
Tliq and Tsol determination in the Galakhov microfurnace
Sample 2
1704C
1755C
1846C
1898C
2017C
Visual polythermal analysis in the Galakhov microfurnace Tsol= 1755С; Tliq=2017С
Tliq, determined by the VPA IMCC (208330С) and by the Galakhov method (2017С) for the composition in question differ by 66С, presumably, due to the interaction of the sample with the holder in the Galakhov microfurnace
Beginning of melting
Complete spreading
UO2 –FeO-SiO2 system: PRS 13 test results (4)

## Slide 19
Experimental objectives
Annealing, melting and quenching in the Galakhov microfurnace (estimation of ternary eutectic position)
Test | Content, mol.% |  |  | Tempera-ture, С | Exposure time, min | Note
 | UO2 | SiO2 | FeO |  |  | 
GPRS33 | 5.0 | 70.0 | 25.0 | 1100 | 60 | Annealing
 |  |  |  | 2100 | 5 | Melting and quenching
GPRS34 | 10.0 | 80.0 | 10.0 | 1100 | 60 | Annealing
 |  |  |  | 1850 | 5 | Melting and quenching
GPRS35 | 20.0 | 73.0 | 7.0 | 1100 | 60 | Annealing
 |  |  |  | 1950 | 5 | Melting and quenching
GPRS36 | 1.7 | 65.5 | 32.8 | 1100 | 60 | Annealing
 |  |  |  | 1300 | 20 | Melting
 |  |  |  | 1300-900 | 240 | Cooling at 100C/h
Study the miscibility gap boundaries
Determine ternary eutectic point
UO2
SiO2
FeO
Fe2SiO4
GPRS33
GPRS35
GPRS34
GPRS36
UO2 of >99.0 % purity, SiO2 of 99.99% purity, charge mass – 150 mg, molybdenum crucibles  6 mm
UO2-FeO-SiO2 system: GPRS #33-36 test results (5)

## Slide 20
UO2-FeO-SiO2 system:GPRS #33-36 test results(6)
SEM/EDX GPRS 33
Conditions:
Charge composition, mol%
5UO2 + 25FeO +70SiO2
isothermal exposure at 1100°С for 1 h., heating up to 2100°С, 5-min. exposure, quenching
SQ1
167 m
25 m
0.92 m
.P1
.P2
.P3
No macrostratification was found in the oxidic part of the polished section
Microstructure resembling that of the ‘heavy’ liquid in the UO2-SiO2 system. As a result of the interaction between the melt and the crucible, the composition got depleted in Fe, but no molybdenum was found in the oxidic part
Notes: The slide shows specification and polished section of experiment with microimages of characteristic zones. In the oxidic part no macro-stratification into light and heavy liquids is observed, and similar to the UO2-SiO2 system the microstructure resembles the heavy liquid one. There the interaction of crucible material (Mo) with iron is observed. The iron was introduced in excess for FeO stoichiometry, but in the oxidic part Mo is absent.

## Slide 21: SEM/EDX GPRS 34
Fe
UO2
SiO2 with inclusions
FeSiO3
124 m
25 m
49.9 m
12.5 m
100 m
UO2-FeO-SiO2 system:GPRS #33-36 test results(7)
Conditions:
Charge composition, mol% 10 UO2 + 10 FeO +80 SiO2
Isothermal exposure at 1100°С for 1 h., heating up to 1950°С and a 5-min. exposure, quenching
Indication of MG
The microstructure is nonuniform. Inclusions of irregular shape indicate that the melt exposure time was insufficient (equilibrium was not reached). The globules of heavy liquid contain Femet drops
6.67 m
100 m
SiO2 with inclusions
Mo(Fe)
UO2
SQ2
SQ1
SQ3
Notes: The slide shows specification and polished section of experiment with microimages of characteristic zones. Microstructure is inhomogeneous. Inclusions have irregular shape, which indicates the insufficient time of melt exposition (equilibrium not reached). Heavy liquid globules and light liquid matrix confirm that the composition was in the miscibility gap. For future studies it is suggested to increase the melt exposition time to 20 minutes.

## Slide 22
UO2-FeO-SiO2 system:GPRS #33-36 test results(8)
Conditions:
Charge composition, mol%
20 UO2 + 7 FeO +73 SiO2
Isothermal exposure at 1100°С for 1 h., heating up to 1850°С, 5-min. exposure, quenching
Though the macrostructure is uniform, the microstructure is extremely inhomogeneous and resembles that in UO2-SiO2 near the binodal
SEM/EDX GPRS 35
4 m
2.5 m
167 m
6.67 m
144 m
SQ1
SQ3
SQ2
Notes: The slide shows specification and polished section of experiment with microimages of typical zones. The macrostructure is homogeneous. But the microstructure is definitely inhomogeneous. Note that the microstructure in UO2-SiO2 is above binodal. For this composition it is planned to decrease annealing temperature to 1800С

## Slide 23
UO2-FeO-SiO2 system:GPRS #33-36 test results (9)
XRD of sample of GPRS 36 test
2
The analysis was done using FARAD desktop diffractometer with CrKα1 radiation (λ = 0.22897 nm)
Notes: After the experiment a sample was prepared and its XRF analysis made. The result on slide confirms that the composition is located in the sectoral triangle of the diagram: UO2-Fayalite-SiO2

## Slide 24: SEM/EDX GPRS 36
UO2-FeO-SiO2 system:GPRS #33-36 test results(10)
SQ2
144 m
40.1 m
1.67 m
SQ1
Conditions:
Charge composition, mol% 1.7 UO2 + 32.8 FeO +65.5 SiO2
Isothermal exposure at 1100°С for 1 h., heating up to 1300°С, 20-min. exposure, chilling from 1300 down to 900°С for 240 min.
Microstructure in the lower part of the crucible shows the eutectic crystallization. In terms of composition, this eutectics lies within a specific triangle UO2-Fe2SiO4-SiO2.
SQ3
Notes: The slide shows specification and polished section of experiment with microimages of characteristic zones. Eutectic microstructure in the bottom part of the crucible is found; its composition is given in the table.

## Slide 25
UO2-FeO-SiO2 system: GPRS #33-36 test results(11)
SiO2
Bulk composition of the total microstructure in GPRS 35
‘Heavy’ liquid in GPRS 34 (T from Tq up to Tm)
Composition of the light matrix in GPRS 34 (T~Tm)
Composition of the ‘light’ liquid with globules in GPRS 34 (T~Tq~1850C)
Composition of the liquid at T~Tq~1950C (above MG)
Characteristic points of the diagram
Initial composition of the charge
Light matrix composition in GPRS 35 (T is presumably around Tm)
Composition of globules in the light matrix in GPRS 35 (T is presumably around Tm)
Ternary eutectics composition in GPRS 36
Solid phase composition in GPRS 36
Bulk composition in GPRS 33 (no MG)
Notes: The slide presents preliminary experimental results of completed studies: shifts of integral compositions from charge compositions and determined compositions of heavy and light liquids. It also shows the composition of eutectics, temperature of which will be determined in a separate experiment

## Slide 26
UO2-FeO-SiO2 system: test results (12)
The performed tests confirm the existence of a miscibility gap in a fairly narrow region adjacent to the diagram corner on the SiO2 side
The ternary eutectics has been determined within a particular triangle of the UO2 - Fe2SiO4 - SiO2 ternary system
The PRS13 test has been performed for determining composition of the second ternary eutectics within a particular triangle of the UO2 - Fe2SiO4 - FeO ternary system. The ingot analysis is underway

## Slide 27
UO2 – FeO – CaO system: PRS 14 test results
Experimental objectives
Charge composition
mol.% 20.1UO2 + 66.7FeO +13.2CaO
Tliq,,was measured by VPA IMCC 3 times; video record of one measurement could not be deciphered. Samples were taken 3 times
Samples
From 4519 s, the pool was pulled out from the inductor at 9 mm/h for 5.9 hours. This has ensured close to equilibrium crystallization and the eutectic liquid displacement into the ingot upper part
Tliq determination by VPA IMCC
Determination of eutectic composition
Tliq

## Slide 28
UO2 – FeO – CaO system: PRS 14 test results (2)
VPA IMCC: Example of thermogram #2 showing melt surface
    Results of Tliq measurements: 1238, 1247oC
# 3

## Slide 29
UO2 – FeO – CaO system: PRS 14 test results (3)
XRF and Chemical analysis of melt samples
* - determined from residue
The results of corium samples XRF and chemical analysis were found to differ significantly
XRF results are believed to be more accurate, since the content of CaO was not determined by chemical analysis, but calculated from the residue
In progress: - the SEM/EDX analysis of melt samples
Notes: The slide shows results of the melt sample analysis. Difference between XRF and chemical analysis has been found. XRF is more precise, because the chemical analysis determines CaO from the residue. The final composition will be determined after SEM/EDX analysis of melt samples.

## Slide 30
1 sm
ingot
250 m
6 m
6 m
15 m
CaU(Fe)O3
Fe(Ca)O
CaFeO3
Eutectic |  | UO2 | FeO | CaO
EDX | mass % | 10.3 | 62.4 | 27.2
 | mol% | 2.8 | 62.4 | 34.9
Eutectic |  | UO2 | FeO | CaO
EDX | mass % | 10.5 | 61.4 | 28.2
 | mol% | 2.8 | 61.2 | 36.0
UO2 – FeO – CaO system: PRS 14 test results (4)
SEM/EDX
Notes: A template was made from ingot. The ingot study is aimed at the detection and composition determination of ternary eutectics, this is exactly what has been done.

## Slide 31
VPA IMCC is used to determine liquidus temperature of composition, mass%: 19.3±1.0 UO2 + 66.6±3.3 FeO + 14.1±0.7 CaO – Tliq= 1242±20 °C
EDX method is used to determine the ternary eutectic composition, mass%:
10.4±0.1 UO2 + 61.9±0.5 FeO + 27.7±0.5 CaO
UO2 – FeO – CaO system: PRS 14 test results (5)

## Slide 32: Joint publication with collaborators within the reported quarters
Almjashev V.I., Barrachin M., Bechta S.V., Bottomley D., Defoort F., Fischer M., Gusarov V.V., Hellmann S., Khabensky V.B., Krushinov E.V., Lopukh D.B., Mezentseva L.P., Miassoedov A., Petrov Yu.B., Vitol S.A.
Phase equilibria in the FeO1+x–UO2–ZrO2 system in the FeO1+x-enriched domain
// JNM. 2010. V. 400. N. 2. P. 119–126

## Slide 33: 3rd PRECOS project meeting ( June 2, 2010, St. Petersburg)
Objectives:
Discuss test results related to binary and ternary oxidic systems:
UO2-SiO2; UO2-CaO; ZrO2-FeOy
UO2-FeO-SiO2; UO2-FeO-CaO
Discuss and agree upon future works
Discuss possible reasons of discrepancies between XRF, Chemical and EDX analyses of UO2-SiO2 and UO2-CaO samples
Publications
To discuss PRECOS project prolongation without additional funding

## Slide 34: 3rd project meeting decisions about further work
Conduct 1 experiment in the UO2-SiO2 system by LPH method
Cancel the studies of eutectic points in the ZrO2–FeO–SiO2, ZrO2–FeO–CaO systems for a more detailed study of priority system
Check melt pollution by the crucible material in the GPRS experiments in the UO2-FeO-SiO2 system, to determine a possibility of studies in the Mo crucibles and discuss it with collaborators

## Slide 35: Concluding remarks
Experimental studies in the UO2-CaO system have been completed
Study of the UO2-CaO-FeO ternary system have been started
Plans for quarters # 10 - 11:
Complete the UO2-CaO systems and start a report preparation
Continue study of the ZrO2-FeOy ; UO2-SiO2-FeO; CaO-UO2-FeO and U-Zr-O systems (the last one by LPH in IVT RAN)