## Slide 1: Progress report on the ISTC project #3813: Phase relation in corium systems (PRECOS)
ISTC
A.P. Alexandrov Research Institute of Technology
Presented by S. Bechta
14th CEG-SAM meeting
September 9-11, 2008, Kiev

## Slide 2: Contents
  General information
  Project status
  Project focus
  Methodology
  PRECOS test matrix
  UO2-SiO2 system
  New experimental facilities
  Possible revision of the O-U-Zr phase diagram
  Conclusions

## Slide 3: PRECOS project general information
Project participants and coordination
Areva NP, Germany
ISTC, Moscow
FZK, Germany
IRSN,
France
ITU,
EK
CEA,
France
Collaborators
Steering committee
Operation Agent: A.P. Alexandrov RIT, Russia
Coordinator
ISC RAS,
Russia
IHT RAS,
Russia
SPb Electrotechnical State University, Russia

## Slide 4: PRECOS project focus
Project objective: Experimental study of phase diagrams of corium mixtures
Data application
  Liquidus and solidus temperatures versus component concentrations
  Temperature-concentration regions of the miscibility gap
  Coordinates of eutectic, dystectic and other characteristic points
  Final solubility in solid solution
Experimental data
  Thermodynamic database optimisation
  Thermodynamic code validation
  Corium behaviour modelling

## Slide 5: Experimental methods of phase diagram studies
Visual polythermal analysis in the cold crucible (VPA IMCC)
Differential thermal analysis (DTA) and differential scanning calorimetry (DSC)
Visual polythermal analysis in the Galakhov microfurnace (GM)
High-temperature microscopy (HTM)
Laser pulse heating (LP)
These methods have been used in the projects: COLOSS, METCOR, CIRMAT, CIT, ENTHALPY, ECOSTAR, OECD/MASCA and CORPHAD

## Slide 6: Methods of posttest analysis
Elemental analysis
 X-ray fluorescence analysis (XRF)
 Chemical analysis (СhA)
Phase analysis
 X-ray diffraction analysis (XRD)
 Energy-dispersive X-ray spectrometry (EDX)
Microstructure analysis
 Optical microscopy
 Scanning electron microscopy (SEM)
Oxygen determination
 Carbothermic reduction

## Slide 7: PRECOS test matrix
Task | Composition | Atmosphere | Experimental data | Priority level | Pt N
1 | Different compositions in the U-Zr-Fe-O system | Argon | Selected points (liquidus, solidus, tie-lines in the miscibility gap) | 1 | 6
2 | ZrO2 - FeOy | Air and pO2 contol | liquidus, solidus, solubility limits | 2 | 3
 | UO2 - SiO2 | Argon | liquidus, solidus, solubility limits, eutectic point | 1 | 7
 | CaO - UO2 |  |  | 1 | 7
3 | UO2 – FeO – SiO2 |  | liquidus, solidus solubility limits, tie-lines in the miscibility gap, ternary eutectic point | 1 | 10
 | UO2 – FeO – CaO |  | liquidus, solidus solubility limits, ternary eutectic point | 1 | 10
 | ZrO2 - FeO - SiO2 |  | ternary eutectic point | 2 | 2
 | ZrO2 - FeO - CaO |  | ternary eutectic point | 2 | 2
4 | Eutectic composition measurement of a realistic complex corium mixture | Argon or Air | System (atmosphere) proposed by French partners (1 system), System (atmosphere) proposed by German partners (1 system), System (atmosphere) proposed by Russian partners (1 system) | 2 | 3
1st PRECOS meeting decisions: NITI will start with UO2-SiO2, ISC - with ZrO2 - FeOy, IVTRAN with U-Zr-O system

## Slide 8: Status of the project
PRECOS test matrix has been finalized with collaborators at the 6th and 7th CORPHAD project meetings
The project was approved for funding by 44th ISTC MB in December 2007
Work Plan was prepared and sent to ROSATOM Export control in January 2008
The Work Plan was approved by the Export control in the end of February 2008. Export licensing is not necessary for PRECOS
Project started from June 1, 2008
Kick-off meeting with the project collaborators took place in St. Petersburg, July 10, 2008
Test matrix and first tests on UO2-SiO2 system has been specified during the meeting
First results on the UO2-SiO2 system were obtained

## Slide 9
  To define the monotectic temperature and the boundary curve of the miscibility gap in vicinity of the monotectic temperature
UO2-SiO2 system: GPRS 1-3 tests
Experimental objectives
Annealing and quenching in Galakhov microfurnace
UO2 of >99.0 % purity, SiO2 of 99.99% purity
Mass of the charge – 150 mg

## Slide 10
Sections of the crucibles
GPRS 1
2050C 5 min.
below monotectic
GPRS 2
2080C 5 min.
GPRS 3
2080C 10 min.
just above monotectic
Mo crucible
Heavy liquid
Light liquid
0.5 mm
0.7 mm
0.8 mm
Heavy liquid
Light liquid
UO2-SiO2 system: GPRS 1-3 tests (2)

## Slide 11
GPRS 2
2080C 5 min
Inclusion near the phase boundary after quenching
30 m
UO2-SiO2 system: GPRS 1-3 tests (3)
Secondary separation of lightweight liquid in the dense liquid during melt cooling

## Slide 12
EDX analysis different domains in heavy liquid layer
Examined region | Composition, mol % | 
 | UO2 | SiO2
SQ1 | 26.7 | 73.3
SQ2 | 27.3 | 72.7
SQ3 | 28.0 | 72.0
SQ4 | 30.3 | 69.7
Overage value | 28.1±1.6 | 71.9±1.6
Examined region | Composition, mol % | 
 | UO2 | SiO2
SQ1 | 28.1 | 71.9
SQ2 | 31.8 | 68.2
SQ3 | 30.0 | 70.0
SQ4 | 28.3 | 71.7
Overage value | 29.5±1.7 | 70.5±1.7
2080C 5 min
2080C 10 min
UO2-SiO2 system: GPRS 1-3 tests (4)

## Slide 13
EDX analysis of different domains in light liquid layer
Examined region | Composition, mol % | 
 | UO2 | SiO2
SQ1 | 12.6 | 87.4
SQ2 | 11.7 | 88.3
SQ3 | 11.7 | 88.3
Overage value | 12.0±0.6 | 88.0±0.6
Examined region | Composition, mol % | 
 | UO2 | SiO2
SQ1 | 11.5 | 88.5
SQ2 | 11.6 | 88.4
SQ3 | 12.7 | 87.3
Overage value | 12.0±0.7 | 88.0±0.7
2080C 5 min
2080C 10 min
UO2-SiO2 system: GPRS 1-3 tests (5)

## Slide 14
UO2-SiO2 system: PRS 1 test
Experimental objectives
Determine liquidus temperature at high UO2 content
VPA IMCC: Fragment of the experiment thermogram showing melt surface
    Tliq was measured three times: 2444 oC, 2404 oC and 2427 oC  Tliq=2425 oC

## Slide 15
Red lines – Lungu’ diagram
Blue lines and blue points –
results of our previous work
within the CORPHAD project
Yellow points – results of the
present work
UO2-SiO2 system: results

## Slide 16: In IVTRAN: Laser pulse heating with 3.3 kW CW-YAG laser
New experimental facilities
- Special ventilation with micro-filtering of the incoming air
- Continuous close cycle dust removal
- Air conditioning
- Thermo stabilized water supply to all experimental set-ups
- Motor-driven jalousie for complete darkening
- Two fibre laser-beam delivery systems
- Laser power regulation according to arbitrary function (time response of ca 1 ms)

## Slide 17: Schematic of the laser pulse heating facility
New experimental facilities (2)
Fiber
Optic
Fiber
Optic
Sample
Laser
Focusing
Unit
Polychromatic
Pyrometer
High-Speed
Pyrometer with
extra channel
Transient recorder
Laser power
Spectra strobe
High Power
Fiber-Laser
Diode Laser
Vacuum/
Pressure
High-Speed
CCD Camera

## Slide 18
at% :59.9Zr+ 19.9Fe+20.2O
(ZrO0.337)0.751Fe0.249
mass%, 28.57 Zr02 + 48.26 Zr + 23,17 Fe
Zr0.464 Fe0.253 O0.283
Cut out from ingot of CORPHAD test
Pressed (but not sintered) sample
Samples after laser pulse heating
New experimental facilities (3)

## Slide 19
NUCLEA 07
Optimized with CORPHAD data
2473 K
Study of O-U-Zr phase diagram
2473 K
Self-contradiction of experimental data of MG boundary and tie line directions
U-ZrO2 section study in IVTRAN was proposed

## Slide 20: Concluding remarks
Short term planning was discussed during 1st PRECOS meeting as well as the existing problem with U-Zr-O system modeling
Preparation of new installation in IVTRAN is in progress. It will be used for U-Zr-O system study
New results were already obtained for UO2-SiO2 system, this work will be continued
Study of ZrO2 – FeOy system will be carried out in the 2nd quarter