## Slide 1: Progress Report on the ISTC project #1950.2 “Phase Diagrams for Multicomponent Systems Containing Corium and Products of its Interaction with NPP Materials” (CORPHAD.2)
Presented by S. Bechta
9th CEG-SAM Meeting
A.P. Alexandrov Research Institute of Technology

## Slide 2: Contents
Project general information
Experimental matrix of CORPHAD Project
Scope of the work in the 10-11 quarters
Zr-Fe-O system
U-Zr-O system
U-Fe-O system
U-O system
Papers
Plans for the period till the end of the Project
Conclusions

## Slide 3: CORPHAD project general information
Project participants and coordination
ISTC, Moscow
FZK, Germany
IRSN,
France
ITU,
EK
CEA,
France
Collaborators
Steering committee
Operation Agent: A.P. Alexandrov RIT, Russia
Coordinator
Framatome ANP, Germany
ISC RAS,
Russia
RRC Kurchatov Institute, Russia
SPb Electrotechnical State University, Russia
*) Should be finished in November 2006

## Slide 4: Experimental matrix of CORPHAD Project

## Slide 5: Scope of work in the 10-11 quarters
Complete the assembly of the Rasplav-4 facility with a 5.28 MHz HF generator for tests in the UO2-SiO2 system
Complete Task 2, three last tests with ternary metal-oxidic systems with miscibility gap have been performed:

## Slide 6: Zr-Fe-O system: CORD39
Determine liquidus temperature
Determine miscibility gap shape above Tliq
Experimental objectives
VPA IMCC Fragment of the experiment thermogram showing melt surface
    Tliq was measured three times: 2490 oC, 2453 oC and 2457 oC  Tliq=2490 oC
    during the second and third measurements the efficient blowing of aerosols was not achieved
    melt temperature is close to the Fe boiling temperature → Fe evaporation
Notes: In accordance wit the CORD33 posttest analysis the miscibility gap area is smaler than the calculated one, and the determined tie-line is on the boundary edge. For this reason it was decided to shift the CORD39 initial charge composition deeper into the gap.

## Slide 7: SEM/EDX
1cm
“Oxidized part”
“Metallized part”
Frozen
liquid
200 m
20 m
20 m
1 mm
400 m
Zr-Fe-O system: CORD39 (continued)
ZrO2 and Fe calibrated data
 | Zr | Fe | O
mass % | 61.3 | 30.7 | 8.0
mol.% | 39.0 | 31.9 | 29.1
 | Zr | Fe | O
mass % | 73.6 | 7.3 | 19.1
mol.% | 37.9 | 6.1 | 56.0
ZrFe(O)
ZrO2
 | Zr | Fe | O
mass % | 64.5 | 25.0 | 10.5
mol.% | 39.0 | 24.8 | 36.2
Zr2Fe(O)
ZrFe2(O)
ZrO2
The oxidized liquid was located in the middle of the pool, as is evidenced by melt samples
Notes: During crystallization, the oxidic liquid, as the most refractory, undergoes monotectic transformation. ZrO2 and metallized liquid crystallize from it, the latter freezes fast, without decompositioning, that is it is quenched. The metallized liquid decomposes into the intermetallic phases containing oxygen and ZrO2, which is the phase of primary crystallization . которая застывает не успев разложится т.е. закаляется.

## Slide 8
Concluding remarks
Zr-Fe-O system
Tie line (Tmelt=2773K)
Tie line (Tmelt=2693K)
Miscibility gap was observed in CORD33 and CORD39 tests
Tliq=2655K (at.% 48.7 Zr – 19.7 Fe – 30.6 O)
Tliq=2763K (at.% 45.4 Zr – 25.8 Fe – 28.8 O)
CORD39
heavy “metallic” liquid, at.% 45.1Zr –31.5Fe –23.4O light “oxidic” liquid , at.% 44.4Zr –7.1Fe –48.5O
CORD33
light “metallic” liquid, at.% 51.5 Zr –24.3 Fe –24.2 O heavy “oxidic” liquid, at.% 47.9 Zr –4.9 Fe –47.2 O
Tliq=2637K (at.% 48.7 Zr – 19.7 Fe - 30.6 O)
CORD35
Depending on position of the figurative point in the miscibility gap, the relation between densities of the oxidic and metallic liquids may differ (in CORD33, oxide density was higher than that of metal
It is important to continue the study of this system in order to determine boundaries of the gap more precisely
2773K
Notes: In comparison with thermodynamic calculation the miscibility gap is a little narrower.

## Slide 9
Test objectives:
To determine liquidus temperature by VPA IMCC
To determine the composition of oxidic and metallic liquids in the miscibility gap
U-Zr-O system: CORD42
VPA IMCC results: example of thermogram with pool surface frames
Tliq = 2390 °C

## Slide 10
U-Zr-O system: CORD42 (continued)
Axial section of the ingot
“Oxidized” part
“Metallized” part
Boundary

## Slide 11
Concluding remarks
U-Zr-O system
CORD29 Tliq=2734K at.% 19.8U – 17.2Zr – 63.0O
CORD28-l Tliq=2665K at.% 7.7U – 53.7Zr –38.6 O
CORD34 Tliq=2578K at.% 21.5U – 34.7Zr – 43.8O
CORD37
CORD28-ll Tliq=2637K at.% 12.9U – 43.9Zr – 43.2O
Tie line CORD37 (Tmelt=2673K)
light “oxidic” liquid, at.% 21.7U –27.7Zr –50.5O heavy “metallic” liquid, at.% 33.5U –42.7Zr –23.7O
Tliq=2601K at.% 32.5U – 28.2Zr – 39.3O
CORD42 Tliq=2663K at.% 40U – 25Zr – 35O
Tie line CORD42 (Tmelt=2843K)
Miscibility gap was observed in CORD37 and CORD42 tests
Tie line for the CORD42 composition has not been determined yet – posttest analysis is underway
The obtained data show the gap to be less extended than predicted by calculations. Additional tests are required for specifying the gap boundaries at different compositions and quenching temperatures.
?
2673К

## Slide 12
Test objectives
Determine liquidus temperature of specified composition
Determine tie-line in the miscibility gap
U-Fe-O system: CORD40 (60U + 20Fe + 20O)
VPA IMCC: experimental thermogram with melt surface frames
Tliq = 2515 °C
Notes: The experiment was conducted in the 6th quarter, Two slides with experimental objectives and liquidus temperature measurements are shown as a reminder

## Slide 13
SEM
U-Fe-O system: CORD40 (continued)
eutectic-like area
1cm
200 m
100 m
Pore
UO2-x
UFe(O)
UFe2O
UO2-x
U6Fe(O)
Metalic globules in oxide matrix
Ox-in-Met
500 m
“Oxidized part”
“Metallized part”
Notes: SEM analysis has determined the presence of metallic droplets in the oxidic part and oxidic ones in the metallic part of the crystallized ingot. The most refractory oxidic liquid undergoes monotectic transformation during crystallization. UO2-x and metallized liquid crystallize from the liquid, it freezes without decomposition, that is it is quenched. которая застывает не успев разложится т.е. закаляется. The metallized liquid decomposes into the intermetallic phases containing oxygen and UO2-x, which is the phase of primary crystallization

## Slide 14
U-Fe-O system
Tie-line (Tmelt=2823K)
Stratification into two liquids is observed in the experiment
light “oxidic” liquid, at.% 42.1U –0.9Fe –56.0O heavy “metallic” liquid, at.% 62.4U –33.7Fe –3.9O
Tliq=2788K at.% 60U – 20Fe – 20O
CORD40
Concluding remarks
No problems with thermodynamic modeling of the U-Fe-O system in its metal-oxidic region due to the low solubility of iron in urania and oxygen in metal
Further studies of tie- lines in the miscibility gap of this system are not quite important. Measurements of eutectic temperature and composition would be useful
Oxygen content in metallized part of the ingot was measured by carbothermic reduction (ASTM E-1569)
LECO analyzer was used

## Slide 15
U-O system: CORD41
Methodological test objectives:
VPA IMCC: experimental thermogram with melt surface frames
Tliq = 2515 °C
Determine Tliq of specified composition, at% 60U – 40O
Determine tie-line in the miscibility gap
Compare with other authors’ data

## Slide 16
U-O system: CORD41 (continued)
SEM
500 m
Ox-in-Met
Metallic globules in oxide matrix
Oxidized
part
Metallized
part
150 m
500 m
Pore
UO2-x
U(O)
UO2-x
U(O)
Image analysis: U – 93.27 vol.%, UO2 – 6.65 vol.%, pore - 0.08 vol.%
Overall composition: U – 93.5 at.%
O – 6.5 at.%
Notes: По данным SEM анализа зафиксировано наличие капель - металлических в оксидной и оксидных в металлической частях закристаллизованного слитка. По предварительным данным физико-химического анализа содержание кислорода в оксидной части составляет 59.5 %(ат) , а в металлической части ниже предела обнаружения используемых методов. Для определения -уточнения области существования купола расслаивания в настоящее время проводится WDS микроанализ металлических и оксидных капель

## Slide 17
U-O system
Concluding remarks
Tliq=2515oC at.% 60U – 40O
CORD40
Tie line (Tmelt=2670oC)
light “oxidic” liquid, at.% 40.5U – 59.5O (Chemical analysis of oxidized part bulk)
heavy “metallic” liquid - analysis in progress
Miscibility gap was observed in the test
Image analysis metallized part: U – 93.5 at.%
O – 6.5 at.%
Coordinates of the tie-line left point have not been determined yet – metal samples are still analyzed
The data of C.Gueneau, Edwards and Martin concerning a very big miscibility gap were confirmed and efficiency of the methodology proved

## Slide 18
CORPHAD Papers
Bechta S.V., Krushinov E.V., Almjashev V.I., Vitol S.A., Mezentseva L.P., Petrov Yu.B., Lopukh D.B., Khabensky V.B., Barrachin M., Hellmann S., Froment K., Fischer M., Tromm W., Bottomley D., Defoort F., Gusarov V.V. Phase diagram of the ZrO2–FeO system. // J. Nucl. Mater. Vol. 348 (2006), p.p. 114-121
Mezentseva L.P., Popova V.F., Almjashev V.I., Lomanova N.A., Ugolkov V.L., Bechta S.V., Khabensky V.B., Barrachin M., Hellmann S., Gusarov V.V. Phase diagrams of the SiO2–Fe2O3(Fe3O4) systems in different gas atmosphere. // to be published in J. Europ. Ceram. Soc.,
Bechta S.V., Krushinov E.V., Almjashev V.I., Vitol S.A., Mezentseva L.P., Petrov Yu.B., Lopukh D.B., Khabensky V.B., Barrachin M., Hellmann S., Froment K., Fisher M., Tromm W., Bottomley D., Gusarov V.V. UO2–FeO phase diagram. // J. Nucl. Mater., in press

## Slide 19: Plans for the period till the end of the Project
U-Fe- Zr-O system
Two tests to be carried out and report prepared
Complex corium mixture
A test to be carried out and report prepared
UO2-SiO2 system
Two tests to be carried out and report prepared
Final report

## Slide 20: Conclusions
Methodological tests aimed at determining monotectic temperature and tie-line in the miscibility gap of the U-O system have shown the following:
- the measured monotectic temperature agrees with previously published data of Edvards (1966) and Gueneau (1997)
- temperature and compositions of the coexisting liquid phases can be specified after the posttest analysis of samples is completed
Monotectic temperatures and compositions of coexisting liquids above these temperatures have been measured in the miscibility gap of Zr-Fe-O, U-Fe-O, U-Zr-O systems
In the U-Fe-O, U‑Zr‑O systems the oxidized liquids have a lower density and are located on top of the pool. In the Zr-Fe-O system the inversion of oxidized and metallized layers has been observed in one of the tests
The experimental data can be used for the optimization of NUCLEA database if the content of oxygen in the oxidized and metallized parts of the system is specified. The work is in progress