## Slide 1
Post test analysis of PARAMETER-SF3, -SF4
Jon Birchley and Leticia Fernandez-Moguel (PSI)
Presented by Salih Guentay,
CEG-SAM, 30 September 2010, St. Petersburg, Russia

## Slide 2
  Summary of models used
  SF3 analysis
    effect of oxidation correlation
    effect of CCFL on reflood quench
  SF4 analysis
    treatment of air flow boundary conditions
    thermal response
    hydrogen generation
    oxygen consumption
  Conclusions and forward plans
Outline

## Slide 3
  Both packages based on RELAP5 thermal-hydraulics and SCDAP modelling of core components
    neither code as yet recognises oxygen as an active species
  Versions used
    SCDAP/RELAP5/Mod3.2/irs-psi
      extensions for PARAMETER heater rod
      axially uniform shroud and insulation spanning entire length of Ta/Mo/brass heater
      alternative oxidation kinetics (Sokolov, air) and reaction heat (oxygen)
    SCDAP/Sim/Mod3.4/psi
      essentially same pedigree as SCDAP/RELAP5 version above
      composition of shroud and insulation can vary along axial length
  SCDAP/Sim/Mod3.5
    under development
    oxygen recognised as an active species
    new air oxidation model
SCDAP/RELAP5 and SCDAP/Sim

## Slide 4
SCDAP/RELAP5 noding
Same base model for SF2, SF3, SF4
28 axial nodes for test section (lower, central and upper sections)
Radial noding: 1/1/4 in lower/central/upper sections
Heater: 14 Ta, 2x6 Mo, 2x1 brass
Cooling jackets for central and upper sections
Shroud/insulation for central bundle; dummy insulation applied in lower and upper sections (forced by SCDAP limitation)
Except where stated, base model uses default or recommendations
Same external resistance in base case models (8.5 mΩ/rod)

## Slide 5
Physical models
Oxidation in steam
Cathcart-Pawel/Urbanic-Heidrick correlations (default in SCDAP)
d(m2)/dt = 33.6 * exp(-20065/T) ; 10.85 * exp(-16610/T) T < 1853 K ; T > 1853 K
Sokolov correlation
d(m2)/dt = 318.0 * exp(-23040/T); 196.5 * exp(-20800/T) T < 1773 K ; T > 1773 K
Oxidation in air (SF4 air ingress phase); Benjamin et al
d(m2)/dt = 6.22 * exp(-14630/T) (coded in MELCOR)
Δh corresponds to steam or oxygen, as appropriate
The units are kg2 m-4 s-1 for oxygen mass gain
Interphase friction
Ishii drift-flux model (default in RELAP5); SF3: user-chosen CCFL correlation
jg*1/2 + 1.22 jf*1/2 = 0.88 (No, Lee and Song; Nucl. Engrg. Tech. 37, 557-564)
jg*1/2 + jf*1/2 = 0.725 (Wallis original; One-Dimensional Two-Phase Flow)
ji* = ji (ρi/(g dhyd (ρf – ρg)) ½ (i = f,g)

## Slide 6
  Effect of Oxidation correlation
    thermal response
    hydrogen generation
  Effect of CCFL on reflood quench
PARAMETER-SF3

## Slide 7
Moderate effect of oxidation correlation on temperature history
Major effect on hydrogen release
Neither correlation gave ideal agreement; CP/UH chosen for best estimate
Nominal conditions overestimated hydrogen generation and temperature rise during final excursion; power reduced after 13700 s to obtain good initial conditions for reflood simulation
Some uncertainty about experimental power distribution poses difficulty with definition power
Shift in maximum temperature location
code-data difference may be due to temperature discrepancy at 6000-8000 s
Effect of oxidation correlation

## Slide 8
CP/UH oxidation model and reduced power during final excursion to give best conditions for reflood simulation
Experiment shows slow top-down quench to half way down, followed by faster bottom up quench
Without CCFL, quench follows refill curve (not plotted)
No et al CCFL roughly follows experiment; Wallis is too slow
Effect of CCFL on reflood quench
Start of injection

## Slide 9
  Modelling
    both SCDAP/RELAP5 and SCDAP/Sim used; same noding
    boundary conditions
  Thermal response
    overall
    air ingress
    reflood
  Hydrogen generation
  Oxygen consumption
PARAMETER-SF4

## Slide 10
  Pre-oxidation (0 - 13886 s)
  - 2 g/s Ar; 3.5 g/s steam (start at 1716 s)
  - power staged increase to 7900 W
  Cooling phase (13886 - 16022 s)
  - power reduced to 4000 W
  Air ingress (16022 - 17511 s)
  - 0.48 g/s air simulated with steam
  - number of O atoms and total volume flow preserved
  - air oxidation kinetics and Zr+O heat of reaction
  - power increased to 6000 W during this phase, tripped at 17412 s
  Reflood (17434 - 17908 s)
  - bottom injection: 80 g/s water (midway period at 40 g/s)
  - switch Ar injection to upper volume
SF4 boundary conditions

## Slide 11
SCDAP/RELAP5 does not recognise oxygen as an active species
“Air” is modelled by using steam as the oxidising agent and argon as a diluent; flows are defined to preserve total number of oxygen atoms and total molar flow
Oxidation kinetics modified for air
Heat of reaction modified for oxygen
“Air” = argon
+ steam
Modelling of SF4 inlet flows

## Slide 12
Both codes give fair agreement for temperatures at 1250 mm during pre-oxidation in steam
Minor effect of choice of oxidation correlation
SCDAP/Sim calculates better agreement for temperature rise during air ingress.
SCDAP/Sim calculates mild excursion during reflood
SCDAP/REPA5 calculates immediate cooling at start of reflood
S/R5
S/Sim
SF4 data
S/R5
S/Sim
SF4 data
SF4 temperature at 1250 mm

## Slide 13
During pre-oxidation CP/UH gives better total hydrogen generation than Sokolov when used with both SCDAP/RELAP5 and SCDAP/Sim
During reflood SCDAP/Sim calculated a moderate oxidation excursion but underestimated hydrogen generation
During reflood SCDAP/RELAP5 did not calculate any excursion
Code difference might be due to better representation of upper shroud in S/Sim
Pre-oxidation
CP/UH
Sokolov
Reflood
S/Sim
S/R5
SF4 hydrogen generation

## Slide 14
Immediate switch to air kinetics calculates too early consumption and starvation of oxygen
Some discrepancy for oxygen exit flow
Comparison with scaled experimental curve indicates better transient evolution and timing if Sokolov steam kinetics are retained during air phase (CP-UH kinetics gave large excursion) Note: this is not proper modelling, only to illustrate above point
start of complete O2 starvation
SF4 oxygen consumption

## Slide 15
  PARAMETER-SF3 and -SF4 analysed with SCDAP/RELAP5 and SCDAP/Sim
    SCDAP/Sim provides better description of facility and better agreement
  SF3 results show important effect of CCFL during top reflood
    reproduced by SCDAP/RELAP5 with recent CFFL correlation
    recommended for plant applications with upper plenum or hot leg injection
  SF4 shows strong thermal response to switch from 3.5 g/s steam to 0.5 g/s air
    initially due to reduced cooling
    oxygen consumption gradually increases, leading to complete starvation
    immediate switch to air kinetics calculates too early starvation
  Default steam kinetic correlation (Cathcart-Pawel/Urbanic-Heidrick) gives better agreement for hydrogen generation than Sokolov, for these cases/models
    applies for both code versions
  New model for air oxidation developed
    currently being implemented in SCDAP/Sim (Mod 3.5)
    analysis of SF4 will continue with this code version
Conclusions and forward plans

## Slide 16
Thank you for your attention
Notes: Beispiel um die Schlussfolie als Danksagung zu nutzen