## Slide 1: The influence of thermogradient conditions on the physicochemical interaction between the suboxidized molten corium and steel during in-vessel melt retention
Presented by V. Granovsky
3rd METCOR-P project meeting
May 27, 2009, St. Petersburg
International Science and Technology Center
A.P. Alexandrov Research Institute of Technology

## Slide 2: Contents
Objectives
Molten pool structure under IVR conditions
Models of a 3-liquid structure
METCOR results with reference to the analysis of the molten pool structure
Components dissolution under isothermal and thermogradient conditions
Vessel steel corrosion model
Conclusions

## Slide 3: Objectives
Systematization of the results from METCOR with reference to the analysis of the thermogradient molten pool structure under IVR conditions

## Slide 4: Qualitative results from METCOR
A solid crust between the oxidic and metallic liquids does not prevent the components repartitioning
Compositions of the metallic part of the system (IZ in METCOR and molten metal in MASCA) differ under isothermal and thermogradient conditions
Corium melt
Steel
Crust
Interaction
zone (IZ)
UO2-ZrO2-Zr
Fe-U-Zr-(O)

## Slide 5: Structure of the molten pool at the reactor vessel bottom under IVR conditions
The composition of the U-Zr-Fe(Cr,Ni,…)-0 system in the miscibility gap determines compositions and, hence, densities of the metallic and oxidic liquids and their position at the vessel bottom relative to each other
When the metallic liquid is at the bottom
- the focusing effect is absent
- Тox  Тmet; numerical codes (that use thermodynamic databases, which can be verified using MASCA results) are applicable
When the metallic liquid is at the surface
- Мmet>Mst  the focusing effect is decreasing in comparison with neglection of components repartitioning
- Тох-Тmet  1000С, i.e., thermogradient conditions; MASCA results are inapplicable; the computational model is absent
A three-liquid pool structure - ?
Metal
Metal
Oxides
Oxides
MASCA results
Conventional structure
Oxides
Metal

## Slide 6: Existing uncertainties and neglected effects influencing the molten pool structure
Accident scenario (composition, masses, sequence of movement towards the bottom)
Properties of multicomponent melts (density)
Condition and properties of the interface (crust) between the oxidic liquid and the metallic one at the top
Physicochemical processes of interaction with vessel steel (influence on the molten pool composition)
Kinetics of physicochemical interaction between the oxidic and metallic melts
Should (and can) the influence of thermogradient conditions be taken into account?

## Slide 7: Three-liquid pool structure
Crust
Seiler’s model
The mass of steel in molten heavy metal is at the maximum, at which density of heavy metal exceeds that of molten oxides
The temperature of heavy metal is close to that of molten oxides – i.e., isothermal conditions
The remaining steel forms the surface layer (light metal)
The temperature of light metal is much lower than that of molten oxides. The oxidic crust that separates them excludes the possibility of components repartitioning  contradicts METCOR results
Comments:
The model is conservative from the point of view of the minimal thickness of the metallic surface layer
The model is not conservative from the point of view of the possibility of an isolating crust formation on the surface of the metallic liquid, provided U and Zr are present in it
Heavy metal
Light metal
Oxides

## Slide 8: Three-liquid pool structure (2) Computational model (basic)
Computational models of a two-liquid pool under isothermal (available) and thermogradient (absent) conditions are required
Steel partitioning into 2 parts – the hot and cold ones – is specified
Molten oxides are conventionally subdivided into 2 parts - Ох1 and Ох2, which independently interact with hot and cold steel
A solution is sought iterationally by selecting fractions of Ох1 and Ох2, until identity in compositions of both parts of molten oxides (internal iterations) has been achieved. Densities of the melts are determined
The maximum mass of Steel1 (which makes density of heavy metal bigger than that of oxides) is determined through selecting fractions of Steel1 and Steel2 (external iterations)
Steel 2
Ox 2
Ox 1
Steel 1
Light metal
Oxfin 2
Oxfin 1
Heavy metal
Comments:
The availability of a model of a two-liquid thermogradient pool makes an additional model of the three-liquid pool unnecessary
It is more realistic than the Seiler’s model

## Slide 9: Quantitative results from METCOR
Only MC9 can be used for comparing with MASCA

## Slide 10: A comparison of results from МС9 and MASCA. A two-liquid system
  For a comparison with MASCA, parameters of the liquid phase should be separated from those of the liquid-solid IZ, as the solid phase does not interact with molten oxides
GEMINI / NUCLEA calculations
C-30; (U/Zr)at = 1.1; =10.8
Fe concentration and U/Zr atomic ratio in the metallic melt under
thermogradient conditions is sufficiently higher than under isothermal ones
40
50
50
70
80
90
1000
1100
1200
1300
1400
1500
T, C MC9
U, Zr Mass.% Fe
60

## Slide 11: A comparison of compositions of the “hot” (metallic body) and “cold” (in the IZ) metallic liquids in MC6 and MCP-1. A three-liquid system
A considerable difference in compositions of the “hot” and “cold” metallic liquids in a three-liquid system
According to the METCOR conditions (i.e., the fraction of interacting steel is below 10%), both liquids are heavy
Basically, the results of METCOR may be used for verifying computational models of the 2- and 3-liquid thermogradient systems

## Slide 12: Corrosion of the cooled vessel steel in the suboxidized molten corium
Crust
Corium
IZ
Steel
Water
The IZ is formed as a result of two processes, namely:
- components repartitioning between the metallic melt in the IZ and
molten corium
- steel dissolution in the metallic melt in the IZ
Formation of the IZ leads to changes in the molten corium composition
A model for calculating the depth of corrosion and the U and Zr masses transferred into IZ is additionally required for determination of pool composition and structure

## Slide 13: Dissolution
Dissolution will continue as long as the fraction of the liquid phase in the system keeps increasing (not reducing) along with the increasing fraction of the component dissolving in the system  l / i  0
The dissolution boundary criterion  l / i < 0, i = imin
ТА
1
2
В А,1 А,2 А
TB
T0
Teut
A,2= f (T) is the liquidus line
Isothermal conditions
l is the liquid phase fraction; i is the dissolving component fraction

## Slide 14: Dissolution (2) Thermogradient conditions
М1; А,1
А
MA,max
M*A,max
Teut T2 T1
MA
T2
Teut
В А,1 *А,2 А,eut А,2 А
ТB
Т1
ТА
2
2
Тeut
Т2
MA,max is the mass of the component А, found between the initial position of the interface and position of the isothermal surface Тeut
If А,2А,eut – the temperature boundary of dissolution is Тeut
If А,2>А,eut – the temperature boundary of dissolution is T2> Тeut
(II) T=f2(A) is the liquidus line
(III) MA=f(T) links the dissolved mass with the temperature at the dissolution front
(I)

## Slide 15: Final position of the IZ boundary in METCOR
U, Zr Mass.% Fe U, Zr Mass.% Fe
40
50
60
70
80
90
1000
1100
1200
1300
1400
1500
40
50
60
70
80
90
1000
1100
1200
1300
1400
1500
T, 0C MC6 T, 0C MC8
1000
1100
1200
1300
1400
1500
40
50
60
70
80
90
1000
1100
1200
1300
1400
1500
30
40
50
60
70
80
90
30
40
50
60
70
80
90
1000
1100
1200
1300
1400
1500
T, 0C MC7 T, 0C MC9 T, 0C MCP-1
U, Zr Mass.% Fe U, Zr Mass.% Fe U, Zr Mass.% Fe
МС6, МС8 – the boundary is Тliq
МС7, МС9, MCP-1 – the boundary is Тeut

## Slide 16: Final position of the IZ boundary in METCOR (2)
MFe=f7(T) is determined by the temperature field in the specimen
T=f8(Fe,IZ; (U/Zr)IZ) is the liquidus line
U,Z Fe,IZ,1 Fe,eut Fe,IZ,2 Fe
IZ
Мох Тох
Teut
MFe,max
If Fe,IZ> Fe,eut
Fe,Z
Fe,IZ,2
Fe,eut
Fe,IZ,1
1
2
(II)
(I)
(III)
(V)
(IV)
A solution of system of the equations (I)…(V) yields all the unknown parameters, including the temperature at the IZ boundary
Teut
1
2

## Slide 17: Final position of the IZ boundary in METCOR (3)
The number of tests is insufficient for a generalization
Other conditions being equal, a bigger Сn determines a bigger Fe,IZ , like in MASCA
Other conditions being equal, Fe,IZ is bigger for a three-liquid system than for a two-liquid one
Judging from МС7, when  0, Fe,IZ tends to the final value, unlike in MASCA

## Slide 18: Conclusions
The molten pool composition and structure determination under IVR conditions require a model of a two-liquid thermogradient system
The data for said model development and verification can be obtained either from tests analogous to those in MASCA (however, ensuring a temperature difference between the oxidic and metallic liquids), or to those in METCOR
To check the proposed model of determining the IZ temperature boundary, it may be reasonable to performe a test analogous to МС6, but with C-95 oxidation index. A rise of the boundary temperature up to 1300…1400С and the IZ composition that corresponds to that at the liquidus line can be expected