## Slide 1: ISTC project K-1265: Experimental study of core melt in-vessel retention IN-VEssel COrium Retention (INVECOR)
Presented by Vladimir Zhdanov
IAE NNC RK
CEG-SAM 17th Meeting,
March, 29 – 31, 2010
Madrid, Spain

## Slide 2: General information
Project K-1265 has been started from May 1, 2006. It is 16th quarter of Project performance. Planned date of project finishing is April 30, 2010
Technical report on 3 years of Project performance is available in CEG-SAM web-site
Operations have been fulfilled according to the specified Work Plan.

## Slide 3: Project tasks short description
Task 1: Modernization of test facilities and optimization of melting process and simulation of decay heat
technique for protection coating of the graphite crucible and electrode nozzles of plasmatrons has been developed and tested
corium melting mode and its discharge into experimental section has been improved (2 large scale calibration tests)
design and operating modes of the device for decay heat simulation have been developed and tested (7 TOP tests and many plasmatrons tests without corium)
design and manufacturing of RPV model have been done
Task 2: Calculation support of experiments
Pre-test and post test calculation have been performed
Task 3: Large-scale experiments
Four large scale integral tests on transient processes of IVR imitation have been conducted
Task 4: Post-test analysis
Post-test analysis of corium and RPV steel is under way

## Slide 4: Testing of device for decay heat modeling
TOP-2 test
Temperature of inner vessel wall
(temperature of plasmatrons surface was 2650 C)
Scheme of loading

## Slide 5: Corium melt preparation
Electric melting furnace (EMF)
Pyrometer
Heat exchanger
Water cooled housing
Graphite crucible
Inductor
Device for plug splitting
Thermal insulation
Bottom supporting sleeve

## Slide 6: Loading of the melting crucible in EMF
6
Material in electric melting furnace |  |  | 
UO2, g | Zr, g | ZrO2, g | m (Total), g
45720 | 8815 | 5580 | 60115
Zirconium rods
UO2+ZrO2 mix

## Slide 7: Second calibration test
Diagram of corium heat-up
Corium ingot after test (U0,9Zr0,1O2)
(this corium was used for additional loading in the RPV model)

## Slide 8: Test section (RPV model)
Main concept of RPV model design
Longitudinal section of experimental assembly including device for decay heat modeling

## Slide 9: Test section
Test section including device for decay heat modeling inside pressure vessel of large scale facility

## Slide 10: RPV models before tests
10
Test | Material in electric melting furnace |  |  |  | Add corium in RPV model | Total in test | Corium in RPV model after test
 | m (UO2), g | m (Zr), g | m (ZrO2), g | m (Total), g | g | g | g
INECOR-1 | 45720 | 8815 | 5580 | 60115 | ‑ | 60115 | ‑
INECOR-1/2 | 45720 | 8430 | 4830 | 58980 | ‑ | 58980 | ‑
INECOR-1/3 | 46200 | 8530 | 5285 | 60015 | 10000 | 70015 | 47040
INECOR-2 | 46200 | 8485 | 5340 | 60025 | 9400 | 69425 | 68928
INECOR-3 | 46200 | 8491 | 5326 | 60017 | ‑ | 60017 | 58445
INECOR-1/4 | 46200 | 8495 | 5340 | 60035 | ‑ | 60035 | 55370
The tantalum screen
Steel screen
SS clad
Graphite felt
Solidified corium
Thermal insulation (asbestos)
Copper brackets
Thermal insulation (glass cloth)
Thermal insulation (asbestos)
Notes: 10

## Slide 11: Thermocouples placement in RPV model
Additional thermocouples have been installed for INVECOR-1.4 test between MDT.14 and MDT.24

## Slide 12: Diagrams of IVR modeling
INVECOR-2
Test duration – 50 minutes
Maximum temperature of RPV model – 1050 C
Maximum plasmatrons power – 74 kW
INVECOR-1.3
Test duration – 1 hour
Maximum temperature of RPV model – 820 C
Maximum plasmatrons power – 65 kW
Test duration time from melt discharging to plasmatrons switching off

## Slide 13: Diagrams of IVR modeling
INVECOR-3
Test duration – 1 hour
Maximum temperature of RPV model – 1350 C
Maximum plasmatrons power – 78 kW

## Slide 14: Diagrams of IVR modeling
INVECOR-1.4
Test duration 2 hours
Maximum temperature of RPV model – 1400 C
Maximum plasmatrons power – 75 kW

## Slide 15: Corium placement in RPV model after tests
15
Fragmented material dropped from tantalum cone (during melt discharging)
Fragmented debris bed
Corium ingot
Corium ingot containing stainless steel components
Adhered ingot
Fraction of fragmented debris above corium ingot is higher at highest temperature in RPV model
Notes: 15

## Slide 16: Results of post-test calculation (1)
Test INVECOR-1.3: Temperature field in RPV model in 1 hour after melt discharging
Test INVECOR-2: Temperature field in RPV model after plasmatrons switching off

## Slide 17: Results of post-test calculation (1)
Test INVECOR-3: Temperature field in RPV model after plasmatrons switching off
Test INVECOR-1.4: Temperature field in RPV model after plasmatrons switching off
Note. Maximum measure temperature was in the central part of RPV model

## Slide 18: Post-test research after INVECOR-1/3 test
18
S 1
S2
S3
F1
F2
S 4
200 m
100 m
S5
S6
Sample | Phase composition | Element composition, wt.% |  | 
 |  | Zr | U | U/Zr
F1 | U0.95Zr0,05O2; α-Zr(O); ZrO2MKL; Zr(O,N,С)1-x; (Zr,U)O2 | 31,6% | 68,4% | 2,17
F2 | U0.95Zr0,05O2; α-Zr(O); (Zr,U)O2 ZrO2MKL; | 34,0% | 66,0% | 1,94
S 1 | U0.95Zr0,05O2 α-Zr(O); α-(U,Zr) | 31,6% | 68,4% | 2,16
S 2 | U0.9Zr0,1O2 α-Zr(O); α-(U,Zr) | 30,3% | 69,7% | 2,30
S 3 | U0.9Zr0,1O2 α-Zr(O); α-(U,Zr) | 31,7% | 68,3% | 2,16
S 4 | U0.9Zr0,1O2 α-Zr(O); α-(U,Zr) | 31,2% | 68,8% | 2,20
S 5 | U0.9Zr0,1O2 α-Zr(O); α-(U,Zr) | 32,4% | 67,6% | 2,08
S 6 | U0.9Zr0,1O2 α-Zr(O); α-(U,Zr) | 31,2% | 68,8% | 2,20

## Slide 19
19
Post-test research after INVECOR-2 test (1)
F 1
S 3
S 1
S 2
S 4
S 5
S 6
S 7
S 8
F 2
Ingot surface faced to RPV model
Sample | Phase composition | Element composition, wt.% |  | 
 |  | Zr | U | U/Zr
F 1 | U0.95Zr0,05O2); ZrO2tetrag; ZrO2mcl; (U,Zr)(C,O)1-x | 20,4% | 79,6% | 3,89
F 2 | U0.95Zr0,05O2; ZrO2tetrag; ZrO2mcl; (U,Zr)(C,O)1-x | 19,4% | 80,6% | 4,15
S 1 | U~0.95Zr~0,05O2; α-(U,Zr) | 23,6% | 76,4% | 3,23
S 2 | U~0.95Zr~0,05O2; α-(U,Zr) | 25,0% | 75,0% | 3,00
S 3 | U~0.95Zr~0,05O2; α-(U,Zr) | 22,7% | 77,3% | 3,41
S 4 | U~0.95Zr~0,05O2; α-(U,Zr) | 24,9% | 75,1% | 3,02
S 5 | U~0.95Zr~0,05O2; α-(U,Zr) | 23,8% | 76,2% | 3,21
S 6 | U~0.97Zr~0,03O2; α-(U,Zr) | 21,6% | 78,4% | 3,64
S 7 | U~0.97Zr~0,03O2; α-(U,Zr); (U,Zr)Fe2 | 20,3% | 79,7% | 3,93
S 8 | U~0.9Zr~0,1O2; α-(U,Zr); (U,Zr)Fe2 | 22,4% | 77,6% | 3,47
Corium ingot fragment from central part of RPV model

## Slide 20
20
Post-test research after INVECOR-2 test (2)
Section of corium ingot in central part of RPV model
Section of corium ingot under plasmatrons
150 m
25 m
(U, Zr)O2
Zr(O,N,С)1-x
α-(U,Zr)
500 m

## Slide 21
21
Post-test research after INVECOR-3 test
F 1
F 2
S 5
S 4
S 1
S 2
S 3
Sample | Phase composition | Density, g/cm3 | Thermal conductivity (at 20 deg. C), Wtm-1K-1
F 1 | U0.95Zr0,05O2; ZrO2tetr; ZrO2mcl; (U,Zr)(C,O)1-x |  | 
F 2 | U0.95Zr0,05O2; ZrO2tetr; ZrO2mcl; (U,Zr)(C,O)1-x |  | 
S 1 | U~0.97Zr~0,03O2; U6Fe(?); α-(U,Zr); (U,Zr)Fe2 | 9,85 | 6,93
S 2 | U~0.98Zr~0,02O2; (U,Zr)Fe2; U6Fe(?); | 10,0 | 6,90
S3 | U~0.95Zr~0,05O2; UO2; (U,Fe)C2; |  | 
S4 | (U,Zr)Fe2 ; U~0.75Zr~0,25O2; U~0.95Zr~0,05O2; Zr2FeOx |  | 
S5 | U~0.95Zr~0,05O2; UO2; (U,Fe)C2 |  | 

## Slide 22
22
Post-test research after INVECOR-1/4 test (1)
F 1
F 2
S 1
S 2
Fragment of RPV wall from the central part (top view)
S 6
S 5
S 4
S 3
Fragment of corium ingot from the contact with RPV model wall

## Slide 23
Post-test research after INVECOR-1/4 test (2)
Sample | Phase composition | Element composition, wt.% |  |  | U/Zr
 |  | U | Zr | Fe | 
F 1 | U0.85Zr0,15O2; ZrO2mcl; ZrO2tetr ; U0.5Zr0, 5O2; UO2; U3O8 |  |  |  | 
F 2 | U0.94Zr0, 06O2; U0.8Zr0,2O2; ZrO2mcl; ZrO2tetr; α-Zr(O); U0.5Zr0, 5O2; U3O8 |  |  |  | 
S 1 | U~0.95Zr~0,05O2; α-Zr(O); α-(U,Zr); Zr2FeOx | 29,8 | 69,8 | 0,46 | 2,3
S 2 | U~0.95Zr~0,05O2; α-Zr(O); α-(U,Zr); Zr2FeOx | 31,8 | 67,7 | 0,46 | 2,1
S 3 | U~0.85Zr~0,15O2; (Zr,U)O2tetr; (Zr,U)O2mcl; (U,Zr)(C,O)1-x; Zr2FeOx | 31,1 | 68,6 | 0,32 | 2,2
S 4 | U~0.95Zr~0,05O2 ; α-Zr(O); α-(U,Zr);Zr2FeOx; -Fe | 29,8 | 69,3 | 0,83 | 2,3
S 5 | U~0.95Zr~0,05O2; (U,Zr)Fe2 ; ZrFe3; -Fe; (Zr)(C,O)1-x; α-Zr(O); α-(U,Zr);Zr2FeOx | 25,3 | 58,0 | 16,7 | 2,3
S 6 | U~0.95Zr~0,05O2; (U,Zr)Fe2 ; ZrFe3 -Fe; (Zr)(C,O)1-x; α-Zr(O); α-(U,Zr);Zr2FeOx | 27,5 | 57,2 | 15,3 | 2,1
С 4
С 5
С 1
С 6
Sample | Phase composition | Density, g/cm3 | Thermal conductivity (at 20 deg. C), Wtm-1K-1
C 1 | U~0.95Zr~0,05O2; α-Zr(O); α-(U,Zr); (Zr)(C,O)1-x ;Zr2FeOx | 9,76 | 5,8
C4 | α-Zr(O); (Zr)(C,O)1-x; U~0.95Zr~0,05O2; α-(U,Zr); Zr2FeOx (U,Zr)Fe2 ; -Fe | 10,01 | 5,7
C5 | U~0.95Zr~0,05O2; α-Zr(O); α-(U,Zr); (Zr)(C,O)1-x ;Zr2FeOx; (U,Zr)Fe2 ; -Fe | 9,43 | 5,9
C6 | U~0.95Zr~0,05O2; α-Zr(O); α-(U,Zr); (Zr)(C,O)1-x;Zr2FeOx; (U,Zr)Fe2 | 9,42 | 6,3
23

## Slide 24: Summary
1) Low thermal fluxes from corium through a wall of RPV model were received in the course of experiments that it is possible to explain by:
thermal insulation presence on an external surface of the model leading to redistribution of thermal fluxes to perpendicularly wall and along a wall to the top massive flange of RPV model;
incomplete dissolution of uranium dioxide in the molten zirconium in the electric melting furnace and continuation of endothermal dissolution of urania in the course of IVR modeling;
gap formation between a corium crust and a RPV wall caused by initial thermal expansion of RPV model;
layered character of a lower corium crust, that leads to decrease of effective heat conductivity of a crust.
2) Steady-state phenomena during IVR substantially depend on:
previous transient processes connected with formation of corium pool in a reactor core;
time of existence of this pool in an average elevation of core;
character and speed of the melt dropping on the lower head.
The final report by results of work on the project will be placed in CEG web-page after finishing of the project (May-June, 2010)

## Slide 25: Acknowledgments
Project INVECOR was carried out at financial support of EC. I am very grateful to collaborators of the project from
СЕА, Saclay and Cadarache;
FZK and JRC-ITU, Karlsruhe;
FZR, Dresden;
Pisa University;
for recommendations on test conditions and useful discussions and the analysis of obtained results.
I am grateful also to employees of the NITI for active participation in the project and to IBRAE employees for useful discussions.
Thanks a lot to all CEG-SAM participants and to ISTS employees for supporting of INVECOR project.
I hope for the further fruitful cooperation