## Slide 1
Results of PARAMETER –SF3 pre- and post-test numerical modeling
15th CEG-SAM Meeting, Villigen, Switzerland, 10-12 March 2009 г.
Presented by A.Kiselev

## Slide 2: Used codes and participants for SF3 calculations
SOCRAT –IBRAE
ICARE/CATHARE - NSI RRC KI
ATHLET-CD – GRS
RELAP/SCDAPSIM MOD3.2 (RELAP) - FSUE EDO “GIDROPRESS”
SCDAP/RELAP/IRS (RELAP/IRS) –PSI
PARAM-TG - FSUE SRI SIA “LUCH”

## Slide 3: PARAMETER-SF3 test bundle for pretest calculations (Specification)
Bundle type VVER-1000
- number of fuel rods 19
- heated 18
- unheated 1
Fuel rod
- cladding, mm  9,13/7,73
(Zr1%Nb)
pellets UO2
- heater length , mm 1275
Spacer grid Zr1%Nb Shroud Zr1%Nb
-SF3, -SF4 cylindrical
Heater Ta
Thermal insulation ZrO2 ZYFB-3

## Slide 4: PARAMETER-SF3 pre-test calculations Initial and Boundary conditions
Electrical power:
Pre-oxidation phase ~ 7.7 kW
Transient phase ~ 10.5 kW

## Slide 5: Heat balance PARAMETER-SF3 pre-test analysis

## Slide 6: Heat balance PARAMETER-SF3 pre-test analysis
Heat loss through shroud
at pre-oxidation phase
~15% of core power over 0-1275 mm

## Slide 7: Claddings temperature evolution - hottest zone PARAMETER-SF3 pre-test analysis

## Slide 8: Claddings temperature evolution: 700-900 mm PARAMETER-SF3 pre-test analysis

## Slide 9: Shroud temperature evolution PARAMETER-SF3 pre-test analysis

## Slide 10: Temperature profile PARAMETER-SF3 pre-test analysis

## Slide 11: Oxide scale thickness PARAMETER-SF3 pre-test analysis

## Slide 12: Hydrogen release PARAMETER-SF3 pre-test analysis
Hydrogen release predicted ~ 13-32 g
No extra hydrogen release at the flooding stage

## Slide 13: Flooding Phase (SOCRAT calculations)

## Slide 14: Modified SF3 test bundle

## Slide 15: PARAMETER-SF3 post-test calculations Initial and boundary conditions

## Slide 16: Heat balance PARAMETER-SF3 post-test analysis
Oxidation reaction power
Pre-oxidation phase - up to 1kW
Before flooding up to 10 kW
Joel heating power
Pre-oxidation phase~ 6-8 kW
Before flooding onset ~ 9-11 kW

## Slide 17: Heat balance PARAMETER-SF3 post-test analysis
Coolant heating power
Pre-oxidation phase ~5- 6 kW
Before flooding onset ~ 8-10 kW
Radial heat loss through shroud
Pre-oxidation phase ~ 0.5-1 kW
Transient and flooding phase ~ 2 kW

## Slide 18: Claddings temperature evolution PARAMETER-SF3 post-test analysis

## Slide 19: Shroud temperature evolution PARAMETER-SF3 post-test analysis

## Slide 20: Hydrogen release PARAMETER-SF3 post-test analysis
Hydrogen release
Experimental ~34 g
ICARE ~ 33 g
PARAM-TG – 32 g
SOCRAT ~ 26 g
RELAP – 32 g
No hydrogen release at flooding phase

## Slide 21: Cladding oxide scale thickness PARAMETER-SF3 post-test analysis

## Slide 22: Main outcomes from SF3 post-test calculations
Post-test calculations and experimental data on temperature evolution are in a good agreement
The most codes estimate hydrogen total amount well.