## Slide 1
Project Title
#3831 (MCCI) «Development and experiments at large-scale installation for heating and retention of corium» Part I.
(Work Plan)
Tasks: - to develop a technology of PTC producing and retention of corium;
- to develop a measuring system for corium temperature and concrete heat flow diagnosis;
- to establish a middle-scale installation and to carry out experiments on corium and concrete interaction.
Installation characteristics:
- mfin ≈100-120 kg;
- Vfin = 15-18 l;
- Тfin = 2500-2700 С;
- Р = 100 kW/m2;
- t = 10-12 min.

## Slide 2
I. General geometry of a middle-scale experiment
200
50
150
200
200
 300
 1000
 120
200
н | 1 m
H | 0.6 m
в | 0.3 m
Hв | 0.4 m
m0 | 25-30 kg
mfin | 100-120 kg
62%ZrO2+38%Fe | 
P | 100kW/m2
T | 2500-2700C
Hp | 0.15-0.2 m
PTC: 2Fe2O3 + 3Zr = 3ZrO2 + 4Fe + 2800 kJ/kg
1

## Slide 3
II. Composition recommended for the middle-scale experiment
Test | VB-U4 | VB-U5 | VB-U6
Corium load composition | 45 wt.% UO2, 19% ZrO2, 20% SiO2, 15% Fe2O3 | 45 wt.% UO2, 19% ZrO2, 20% SiO2, 15% Fe2O3 | 45 % UO2, 19% ZrO2, 20% SiO2, 15% Fe2O3
Corium mass | 45 kg | 28 kg | 31 kg
Concrete chemical composition (after drying) | 63 wt.% SiO2, 25% CaO, 5% Ai2O3, 9% CO2, 3% H2O | 63 wt.% SiO2, 25% CaO, 5% Ai2O3, 9% CO2, 3% H2O | 25 wt.% SiO2, 41% CaO, 2% Ai2O3, 25% CO2, 3% H2O
Initial Temperature | 2200 К | 2200 К | 2200 К
Test duration | 2 hr | 2.5 hr | 2 hr
Ratio of horizontal to vertical ablation | 2.5 : 1 | 5 : 1 | 2 : 1 the first hour 1: 1 the next hour
Concrete composition recommended
for the middle-scale experiment
2

## Slide 4
Igniting wire
Collector
Initiating
system
Injector
PTC
(3Zr + 2Fe2O3)
30 kg
Concrete tank
III. Equipping scheme of PTC into the concrete tank.
3

## Slide 5
IV. PTC initiating and burning scheme
Initiating of PTC burning by means of igniting wire
Collector
Injector
Burning compound
(3Zr + 2Fe2O3=
=3ZrO2+4Fe+Q)
Concrete tank
Gas mixture
(propane + air)
20-30 kW
4

## Slide 6
V. Scheme of melt temperature and heat flows support using briquettes burning
Collector
Injector
Melt
3ZrO2+4Fe
Concrete tank
Gas mixture
(propane + air)
Briquette
5
m0=25-30 kg
mfin≈100 kg
t = 10-12 min
m=0.5-1kg
t=5-10 s

## Slide 7
Briquettes producing
(m=0,5-1kg)
Zr
Fe2O3
3Zr+2Fe2O3
VI. Briquettes production process scheme
Blocks pressing
(m=0,1kg)
Preparation of PTC
Preparation of
powder compounds
6

## Slide 8
PC

VII. Scheme of carrying out the temperature measurements
N=8
N=24 (6 groups of 4 items)
1
2
3
4
1=5
2=10
3=15
4=20
Zirconium oxide tube (ZrO2)
Optical monofilament (=400mkm)
32 thermocouples
P2
P8
P1
…………………………….
250
7

## Slide 9
VIII. Thermocouples construction and preparation technology
8
Chromel-Allimel thermocouples – up to 1500
Rhenium-Tungsten thermocouples – up to 2500

## Slide 10
IX. Experiment visualization
9

## Slide 11
Middle-scale experiment | Large-scale experiment
1. To develop and produce the concrete tank for corium | 1. The same
2. To develop the technology and produce pyrotechnic briquettes Fe2O3+Zr (100 kg) | 2. To develop the technology and produce pyrotechnic briquettes Fe2O3+U (1000 kg)
3. To develop the technology of pyrotechnic briquettes initiating | 3. The same
4. To develop the technology of pyrotechnic briquettes dumping into the molten pool | 4. The same
5. To develop and make the measuring system of the melt temperature by means of pyrometry | 5. The same
6. To develop and make the measuring system of the melt temperature and heat flows in concrete by means of thermocouples | 6. The same
7. To develop the technology of the frozen melt cutting | 7. The same
8. Metallographic analysis of the frozen melt composition | 8. The same
9. Design-theoretical analysis of experimental results | 9. The same
X. Scope of activities