## Slide 1: Interaction of suboxidized molten corium with European vessel steel
A.P. Alexandrov Research Institute of Technology (Russia)
Presented by V. Granovsky
4th METCOR-P Meeting
St. Petersburg, Russia,
June 1, 2010
TEST MCP-5

## Slide 2: Contents
Experimental objectives
Schematics
Experimental procedure
Experimental results
Post-test analysis
Comparison of corrosion characteristics for the European and Russian vessel steels
First conclusions

## Slide 3: Objectives
Comparison of corrosion rate and depth for European and Russian vessel steels at their interaction with suboxidized molten corium

## Slide 4: Gas-aerosol system
1 – Ar tank; 2 – silica gel drier; 3 – flow-rate transducer; 4 – cyclone; 5 – LAF filter; 6 – AFA filter; 7 – electrochemical oxygen detector; 8 – hydro lock; 9,10 – vacuum pump

## Slide 5: Experimental procedure

## Slide 6
Specimen temperatures versus time
Thermocouple readings in the plot are interrupted when a TC breaks down
As the heated top-level TCs break down, the stationary regime is controlled using the indications of lower and cooler thermocouples

## Slide 7
Corrosion depth dynamics
Long incubation period - approximately 20 000 s
Corrosion decreases as its front progresses into the specimen bulk – a lower-temperature region
Corrosion process is not finished ?
Uncertaint sounding interpretation
0
2
4
6
8
10
12
0
10000
20000
30000
40000
50000
Time, s
MCP-5
h, mm
Uncertaint sounding
interpretation
 – US measurement;  – Post test measurement of specimen section

## Slide 8: Specimen axial section
The section is perpendicular to the ultrasonic defect axis
Non-even boundary of the interaction zone
2 different structures in the IZ visible at the macrolevel
mass.%
U – 40
Zr – 16
Fe – 42
?
Molten oxidic pool having free surface
C-30; TB=1060-1250C; hB=10mm

## Slide 9: Specimen temperature conditions and IZ final boundary position in the end of the test
Calculated by the ANSYS code using the measured boundary conditions and temperatures in TC locations
A – initial position of the specimen surface, В – final boundary of the interaction zone
The IZ boundary is located in the 1060 - 1250 C temperature region
Т,oC
h, m
A

## Slide 10: Comparison with corrosion of Russian vessel steel
U – 25.6
Zr – 5.4
Fe – 64.4
MC6
mass.%
Molten oxidic pool with the surface crust
C-30; TB=1120-1200C; hB=6mm; 1 layer in IZ

## Slide 11: Comparison with corrosion of Russian vessel steel (2)
U – 27.0
Zr – 11.0
Fe – 56.0
U – 39.5
Zr – 5.4
Fe – 50.0
MC9
mass.%
Molten oxidic/metallic pool having free surface
C-30; TB=1060-1100C; hB=15mm; 2 layers in IZ

## Slide 12: Comparison with corrosion of Russian vessel steel (3) Vertical position of interface
U – 52.4
Zr – 13.7
Fe – 32.2
U – 36.4
Zr – 14.3
Fe – 49.1
MCP-1
Molten oxidic pool
with the surface crust
C-17; TB=1000-1190C; hB=6mm
2 layers in IZ
mass.%

## Slide 13: Corrosion kinetics of Russian vessel steel

## Slide 14: Comparison with corrosion kinetics of Russian vessel steel
Corrosion kinetics
1
2
Exp.
Correlations for corrosion rates
Russian steel (4 summarized tests)
European steel
h, mm
t, s

## Slide 15: First conclusions
Corrosion kinetics in MCP-5 and МС6 tests are qualitatively similar and have an incubation phase, transient to fast corrosion and saturation phase
In comparison with МС6 the MCP-5 incubation period increased from 16000 s to 20000 s
Differently from МС6 the final boundary of interaction zone is irregular (not smooth)
The final position of the interaction zone boundary was found in the temperature range of 1060-1250 С ( for comparison: МС6 – 1120…1200С)
Posttest analysis is in progress