## Slide 1: Interaction of SS – Zr – U melt with vertically positioned vessel steel specimen. Test MCP - 8
A.P. Alexandrov Research Institute of Technology (Russia)
Presented by V. Granovsky
5th METCOR-P Meeting
St. Petersburg, Russia
June 7, 2011

## Slide 2: Contents
Objectives
Schematics
Experimental procedure
Test results
Post-test analysis
Physicochemical analysis
Corrosion kinetics
Conclusions

## Slide 3: Objectives
Determine corrosion kinetics and final corrosion depth of vertically positioned vessel steel specimen at its interaction with SS-Zr-U melt
Test parameters :
SS-U-Zr melt corium
15Kh2NMFA vessel steel
Pure argon above the melt
10 h exposition

## Slide 4: Specimen schematics

## Slide 5: MCP-8 furnace schematics
1 – cooled SS cover
2 – quartz tube
3 – cooled copper screen
4 – specimen
5 – inductor
6 – bottom calorimeter
7 – supporting screen
8 – crucible sections
9 – crucible collector
– melt
– US sensor
1
2
3
4
6
7
8
5
9
10
11

## Slide 6
TC locations in the specimen
Specimen section
Coordinates of hot junctions

## Slide 7
SS
Zr
U
Crucible charge
Oxidic powders were placed around SS body (except the gap with specimen)

## Slide 8: Test procedure
Time, s | Stages in the experimental procedure
0-300 | Furnace deoxygenation by argon flow
300-7200 | Formation of the molten pool. Increase of power in the melt to get local maximum of 1400oC of the specimen surface
7200-39300 | Keeping constant specimen temperature by inductor voltage control during ~ 10 hr
39300-41000 | Heating disconnection, melt solidification and ingot cooling in argon

## Slide 9: Test results: TC readings
Damaged thermocouples continue to operate but in a wrong way (new junction is formed to replace the defect one)

## Slide 10: Test results: Powers extracted from the crucible, specimen and bottom calorimeter
Practically constant power into the specimen

## Slide 11: Test results: Ingot view during furnace disassembling
Specimen
Surface oxidic crust
Metallic corium ingot

## Slide 12: Test results: Ingot side views
Specimen top
Ingot
Specimen surface with corium
US sensor calorimeter
TC cables

## Slide 13: Posttest analysis Specimen axial section (0º, see slide 6)
1
2
2
1 – Steel of initial structure 2 – Zone of thermal influence 3 - Interaction zone
Maximum corrosion depth – 9 mm at the elevation of 40 mm
Acoustic ‘mirror’
Acoustic defect
Thermocouple
3

## Slide 14: Post-test analysis (2) Cross section, 30 mm elevation (reconstruction)
Specimen
Isotherm of Fe-Fe3C
eutectic formation
(727C)
Metallic corium crust

## Slide 15: Post-test analysis (3)
Axial section schematics
Cross section schematics
Isotherm of Fe-Fe3C
eutectic
Final boundary
Initial boundary

## Slide 16: Post-test analysis (4)
T, C
Radial distribution I
O –specimen axis
А – isotherm of Fe-Fe3C eutectoid formation (727C)
1 – 400; 2 – 500; 3 – 600; 4 – 700; 5 – 800; 6 – 900; 7 – 1000; 8 - 1100 C
Axial section
Temperature of corrosion boundary final position is in the range of 1050…1150 C
Temperature conditions calculated by ANSYS

## Slide 17: Post-test analysis (5)
T, C
T, C
T, C
r, mm
r, mm
r, mm
Temperature field of the specimen cross section (elevation of TC location: 30 mm)
Radial distribution II
Radial distribution III
Radial distribution I
T, 0C

## Slide 18: Post-test analysis (6)
Temperature at the surface of the specimen – Tliq of the melt (1220°C, see slide 19)
Average melt temperature (~1280°C) is higher than liquidus temperature by approx. 50°C
Molten pool modeling

## Slide 19: Physicochemical analysis
T, º C
Fe
U, Zr, Cr, Ni
Temperature of specimen
final boundary
Ingot (melt) composition
Minor oxygen content in metal due to low melt temperature
Temperature of specimen final boundary is equal to the minimal value of liquidus temperature of the phase diagram section
Section of phase diagram (GEMINI 2, v.3.41 / NUCLEA 10.1)
Ingot composition, mass% (XRF) |  |  |  |  | 
U | Zr | Fe | Cr | Ni | Si
35.2 | 14.2 | 36.7 | 8.6 | 5.0 | 0.3
mass. %

## Slide 20: Physicochemical analysis(2)
Probably Seiler defined the Fe dissolution limit as a minimal liquidus temperature.
 | Zr | Sn | Cr | Ni | Fe | U
M, kg | 8000 | 300 | 5000 | 3000 | 18000 | 8600
Froment K., Seiler J. M. et al. Physico-Chemistry and Corium Properties
for in-Vessel Retention. In-Vessel Core Debris Retention and Coolability
Workshop Proceedings, 3–6 March, 1998, Garching near Munich, Germany
Temperature limit of Fe dissolution - 1100ºC
T, ºC
U, Zr, Cr, Ni
Fe
mass. %

## Slide 21: Physicochemical analysis(3)
If the composition of interaction zone is in the initial crystallization zone of U, Zr, the temperature at the final corrosion boundary is equal to solidus temperature.
Sections of U-Zr-Fe phase diagram
- experiment
 - calculation
Interaction of the vessel steel with suboxidized corium melt

## Slide 22: Physicochemical analysis(4)
The content of iron in the melt at the boundary with specimen achieves the value corresponding to the minimal liquidus temperature (55%) . Therefore, further dissolution of steel is impossible.
SEM/EDX MCP-8
 | Mass % |  |  |  | 
 | U | Zr | Fe | Cr | Ni
SQ2 | 20.9 | 10.7 | 56.6 | 9.1 | 2.1
SQ3 | 24.2 | 15.4 | 49.5 | 6.6 | 3.5
SQ4 | 24.4 | 22.1 | 43.8 | 5.0 | 4.7
Ingot | 35.2 | 14.2 | 36.7 | 8.6 | 5.0

## Slide 23: Physicochemical analysis(5)
The content of iron in the melt at the boundary with specimen is less than the value corresponding to the minimal liquidus temperature (65%) , i.e. the composition is in the initial crystallization zone of U, Zr. Therefore, Fe dissolution occurs to solidus temperature.
SEM/EDX MCP-1
 P1
 P2
U – 38.3; Zr – 6.9; Fe – 51.2; Cr – 1.9; Ni – 0.8, mass %

## Slide 24: Сorrosion kinetics
1
2
Correlations for corrosion rates
MCP-8 (metallic melt, vertical interface)
MC6, MC7, MC8, MC9 (oxidic melt, horizontal interface)
h, mm
t, s
(+8800)
 - direct post-test measurement
- post-test processing of on-line US-measurement
No tests with metal melt and horizontal interface

## Slide 25
Conclusions
No indications of interaction interface orientation effect on steel corrosion by U-Zr-Fe-Cr-Ni metal melt. Physicochemical effects are governing.
The lowest corrosion temperature limit is determined by the minimal liquidus-temperature value of the phase diagram section, which corresponds to the melt composition. For MCP-8 conditions it was ~1100°C.
The correlation describing the “fast” corrosion period under interaction of steel vessel with metal melt is close to that previously derived for interaction with suboxidized corium melt.