## Slide 1
Fuel assembly tests under severe accident conditions (PARAMETER Facility)
13-16 September, 2004, Dimitrovgrad
NPO “LUTCH”
IBRAE RAS
Presented by N.Ya.Parshin

## Slide 2: Content
Introduction
Experimental facility and equipment
Modeling
Project proposal
  Goals
  Tasks
  Results

## Slide 3: Introduction
ISTC – 1134: Development and Fabrication of Experimental Facility Supplementary Equipment and Control System and Monitoring System Relating to Simulation of VVER (PWR) Severe Accident Scenarios and Tests of Fuel Assemblies and Fuel Rods as well as Their Elements
Leading institute: NPO Lutch, Podolsk, Moscow reg., Russia
Date: October 1997
Status: Delayed without approval

## Slide 4: Goals of PARAMETER Tests: top and bottom flooding of overheated bundle.
Bundle behavior (Тcore 1200оС) under DBA conditions :
  Cladding deformation;
  Fuel rod depressurization :
  Blockage formation;
  Post test material examination of claddings and spacer grids.
Bundle behavior (Тcore1200оС) under SA conditions:
  Hydrogen release;
  Bundle degradation;
  Material properties.

## Slide 5: Experimental Facility
Model FA type | VVER
Number of FE | up to 37
FE length, mm | up to 3500
Fuel | UO2 pellets
Initial inner pressure in FE, MPa | 2,0 – 3,0;
Heat insulation | ZrO2;
Coolant flow rate, g/s per FE | up to 0,2
FA test temperature: DBA, оС Severe accidents, оС | up to 1200; up to 2000;
Integral electric power, kW | up to 400
Water flow rate in the system of “top” and “bottom” FA flooding, g/s | up to 200
Cooling water temperature, оС | up to 60

## Slide 6: Bundle Specification
Heated rod
Unheated rod
Bundle

## Slide 7: Instrumentation
Recording process-system parameters (U, I, T, p – up to 100 control points);
Collection and recording test parameters of model FA (U, I, T, p – up to 200 control points);
Gas analysis (hydrogen concentration) system;
Post-test operations (model FA flooding with a compound to fix position of its elements; partial/complete cutting; video recording, photography, etc.) and transport operations.

## Slide 8
Металлография
Рентгеноструктурный и
рентгенофазовый анализ
Механические испытания
Микрорентгеноспектральный анализ
Cканирующая эл-я микроскопия
Post test Material Examination

## Slide 9: Advantages of PARAMETER Facility
Wide range of possibilities:
  Different assemblies: fuel, cladding, control materials, spacers
  From DBA to BDBA and SA
Use of reactor materials
  UO2 Pellets application available
Modern level of instrumentation
Simulation of accident management measures
  Top and/or bottom flooding

## Slide 10: Set of Performed Tests
Характеристики модельной ТВС и параметры испытаний | Номер модельной ТВС и год проведения испытаний |  |  |  |  |  |  |  |  |  |  |  |  | 
 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14
 | 1999 |  |  | 2000 |  | 2001 |  | 2002 |  | 2003 |  |  |  | 2004
Общее количество твэлов в модельной ТВС, шт. | 19 | 19 | 19 | 37 | 37 | 37 | 37 | 37 | 37 | 37 | 37 | 19 | 19 | 19
Количество нагревательных твэлов, шт. | 19 | 19 | 19 | 24 | 22 | 23 | 36 | 36 | 36 | 36 | 36 | 18 | 18 | 18+ ПЭЛ
Высота активной части, мм | 800 | 800 | 800 | 1275 | 1275 | 1275 | 1275 | 1275 | 1275 | 1275 | 1275 | 1275 | 1275 | 1275
Материал оболочки твэла | Э-110 | Э-635 | Э-110 | Э-110 | Э-635 | Э-110 | Э-110 | Э-635 | Э-110 | Э-110 | Э-635 | Э-110 | Э-110 | Э-110
Исходное давление гелия при 20оС, МПа | 2.0 0.25 | 2.0 0.25 | 2.0 0.25 | 2.0 0.25 | 2.0 0.25 | 2.0 0.25 | 3.0 0.25 | 3.0 0.25 | 2.0 0.25 | 0.5-0.7 | 2.0 0.25 | 2.0 0.25 | 2.0 0.25 | 2.0 0.25
Температура пара на входе, оС | 300-450 | 300-450 | 300-450 | 300-480 | 300-480 | 300-480 | 300-480 | 300-480 | 300-480 | 300-480 | 300-480 | 300-480 | 300-480 | 300-480
Расход пара через сборку, г/с | 4 | 4 | 4 | 8 | 6 | 6 | 6 | 6 | 6 | 8 | 8 | 6 | 6 | 6
Скорость нагрева оболочек в момент разгерметизации, К/с | 1,5 2,0 | 1,0 1,5 | 0,2 0,3 | 0,4 0,5 | 1,5 2,2 | 1,4 1,8 | 3,0 4,0 | 2,0-4,0 | 2,0-4,0 | 1,5 3,5 | 2,0-4,0 | 0,5 | 0,5-1,0 | 0,5-1,0
Максимальная температура оболочек твэлов, оС | 1100 | 1200 | 900 | 1200 | 900 | 900 | 850 | 1100 | 1100 *) | 860 **) | 1100 *) | 1290 ***) | 2500 ***) | 2500 ***)
Скорость залива модельной ТВС водой снизу, мм/сек | *****) | *****) | 50 | 30 | 80 | 80 | 80 | 80 | 80 | 80 | 80 | 80 | 80 | 80
Примечание: *) Радиальный температурный перекос  300 град;
**) ТВС типа ВВЭР-440;
***) Испытания ТВС в условиях запроектной аварии.
*****) Программой не предусмотрен.

## Slide 11: Some results of completed DBA tests
Test Scenario
Cladding Temperature
Internal Pressure
Т°.
Bottom Flooding
Notes: лоч

## Slide 12: Some results of completed SA tests
Test Scenario
Залив снизу
Cladding T
Internal Pressure
Т°об.
Bottom Flooding

## Slide 13
Вход пара
Залив снизу
Post Test Bundle View

## Slide 14
Electron microscopy
Zr-Fe-Cr-U Eutectic melt Zr-U
BDBA
SA
Post Test Material Investigations
Cladding oxidation
Cladding oxidation

## Slide 15: Results of Facility modeling by RATEG/SVECHA Code
1.Cladding Temperatures

## Slide 16: Results of Facility modeling by RATEG/SVECHA Code
Heated rods
2. Gap internal pressure

## Slide 17: Results of Facility modeling by RATEG/SVECHA Code
3.Liner Temperature
4.Hydrogen Release
ЭКСП.

## Slide 18: Current Status
Facility was successfully tested against set of BDBA and SA scenarios. Facility is ready to be used for future tests.
Code RATEG/SVECHA was successfully tested against PARAMETER Data. Obtained results demonstrated that main features of PARAMETER Facility can be well predicted by SA computer codes.

## Slide 19: Project Proposal
Goal: Two test of overheated up to 2000 C bundle:
  1-st test: top flooding
  2-nd test: simultaneous top and bottom flooding
Project Manager: Nalivaev V.I.
Participating organization
  NPO “Lutch”
  IBRAE
  Other organizations: IPPE, NIKIET, OKB “Gidropress"
Cost estimate: $360k
  Equipment:$53k
  Materials:$48k
  Overhead: $36k
  Personal grants: $180k
  Travel: $21k
  Other direct cost: $23k
Project duration: 24 months

## Slide 20: Project proposal: Tasks
Task 1: Study of the top flooding of 19 FE bundle under severe accident conditions
Task 2: Study of the simultaneous top and bottom flooding of 19 FE bundle under severe accident conditions
Each task consists of the following subtasks:
  Subtask 1.1 Preparatory work
  Subtask 1.2 Pretest analysis, choice of the test scenario and parameters
  Subtask 1.3 Test conduction
  Subtask 1.4 Post test examination and analysis
    Material study
    Post test analysis