## Slide 1: PARAMETER-SF4 post-test calculation with MAAP4.07
Emilie Beuzet
March 2010

## Slide 2
Sommaire
1. PARAMETER-SF4 test section
2. Specification of PARAMETER-SF4 test
3. Model parameters used in MAAP
4. First results of PARAMETER-SF4 post-test calculation
 Temperatures at different elevations
 Hydrogen production
 O2 flow rates
5. First conclusions

## Slide 3: PARAMETER-SF4 test section
PARAMETER cross section
PARAMETER test facility

## Slide 4: Specification of PARAMETER-SF4 test
Post-test calculation for PARAMETER SF4 has been carried out with a local version of MAAP4.07, containing extensions developed by EDF, specifically :
- Zr oxidation by air,
- introduction of material properties of the heater element materials (tantalum, molybdenum and brass) used in PARAMETER.
The simulation covers :
- establishment of a stable pre-oxidation plateau,
- power reduction,
- air ingress phase,
- bottom reflood.

## Slide 5: Specification of PARAMETER-SF4 test
Argon 2g/s
Air 0.5g/s
Steam 3.5g/s
~770 K
~1470 K
~2020 K
Bottom reflood 80g/s
1500 s
16000 s
~1170 K

## Slide 6: Model parameters used in MAAP
Steam pre-oxidation = Cathcart + Urbanic correlation
Air oxidation = NUREG correlation
External resistance : 4.5mΩ / rod
Distribution in : - 3 rows : 1 unheated rod / 6 rods / 12 rods + 12 ‘little’ rods , - 58 axial meshes : 5 for the lower plenum, 48 for the core and 5 for the upper plenum.
58 meshes
3 rows

## Slide 7: Cladding temperatures at 500 mm high

## Slide 8: Cladding temperatures at 700 mm high

## Slide 9: Cladding temperatures at 800 mm high

## Slide 10: Cladding temperatures at 900 mm high

## Slide 11: Cladding temperatures at 1000 mm high

## Slide 12: Cladding temperatures at 1100 mm high

## Slide 13: Shroud temperatures

## Slide 14: Hydrogen production
good prediction of the hydrogen production during pre-oxidation phase

## Slide 15: O2 flow rates during air ingress
Modelling does not predict O2 starvation during air ingress

## Slide 16: First conclusions
Thermal behaviour :
- bigger difference for 3rd rod = impact of the 12 external rods ?
- better precision in the 2nd rod
Hydrogen production :
- good prediction during pre-oxidation phase
- simulation does not cover reflood yet
Modelling does not predict O2 starvation (which is probably not correct)