## Slide 1: The Phebus FP Programme and Safety Needs examined by an International Group of Experts B. Clément (IRSN)

## Slide 2
PHEBUS FP FACILITY
  Experimental simulation of reactor core, reactor cooling system and containment
Scaling down 1/5000

## Slide 3
PHEBUS FP TEST MATRIX

## Slide 4
MAIN OUTCOMES: FUEL DEGRADATION
  Cladding Oxidation
  More violent cladding oxidation runaway than predicted in the first test FPT-0
  Need to revise correlations for “cladding dislocation criteria” based on temperature and oxide scale thickness
  Now correct predictions of cladding oxidation and hydrogen production for FPT-0, FPT-1, FPT-2 in different conditions

## Slide 5
MAIN OUTCOMES: FUEL DEGRADATION
  Fuel relocation
  Fuel liquefaction and transition from rod-like geometry to molten pool at temperatures (2600  200 K) largely below actual melting point of pure UO2 (3100 K)
  Severe damage observed due to significant material interactions, initiated by structural materials possibly enhanced by fuel swelling, fragmentation and changes in stoichiometry
  Detailed modelling of interactions still to be improved but codes succeed in describing the final state of degradation given suitable reduction of bulk fuel temperature relocation from ceramic value

## Slide 6
MAIN OUTCOMES: FUEL DEGRADATION
  Fuel relocation
  Example of calculated material axial distribution at the end of Phébus FPT-1 test (from ISP-46)

## Slide 7
MAIN OUTCOMES: FUEL DEGRADATION
  FPT-3 Boron Carbide Test
  Quite early fuel degradation involving low melting point alloys, likely during the cladding oxidation phase
  Limited final fuel degradation, as planned
  IRSN ICARE/ CATHARE calculation
    As in the test no molten pool formation predicted
    No degradation predicted in the middle bundle part
    No material relocation below the fuel active zone predicted
  Similar conclusions for GRS calculation with ATHLET-CD and PSI calculation with MELCOR
  Effects linked to boron carbide suspected, under investigation in the International Source Term Programme (SETs)

## Slide 8
FP AND STRUCTURE MATERIAL RELEASE
  Release of FPs
  Volatile generally well calculated even if CORSOR approach tends to overestimate kinetic at the beginning of transient
  Semi-empirical models ,though not describing all processes, able to do well for volatiles using consistent set of parameters for Phébus and separate-effect of experiments
  Situation more contrasted for less volatiles for which chemistry plays an important role – insights gained from mechanistic codes
  Coupling with Fuel Degradation
  In FPT-0 using 9-days irradiated fuel, early release of volatiles can only be explained by fuel dissolution during cladding oxidation phase
  Barium release much smaller in Phébus than in Separate-Effect experiments – difference attributed to interactions of fuel with cladding material and maybe iron reducing barium volatility
  Low release from Molten Pool

## Slide 9
FP AND STRUCTURE MATERIAL RELEASE
  Release from silver-Indium-Cadmium Control Rod
    Often not well enough calculated especially for silver which has an important impact on iodine chemistry
    Governing phenomena well understood but modelling effort still needed, especially for coupling with degradation processes

## Slide 10
FP AND AEROSOL TRANSPORT IN RCS
  Fission Products and Structural material Speciation
  In the hot leg, iodine and cadmium were the only non condensed elements in FPT-0 and FPT-1 – CsOH was not the dominant species for caesium transport
  From FPT-2, not all iodine transported as CsI
  FP volatility can be reproduced by codes calculating the chemical speciation and using a sufficiently extended database
  Deposition
  High deposition on the vertical section of the hot leg above the bundle where gas temperature drops down to 700°C, underestimated by codes
  Can be accounted for by the effect of developing flow characterised by much higher temperature gradients and mass transfer than for developed flow
  Deposition by thermophoresis in the steam generator overestimated by codes
  Attempt to reproduce the experiment by 2D particle tracking calculations

## Slide 11
T/H AND AEROSOL IN CONTAINMENT
  Thermal-hydraulics
  Governed by the balance between incoming steam and its condensation –generally well calculated by lumped parameter codes even with a with coarse noding
  Aerosol depletion
  Mainly by gravitational settling and diffusiophoresis - generally well calculated by lumped parameter codes even with a coarse noding

## Slide 12
IODINE CHEMISTRY
    Overall Gaseous Iodine concentration in FPT-0 / FPT-1
Early Presence
Decrease
Sustained Level

## Slide 13
IODINE CHEMISTRY
  Early presence of gaseous iodine in containment
  Likely to have been formed in the Primary Circuit
  Probably linked to non equilibrium chemical effects
  Assumption supported by existence of sharp and large temperature gradients in the circuit especially at the bundle exit and at the inlet of steam generator
  Fully compatible with higher fraction in FPT-0 with lower FP concentrations as compared with FPT-1
  Role of Silver
  Reaction of silver with iodine in sump water to form non soluble species
  Important inhibition of gaseous iodine production by radiolytic oxidation of iodides or organic iodides formation in sump water
  Needs an excess of silver compared with iodine
  Well quantified and modelled thanks to dedicated experiments

## Slide 14
IODINE CHEMISTRY
  Gas phase chemistry
  Volatile iodine concentration mostly determined by gas phase chemistry
  Importance of gaseous iodine injection from RCS
  Equilibrium between iodine formation/destruction processes and/or reversibility of iodine adsorption/desorption processes yield a steady-state concentration in the long term
  In FPT-0 and FPT-1 most of gaseous iodine is organic in the long term
  Role of homogeneous gas phase radiolysis reactions determining speciation and evolution of iodine not to be underestimated
  Idem for inorganic volatile species produced by I2 and CH3I radiolysis

## Slide 15
INTERNATIONAL GROUP OF EXPERTS
  Objectives
  Identify potential programmes of integral tests responding to safety technical issues and likely to receive a strong scientific and sufficient financial support from the international safety community
  Potential safety domains are Severe Accidents and design basis LOCAs for present and future reactors
  Meetings
  First meeting of the whole group in March 2005
  Specialists meeting on Severe Accidents in April 2006
  In addition, OECD Specialists meeting on LOCA in June 2006 for R&D review

## Slide 16
INTERNATIONAL GROUP OF EXPERTS
  Outcomes of meetings on Severe Accidents
  Three main issues recognised important and discussed in detail
    Air Ingress situations
    High burn-up and MOX fuel
    Reflooding of a degrading core
  For each issue, discussion on
    Significant safety issues/questions/open areas
    Past, ongoing and planned separate-effect experiments
    Possible role of a Phebus integral experiment

## Slide 17
INTERNATIONAL GROUP OF EXPERTS
  Outcomes of meetings on Severe Accidents
Air Ingress
  Issue associated with reactor accidents, spent fuel pool drainage, handling or transportation accidents
  Possible redefinition of source term taking into account ruthenium
  Past, ongoing and planned separate-effect experiments cover main aspects of the problem: cladding oxidation, Ru release, Ru transport and behaviour in containment, FP re-vaporisation
  Integral experiment
    Potentially important phenomena not all covered so far in SETs
    Coupling between fuel degradation and FP release
    Potential role of control rod material on FP chemistry especially iodine
    Behaviour of Ru in RCS in presence of structural material and other FPs
    More focus on Source Term than on fuel degradation

## Slide 18
INTERNATIONAL GROUP OF EXPERTS
  Outcomes of meetings on Severe Accidents
High burn-up and MOX fuels
  Main questions associated with the source term: faster release of volatiles, higher release of medium and low volatile FPs
  Investigation of fuel foaming
  Information on release of FP from HBU and MOX fuel will be available from SETs before any Phebus experiment
  Integral experiment
    Not easy to run SETs on fuel degradation
    Entire chemistry is present in an integral test
    Look at the effects of fuel foaming
    Concentrate on phenomena in the fuel bundle – no surprises expected in relation to the other issues (aerosol, transport, chemistry in containment...)

## Slide 19
INTERNATIONAL GROUP OF EXPERTS
  Outcomes of meetings on Severe Accidents
Reflooding of damaged core
  Reflooding is an unavoidable accident management measure
  Main questions associated with hydrogen generation rate, size and coolability of debris produced, source term during this phase of an accident (FP release and re entrainment of deposits)
  Ongoing programmes
    On bundles: QUENCH, PARAMETER
    On small samples: QUENCH SETs, QUENCH ISTC (irradiated fuel)
  Integral experiment
    Interest in irradiated bundle tests: rod-to-rod interactions, blockages, temperature distribution, quantity of debris formed
    Continuous nuclear heating allows to study properly the behaviour of debris
    Coupling between fuel degradation and FP release

## Slide 20
INTERNATIONAL GROUP OF EXPERTS
  Outcomes of meetings on Severe Accidents
Relative Priority
    Priority to air ingress and reflooding tests
    Lowest priority to high burn-up and MOX tests

## Slide 21
INTERNATIONAL GROUP OF EXPERTS
  Outcomes of meetings on LOCA
  Safety needs
    Evaluation of flow blockage in an assembly due to ballooning of irradiated fuel rods, including modern alloys
    Characterisation of fuel relocation in ballooned zones and its influence on the accidental transient
    Coolability of blocked areas in bundles
    Embrittlement of irradiated claddings
  First point needs experiments that could be done in Phebus – type of experiments to be discussed at the specialists meeting
  Second point can be done with experiments on irradiated single rods
  Third point more linked to out-of-pile thermal-hydraulic experiments
  Fourth point addressed by separate-effect experiments
  Specialists meeting scheduled end of 2006

## Slide 22
INTERNATIONAL GROUP OF EXPERTS
  Generation IV
  Consideration of needs for GEN IV reactors is foreseen