## Slide 1: Proposals on the Ternary Oxide System Study: UO2-FeO-SiO2 and UO2-FeO-CaO
ISTC PRECOS Project
#3813
A.P. Alexandrov Research Institute of Technology
Presented by Svetlana Kirillova
2nd PRECOS Meeting
ETU
Saint-Petersburg

## Slide 2: PRECOS matrix
Task | Composition | Atmosphere | Experimental data | Priority level | Pt N
1 | Different compositions in the U–Zr–Fe–O system | Argon | Selected points (liquidus, solidus, tie-lines in the miscibility gap) | 1 | 6
 | U–O |  |  |  | 
2 | ZrO2–FeOy | Air and oxygen | liquidus, solidus, solubility limits | 2 | 3
 | UO2–SiO2 | Argon | liquidus, solidus, tie-lines in the miscibility gap, eutectic point | 1 | 7
 | CaO–UO2 |  | liquidus, solidus, solubility limits, eutectic point | 1 | 7
3 | UO2–FeO–SiO2 |  | liquidus, solidus, solubility limits, tie-lines in the miscibility gap, ternary eutectic point | 1 | 10
 | UO2–FeO–CaO |  | liquidus, solidus, solubility limits, ternary eutectic point | 1 | 10
 | ZrO2–FeO–SiO2 |  | ternary eutectic point | 2 | 2
 | ZrO2–FeO–CaO |  | ternary eutectic point | 2 | 2
4 | Eutectic composition measurement of a realistic complex corium mixture | Argon or Air | System (atmosphere) proposed by French partners (1 system), System (atmosphere) proposed by German partners (1 system), System (atmosphere) proposed by Russian partners (1 system) | 2 | 3

## Slide 3
PRECOS project meeting
3
Research objectives
To specify the binary and ternary eutectic points in the inert atmosphere
To determine the solidus and liquidus curves
To determine solubility limits of components in the formed solid solutions
To find the existence limits of compounds
To determine the tie-lines in the miscibility gap

## Slide 4
PRECOS project meeting
4
Methods
Visual-polythermal analysis
(Galakhov microfurnace, induction melting in the cold crucible)
Complex thermal analysis (DTA/TG)
In situ measurements
X-ray powder diffraction
X-ray fluorescent analysis
Post-test analysis
Chemical analysis
Scanning electron microscopy/energy-dispersion X-ray analysis (wave-dispersion analysis)

## Slide 5
UO2–FeO–SiO2 system
Pt | UO2 | FeO | Objectives
 | mol % |  | 
1 | 5.0 | 63.3 | eutectic (5 UO2 – 95 Fe2SiO4)
2 | 30.0 | 46.7 | liquidus solidus
3 | 70.0 | 20.0 | 
4 | ~3 | ~71 | eutectic
5 | ~3 | ~58 | 
6 | 15.0 | 46.7 | liquidus solidus
7 | 35.0 | 20.0 | 
8 | 5.0 | 25.0 | miscibility gap
9 | 10.0 | 10.0 | 
10 | 20.0 | 7.0 | 
PRECOS matrix – 10 points
2500
Fe2SiO4
80
60
40
20
UO2
1600
1300
1900
2200
T, C
2800
mol % Fe2SiO4
?
UO2
SS
1300
1700
2100
2500
20
40
60
80
FeO
FeO, mol. %
T, °C
L+SS
L
Published
SiO2
UO2
FeO
CORPHAD
CORPHAD+PRECOS
Fe2SiO4
?
?
1
2
3
4
5
6
8
10
9
7
2600
1719±10
SiO2
80
60
40
20
UO2
2000
UO2 + SiO2
1600
1800
2200
2400
UO2 + L
T, C
2800
L1 + L2
2080
2070±10
mol.% SiO2
FeO, mol. %
FeO1.5, mol.%
1200
1400
1600
1800
80
60
40
20
SiO2
5
FeO
1723
1377
T, C
Fe2SiO4
L1 + L2
crystobalite
+ L
tridymite + L
tridymite + fayalite
L +
wustite
fa + w
10
In progress
FeO1.5, mol.%
5
10
1150
1250
1377
T, C
1350
2FeOSiO2
FeO, mol. %
90
80
70
SiO2
FeO
1204±2
1177±2

## Slide 6
PRECOS project meeting
6
UO2–FeO–SiO2 system
Binary section investigation
(UO2-Fe2SiO4, inert atmosphere, without getter)
Fe2SiO4 synthesis
Eutectic point determination (Galakhov -> SEM/EDX, X-Ray -> IMCC -> SEM/EDX, DTA/TG)
Liquidus and solidus determination (Galakhov, VPA IMCC)
Logic and sequence of system study
Ternary eutectics determination
(UO2-FeO-Fe2SiO4, inert atmosphere, with getter)
(UO2-Fe2SiO4-SiO2, inert atmosphere, without getter)
Fe2SiO4 synthesis
Eutectic point determination (Galakhov -> SEM/EDX, X-Ray -> IMCC -> SEM/EDX, DTA/TG)
Liquidus, solidus and miscibility gap determination
(UO2-Fe2SiO4-SiO2, inert atmosphere, without getter)
Fe2SiO4 synthesis
Liquidus and solidus determination (Galakhov, VPA IMCC)
Tie-lines in the miscibility gap (Galakhov, VPA IMCC)

## Slide 7
?
UO2–FeO–CaO system
1300
1700
2100
2500
UO2
20
40
60
80
FeO
FeO, mol %
T, °C
SS
L+SS
L
Published
CaO
UO2
FeO
CORPHAD
PRECOS
Pt | UO2 | FeO | Objectives
 | mol % |  | 
1 | 50.0 | 0 | CaUO4-x Ca2UO4
2 | 33.3 | 0 | 
3 | 20.0 | 50.0 | 
4 | - | - | eutectic
5 | - | - | 
6 | - | - | 
7 | - | - | liquidus solidus
8 | - | - | 
9 | - | - | 
10 | - | - | 
PRECOS matrix – 10 points
1
2
3
mol.%
CaO
20
40
60
80
UO2
T, C
1000
2200
2800
1600
1300
1900
2500
CaUO4-x
Ca2UO4
In progress

## Slide 8
PRECOS project meeting
8
UO2–FeO–CaO system
Composite oxides investigation
Sample preparation of CaO-enriched compositions
CaUO4-x and Ca2UO4 upper the limit’s existence (Galakhov -> SEM/EDX, X-Ray)
Conditions and sequence of system study
Phase composition determination
(CaUO4-x-Ca2UO4-FeO, inert atmosphere, with getter)
Sample preparation of CaO-enriched compositions
Phase composition determination (Galakhov -> SEM/EDX, X-Ray)
?

## Slide 9
Conclusions
UO2–FeO–SiO2 system
The logic and sequence of system study are quite clear
UO2–FeO–CaO system
The composition of points in the observed system is able to define more exactly after the UO2–CaO system revision only