## Slide 1: PRECOS Project Activity in the 9-12 Quarters
ISTC PRECOS
Project #3813
A.P. Alexandrov
Research Institute of Technology
Presented by Victor Gusarov
4rd PRECOS Meeting
SPbSIT (TU)

## Slide 2: PRECOS matrix
Task | Composition | Atmosphere | Experimental data | Priority level | Pt N | State
0 | SiO2–FeOy |  |  | CORPHAD |  | In progress
1 | U–Zr–Fe–O | Argon | liquidus, solidus, tie-lines in the miscibility gap | 1 | 6 | In progress
 | U–O |  |  |  |  | 
2 | ZrO2–FeOy | Air and oxygen | liquidus, solidus, solubility limits | 2 | 3 | In progress
 | ZrO2–FeO | Argon | liquidus, solidus |  | 4 | LPM verification
 | UO2–SiO2 |  | liquidus, solidus, tie-lines in the miscibility gap, eutectic point | 1 | 7 | Complete
 | CaO–UO2 |  | liquidus, solidus, solubility limits, eutectic point | 1 | 7 | Close to completion
3 | UO2–FeO–SiO2 | Argon | liquidus, solidus solubility limits, tie-lines in the miscibility gap, ternary eutectic point | 1 | 10 | Close to completion
 | UO2–FeO–CaO |  | liquidus, solidus solubility limits, ternary eutectic point | 1 | 10 | In progress
 | ZrO2–FeO–SiO2 |  | ternary eutectic point | 2 | 2 | -
 | ZrO2–FeO–CaO |  | ternary eutectic point | 2 | 2 | -
4 | Eutectic composition measurement of a realistic complex corium mixture | Argon or Air | Systems proposed by partners: - French system - German system - Russian system | 2 | 3 | 

## Slide 3
3rd Year Activity
ZrO2-FeO
Will be presented by
Mikhail Sheindlin
UO2-FeO-CaO
UO2-FeO-SiO2 eutectics
Will be presented by
Svetlana Kotova
Will be presented by
Evgeny Krushinov
UO2-FeO-SiO2 miscibility gap
Will be presented by
Vyacheslav Almjashev
SiO2-FeOx
Will be presented by
Svetlana Kirillova