## Slide 1: Proposals for Task 4 of Russian partner
A.P. Alexandrov Research Institute of Technology
Presented by S. Bechta
4th PRECOS Project Meeting
June 8, 2011, St. Petersburg

## Slide 2: Contents
  Objectives of task #4
  Corium composition
  Test procedure
  Post test study

## Slide 3: Objectives of task #4
According to PRECOS Work Plan:
Experimental determination of liquidus and solidus temperature of complex corium composition relevant for plant application
Preparation of data for NUCLEA validation
Additional objectives (optional)
Study of fission product and neutron absorber effect on liquidus and solidus
Study of macro segregation of melt components during slow crystallization

## Slide 4: Corium composition
Ex-vessel corium during melt retention in VVER core catcher
Formed during interaction of in-vessel corium with sacrificial materials of ex-vessel core catcher
Oxidic part of system in miscibility gap
Macrocomposition (mass %): 47.8 UO2+ 21.1 ZrO2+ 22.0 FeO + 9.1Al2O3
Impurities: B2O3, Gd2O3, BaO, SrO, La2O3, CeO2

## Slide 5: Test procedure
The first phase of the test
Preparation of a molten pool without FP and absorbers
Liquidus temperature measurements by VPA IMCC with simultaneous melt sampling for composition measurement and post test study of solidus temperature
The second phase of the test
Addition of FP and absorbers on the pool surface with rapid layering by additional corium charge. Pool homogenization.
Liquidus temperature measurements by VPA IMCC with simultaneous melt sampling for composition measurement and post test study of solidus temperature
The final phase of the tests
Slow pool extraction from the inductor coil to have close to equilibrium crystallization

## Slide 6: Post test study
Determination of melt composition during liquidus measurements
by XRF, ChA, XRD and SEM/EDX of samples taken before and after FPS addition
Measuremens of solidus temperatures of samples taken before and after FPS addition
by VPA in Galakhov microfurnace
by HTM
Study of macro segregation
by SEM/EDX of ingot
by ICP MS of samples cut from different location
by XRD and XRF of samples cut from different location

## Slide 7: Conclusive remarks
The proposed procedure can be applied for other compositions proposed by French and German partners
Risk of unexpected test problems can be reduced by checking the methodology in the first test with corium composition proposed by Russian partner
The decision regarding the 2nd and 3rd tests of Task #4 can be made after primary results of the first test will be available