## Slide 1
Proposal for modifications in the METCOR-P test matrix
Manfred Fischer, Areva NP GmbH
with support by Sevostian Bechta, ARIT

## Slide 2: METCOR-P Current objectives
Investigation of selected phenomena related to in-vessel melt behavior (melt - reactor vessel interaction). These phenomena are mainly relevant for IVR
Past experiments revealed two effects:
Formation of a metallic eutectic behind the oxidic crust, resulting in a lowering of the interface temperature (down to 1150°C) to be considered in the analysis and a correspondingly reduced final vessel wall thickness  impact on IVR checked but found to be not critical
Progressive exothermic oxidation of vessel steel by fully oxidized corium with the risk of vessel “burn-through”  could be a critical issue, relevance of underlying situation to be checked
Besides these two effect, other thermochemical phenomena are also of relevance for IVR. This motivates a reassessment of the test matrix.

## Slide 3: Issues related to IVR Evolution of the molten pool
Relocation of molten core into the lower plenum after lateral failure of core barrel
Melt interaction with the residual water partial oxidation / fragmentation
Remelting of debris bed and subsequent addition of molten structures
Sub-stoichiometric oxidic pool surrounded by oxidic crust (bottom and top) with dense metallic phase
Light metallic phase at the top of an oxidic crust

## Slide 4: Issues related to IVR Remaining uncertainties
Will the light metallic phase (contains Zr/U/Cr) “protect” the oxidic pool against further oxidation by forming a refractory insulating layer that could aggravate the focusing effect?
 Experimental investigation of metallic layer oxidation (once proposed for METCOR-P) is already under progress at AREVA NP

## Slide 5: Issues related to IVR Remaining uncertainties
What is the risk of forming an only “thin” upper metal layer that aggrevates the focussing effect?
Remains the heavy metal layer stable when more metal (or oxygen) is added? Can the heavily superheated steel layer rise to the top and contact the RPV wall under certain conditions?
 Depends, among others, on the evolution of the densities of the involved phases in the possile range of variation of composition and temperature (thermodynamic equilibrium?)

## Slide 6: Issues related to IVR Remaining uncertainties
Densities of oxidic and metallic melts in equilibrium are influenced by:
Corium oxidation index
U/Zr atomic ratio
Steel mass fraction
Temperature
The prediction of layer inversion effects with current data bases involves large uncertainties.
It is proposed to perform a limited number of experiments to create data points on oxide-metal density under equilibrium conditions with the target to check and improve these models and to reinforce the reliability of prediction for IVR application.

## Slide 7: Proposed experiments Test objective
Determination of compositions of coexisting melts, at which layer inversion takes place
Determination of oxide and metal density at ambient temperature
Variable parameters: Cn, U/Zr, mass of Fe/mass of corium, T
Option
Simplified test objective is determination of system integral composition, at which layer inversion takes place. In this case several parameter variations can be realized during one test. System composition will be calculated from mass balance (charge+additives-aerosols-samples)

## Slide 8: Proposed experiments Simplified test procedure
1 - Preparation of molten pool of specified composition and temperature with bottom location of metallic layer
2 - Step by step addition of Fe into the pool
3 - Visual determination of metallic melt rising
4- Ingot quenching
5 - Post test analysis of ingot (the main part of the work having the highest manpower)
Option 1
For simplified objectives, steps 2 and 3 can be repeated after metal melt surfacing. Addition of U (and Zr) or their oxides into the melt will be done for this.
Option 2
For simplified objectives, oxidic melt samples can be used for estimation of inversion densities. Oxidic melt samples will be taken before inversion but after every Fe addition and system exposition. Metallic melt sample will be taken just after inversion.
Option 3
Density of oxide melt having inversion composition will be determined in separate tests with accuracy of about 4 rel. %. We have set-up designed and tested for oxide melt density measurements.