## Slide 1
Jon Birchley, PSI
PARAMETER Meeting
29th July 2009
Podolsk, Russia
PARAMETER SF3 first post-test calculation

## Slide 2
  Outline
  ● PARAMETER SF3 experiment
  ● Modelling
  ● Boundary conditions
  ● Results
  - overall
  - reflood
  ● Summary

## Slide 3
  PARAMETER SF3 experiment
  ● Initial power ramp and thermal escalation
  ● Approximate temperature plateau for pre-oxidation
  ● Second power ramp and thermal escalation to ca. 1600 °C
  ● Top injection at ca. 40 g/s
  - primary aim to address top-down quenching

## Slide 4
  Modelling
  ● PSI version(s) of SCDAP/RELAP5/irs
  - properties for Ta, Mo and brass
  - oxidation models
  - standard SCDAP (Cathcart-Pawel/Urbanic-Heidrick)
  - Sokolov correlation implemented but not used in this calculation
  - separate correlations for weight gain and thickness
  ● Input model
  - single hydraulic channel for test section
  - cooling circuits; dummy volumes for lab temperature
  - 5 core components (central, 2*heater, peripheral rods, shroud)
  - problems in modelling upper section of shroud
  - 28 axial nodes for heaters (14 Ta, 2x6 Mo, 2x1 brass)
  - external resistance 8.5 mohm/rod
  - interphase drag with and without CCFL model

## Slide 5
  Boundary conditions
  ● Inlet flows
  - steam: 3.5 g/s (start at 2300 s); 0 g/s during water injection
  - Ar: 2 g/s
  - reflood: top injection at ca. 40 g/s
  ● Power
  - total DC power follows experimental evolution
  - tripped off at start of injection

## Slide 6
  SF3 electrical power

## Slide 7
  SF3 maximum temperature

## Slide 8
  SF3 hydrogen generation

## Slide 9
  SF3 bundle temperatures - lower

## Slide 10
  SF3 bundle temperatures - upper

## Slide 11
  SF3 reflood – lower (no CCFL model)

## Slide 12
  SF3 reflood – upper (no CCFL model)

## Slide 13
  SF3 quench (no CCFL model)

## Slide 14
  SF3 bundle refill (no CCFL model)

## Slide 15
  SF3 bundle exit velocities (no CCFL)
CCFL model needed?

## Slide 16
  Counter-current flow limitation
  ● Baseline case used “standard” RELAP5 interphase drag
  - annular-mist model allows liquid penetration during injection
  - bundle refills and quenches bottom-up, contrary to experiment
  ● G. B. Wallis says “no way water could penetrate so easily through the bundle with all that steam flowing”
  ● Introduce Wallis CCFL correlations
  - No, Lee, Song (Nucl. Engrg. Tech. 37 (6) 557-564, (2005))
  - aimed at top injection; CCFL at upper core support plate
  jg*1/2 + 1.22 jl*1/2 = 0.88 (A)
  - Wallis, One-dimensional two-phase flow, McGraw-Hill (1969)
  - Original modelling; CCFL in single tube
  jg*1/2 + jl*1/2 = 0.725 (B)

## Slide 17
  SF3 quench – lower (CCFL model A)

## Slide 18
  SF3 quench – upper (CCFL model A)

## Slide 19
  SF3 bundle refilling (CCFL model A)

## Slide 20
  SF3 bundle exit velocities (CCFL model A)
not enough steam for CCFL
CCFL model needed?
filling of central bundle

## Slide 21
  SF3 T,max (CCFL models: none A, B)

## Slide 22
  SF3 reflood (CCFL models: none A, B)

## Slide 23
  Summary
  ● First SF3 post-test calculations performed
  ● Difficulties encountered in two areas
  - limitations in modelling upper part of bundle
  - representation of power history and distribution
  ● Power reduced during final heat-up
  - sought to simulate actual conditions at start of injection
  ● RELAP5 interphase drag model fails to capture CCFL
  - water penetrated directly through bundle, quenched from bottom up
  ● CCFL successfully captured with Wallis-type correlation
  - water collected first in upper bundle before filling bundle
  - quench initially top-middle, then bottom-middle
  - recent correlation aimed at top injection works better than original
  ● Analyses will continue with new code version just available

## Slide 24
  Acknowledgments
  The work is supported by Swissnuclear and by the European Commission in the frame of SARNET and SARNET-2
  Thank you for your attention
  ☺