## Slide 1
FSUE SRI SIA “LUCH”
IBRAE RAS
JSC OKB “GIDROPRESS”
29 July, 2009, Podolsk
Experimental results of complex starting-up and adjustment on preparation of the PARAMETER-SF4 Experiment
Presented by W. Konstantinov
(Status of Project # 3690)
Notes: 1
1

## Slide 2
The study of behaviour of VVER-1000-type FA overheated to 1750°C under severe accident conditions with air ingress and bottom quenching
Objective

## Slide 3
Development of technological systems for carrying out of PARAMETER-SF4 Experiment :
а) The control of air flow rate;
б) The control of the gas environment;
в) Bottom flow;
г) Steam generation and heating of argon flow;
- Check up of technological systems
- Carrying out of control test up to 500 C
-
Main Tasks of the Project

## Slide 4
Test bundle
Main technical characteristics
Main technical characteristics
Bundle type VVER-1000
number of fuel rods 19
- heated 18
- unheated 1
Grid type triangle
Grid pitch, mm 12.75
Spacing grid Zr1%Nb
- height, mm 20
- spacing, mm 255
Shroud Zr1%Nb
- shape cylinder
- height, mm 1490
Thermal insulation ZrO2 ZYFB-3
- thickness, mm 23
- height, mm 1490

## Slide 5: Test instrumentation

## Slide 6: Test facility
Functional scheme

## Slide 7
Results of check of technological systems
- Parameters of argon and pair;
- Air flowrate;
- Calibration of the hydrogen measurement device;
- Parameters of the bottom flooding;
- Trial experiment at 500°С.

## Slide 8
G st in = 3,5 g/s Tst in = 500±50°C
Garg in = 2 g/s T arg in = 280±20°C
Results of measurement of parameters of argon and steam

## Slide 9
Results of check of system of measurement of the air flow rate
Gair = 0,48±0,04 g/s
Tair = 30±5°C

## Slide 10
Check of system of the bottom flooding
Gbf = 80 g/s

## Slide 11
Check of the monitoring system of hydrogen
№ items | Reference gas mix. (Ar + X %H2), X%
1 | 5,56
2 | 10,4
3 | 22,3
4 | 39,2
5 | 41,1
ΤCv(H2)  100 s

## Slide 12
Check of the monitoring system of air
The analysis of oxygen
OLCT-20D
Controll gas - О2
Range of measurements - 0 - 30 % v.
The basic error:
Resulted 0 - 5 %v. - ±5 %;
Relative - 5 - 30%v. - ±5 %
Measurement of air flow rate
EL - FLOW
Controll gas - (20 %) O2 + (80 %) N2
Range of measurements - 0 - 3,75 kg/h
Accuracy of measurements - ±0,5 %

## Slide 13
Τ  170 – 200 s
Time of an establishment of signal
of OLCT - 20
Calibration of air flow rate
IN FLOW
Check of the monitoring system of air

## Slide 14
Some experimental results of control test
The scenario of test experiment

## Slide 15
Temperature of cladding and shroud
Electrical power
Temperature of bundle
Parameters steam and argon
Параметры ТВС
Some experimental results

## Slide 16
CONCLUSIONS
It is made and established in the PARAMETER facility the 19-rods bundle VVER-1000 for carrying out of experiment under severe accident, including stages of ingress of air and a bottom flooding. 2. Submission of argon flow (Garg = 2 g/s, Тarg = 280±20°С) and steam flow (Gst = 3,5 g/s, Тst = 500±50°С) in the test bundle is provided. 3. The system of bottom flooding (Gbf = 80 г/с flow rate) of test bundle is checked up. 4. The system of ingress (Gair=0,5 g/s) of air (20%О2+80%N2) in the test bundle is checked up.
5. . Calibration of system of the gas analysis on reference gas mixes (Ar+XH2, X= (5,56; 10,4; 22,3; 39,2; 41,1))%v.is carried out.