## Slide 1
Final PARAMETER SF4 pre-test calculation with ATHLET-CD Ch. Bals, K. Trambauer
presented by W. Erdmann
Gesellschaft für Anlagen- und Reaktorsicherheit (GRS), Germany

## Slide 2: Content
Final specification of the PARAMETER SF4 experiment and simulation with ATHLET-CD
Input model and options for ATHLET-CD pre-test calculation
Results of PARAMETER SF4 pre-test calculation:
  Temperatures
  Quench fronts
  Hydrogen generation
  Oxide layer thickness
Conclusions

## Slide 3: PARAMETER SF4 Specification and Simulation with ATHLET-CD (1)
Final Specification according to Jon Birchley, (e-mail, 15.5.2009)
Power supply – temperature behavior: - cold bundle at start of test: 25 °C at 0 s
- power initially based on SF3 specification; adjusted to achieve max. plateau temperature of ~1200 °C with given time function (pre-oxidation phase is reached with a time delay of 2000 s compared to previous specification) - at 14000 s (oxide scale thickness of 300 µm is assumed to be reached) power reduction to 5.5 kW to reduce Tmax to ~900 °C before air injection is started at t= 16000 s - constant power of 5.5 kW during air injection phase is switched off when max. temperature of 1750 °C is reached; at same time bottom injection of water is started

## Slide 4: PARAMETER SF4 Specification and Simulation with ATHLET-CD (2)
Argon inlet flow : - constant rate of 2.0 g/s - switch to upper injection after start of reflood - T= 450 °C
Steam inlet flow: - 0.0 g/s until 1500 s - 3.5 g/s until 16000 s, when air injection is started, - T= 500 °C
Air inlet flow: - 0.5 g/s (0.1 g/s O2, 0.4 g/s N2) - air injection starts at 16000 s - air injection is switched off when bottom water injection is started
Bottom flooding : - is initiated as soon as Tmax= 1750 °C is reached (together with power shut off) - Water flow rate: 80 g/s, water temperature: 25 °C - initial water level of 450 mm below inlet pipe is assumed (as SF3)
Bundle pressure: 3 bar - constant boundary condition of 3 bar
Calculation is finished after quenching of total bundle (t= 17040 s)

## Slide 5: Input model for PARAMETER calculations with ATHLET-CD
Flow Channels
  Central Bundle CORE2 85.7 %
  Outer Bypass CORE3 14.3 %
  Cross connection
  Cooling Jacket
Structures
  Rods: ROD1 (1 unheated rod) ROD2 (6 heated rods) ROD3 (12 heated rods)
  Grids (6)
  Shroud / Insulation
  Cooling Jacket Wall
  Structures at top of bundle (upper plate, separation sheet)
Changes compared to previous calculations (SF2, SF3):
  Additional fills O2FILL, N2FILL for air injection

## Slide 6: Options for ATHLET-CD pre-test calculation of SF4
Cladding oxidation model: Leistikow / Prater-Courtright correlation (IOXMOD= 19) was used as for post-test calculation of SF2; (SF3 post-test calculation: Cathcart / Prater-Courtright (IOXMOD= 15) was used)
External resistance: 1 mΩ/rod
Hydraulic diameter in core region: DH= 3.8·10-3 m (= DH at grid position)
Default values for other models (e.g. interfacial friction model, quench model) are used

## Slide 7: Results of PARAMETER SF4 pre-test calculation
Temperatures in pre-oxidation period (before air oxidation):
- maximum temperature is calculated at 1250 mm elevation
- given time function for power leads to a maximum plateau temperature of Tmax= 1274 °C (expected Tmax ~1200 °C);
- Temperature decrease between 14000 s and 16000 s to ~900 °C is achieved as desired

## Slide 8: Results of PARAMETER SF4 pre-test calculation
Temperatures (air ingress period):
- after a time period of ~700 s following the start of air injection (t= 16000 s) oxygen starvation can be observed at the elevations above ~700 mm
- due to oxygen starvation in the upper bundle region the higher air oxidation and therefore the stronger temperature excursion moves to lower elevations (nitride formation is not considered up to now)
- maximum temperature of 1750 °C is reached at t= 16825 s at bundle elevation 500 mm
- resulting time period of oxygen starvation: Δt= 125 s (16700 to 16825 s)

## Slide 9: Results of PARAMETER SF4 pre-test calculation
Temperatures (quenching period):
- bottom flooding is initiated at 16825 s when Tmax= 1750 °C is reached
- after start of flooding only small temperature increase of ~100 °C is calculated when liquid enters the heated bundle (steam oxidation)
- due to cooling only from the bottom last quench is calculated at the upper bundle elevations

## Slide 10: Results of PARAMETER SF4 pre-test calculation
Shroud temperatures:
- the shroud temperatures show a steeper increase in the air oxidation period compared to the rod temperatures (Tmax= 1900 °C) due to a higher availability of oxygen in the outer core channel (CORE3)

## Slide 11: Results of PARAMETER SF4 pre-test calculation
Quench fronts:
- quenching of bundle within time period of 215 s after start of bottom flooding
- time delay until liquid enters the heated core region ~90 s (initial liquid level of 450 mm below steam/argon inlet pipes is assumed)
- injected liquid until end of quenching: 17.2 kg
- last quench at ~1500 mm bundle elevation (nearly no progress of upper quench front)

## Slide 12: Results of PARAMETER SF4 pre-test calculation
Hydrogen generation:
- Total mass of hydrogen generated: 31.5 g, (21.1 g in bundle region) calculated with Leistikow / Prater-Courtright correlation (IOXMOD= 19) as for SF2
- Hydrogen generated during quench: 5.1 g

## Slide 13: Results of PARAMETER SF4 pre-test calculation
Oxide layer thickness:
- oxide layer at the end of the pre-oxidation phase has a maximum value of ~450 µm (intended oxide scale thickness is ~300 µm)
- max. increase of oxide scale during air oxidation phase is 120 µm at 600 mm elevation
- a max. layer thickness of 462 µm is reached at the end of the calculation (1250 mm elevation)

## Slide 14: Conclusions
ATHLET-CD calculates slightly higher maximal temperatures within the pre-oxidation phase than expected with the given time function for power (calculated: ~1274 °C, expected: 1200 °C) the temperature decreases to 900 °C within 2000 s before the start of air injection is in agreement with the desired value; the maximal temperature within the air ingress phase of 1750 °C as the start point for bottom water injection is reached earlier than expected (calculated: t= 16825 s; 825 s after start of air oxidation)
Air injection with a reduced rate of 0.5 g/s leads to an oxygen starvation at the positions above 700 mm after a time period of ~700 s (at ~16700 s, start of air injection at 16000 s); therefore the elevation of the maximum temperature moves to lower positions (no nitride formation is considered up to now)
Time needed for bottom quenching: 215 s for calculation with injection rate 80 g/s,
Total hydrogen generation is 31.5 g, about 5 g during quench (Leistikow / Prater-Courtright correlation was used as for SF2 post-test calculation)
Oxide layer thickness at the end of the pre-oxidation phase is calculated higher than expected (max. value of 450 µm instead of 300 µm); oxide layer at the end of the calculation is 462 µm