## Slide 1: PARAMETER-SF4 post-test calculation with MAAP4.07 Update
Andreas SCHUMM, Emilie BEUZET
September 2010

## Slide 2
Outline
1. PARAMETER-SF4 test section
2. Specification of PARAMETER-SF4 test
3. Model parameters used in MAAP
5. Comparison with the first post-calculations
4. Results of PARAMETER-SF4 post-test calculation
 Temperatures at different elevations (pre-ox)
 Hydrogen production
 Temperatures at different elevations (air)
 O2 flow rates
5. Conclusions

## Slide 3: PARAMETER-SF4 test section
PARAMETER cross section
PARAMETER test facility

## Slide 4: Specification of PARAMETER-SF4 test
Post-test calculation for PARAMETER SF4 has been carried out with a customized version of MAAP4.07, containing extensions developed by EDF, specifically :
- Zr oxidation by air,
- introduction of material properties of the heater element materials (tantalum, molybdenum and brass) used in PARAMETER.
The simulation covers :
- establishment of a stable pre-oxidation plateau,
- power reduction,
- air ingress phase,
The simulation does not cover :
- hydrogen production during bottom reflood.
t0MAAP=tSF4-1452 (the simulation begins with steam injection)

## Slide 5: Specification of PARAMETER-SF4 test
Argon 2g/s
Air 0.5g/s
Steam 3.5g/s
~770 K
~1470 K
~2020 K
Bottom reflood 80g/s
1452 s
16000 s
~1170 K

## Slide 6: Model parameters used in MAAP
Steam pre-oxidation = Cathcart + Urbanic correlation
Air oxidation = NUREG correlation (like before)
External resistance : 8.5mΩ / rod (4.5mΩ during 1st simulation) (established on the other PARAMETER experiments)
Distribution in : - 4 rows : 1 unheated rod / 6 rods / 12 rods / 12 peripheral rods
(instead of 3 rows for the first post-calculations 1-6-12/12), - 58 axial meshes : 5 for the lower plenum, 48 for the core and 5 for the upper plenum.

## Slide 7: Comparison with the first post-calculations (at 200 mm : overestimated before)

## Slide 8: Comparison with the first post-calculations (at 900 mm)

## Slide 9: Comparison with the first post-calculations (at 1300 mm: underestimated before)

## Slide 10: Cladding temperatures at 500 mm high (pre-oxidation phase and air ingress separated)

## Slide 11: Cladding temperatures at 800 mm high (pre-ox)

## Slide 12: Cladding temperatures at 1100 mm high (pre-ox)

## Slide 13: Cladding temperatures at 1250 mm high (pre-ox)

## Slide 14: Hydrogen production
good prediction of the hydrogen production during pre-oxidation phase
Good cinetics, but still underestimate quantity

## Slide 15: Cladding temperatures at 500 mm high (air)

## Slide 16: Cladding temperatures at 800 mm high (air)

## Slide 17: Cladding temperatures at 1100 mm high (air)

## Slide 18: Cladding temperatures at 1250 mm high (air)

## Slide 19: O2 flow rates during air ingress
Modelling predicts O2 starvation during air ingress at about 17292 s (15840 s in MAAP time) and about 17100 s for the experiment.

## Slide 20: Conclusions
Thermal behaviour :
- better modelling with 4 rows than 3 rows (for the bottom and the top of the bundle)
- good prediction during the steam phase
- good prediction during the air phase for the upper part the bundle but analysis is difficult for the rest of the bundle due to thermocouples failure
Hydrogen production :
- good prediction during pre-oxidation phase, slight underestimation, almost identical to first simulation
- simulation does not cover reflood yet
Modelling now predicts O2 starvation but about 200 s later than the experiment : it is probably due to an under-estimation of temperatures during air ingress (parabolic correlation for the post-breakaway regime)
Nitruration not taken into account (no correlation available)

## Slide 21
Thanks for your attention …