## Slide 1: NITI Proposals for Task 2 tests of the EVAN Project
A.P. Alexandrov Research Institute of Technology
Presented by S. Bechta
1st EVAN Meeting

## Slide 2: Task 2. Study FP release from a molten pool
Experimental data application
Determine rates of low-volatile fission products release (FPR) from molten pool of prototypic corium
Quantify the sensitivity of release rates to the oxygen potential of the above-melt atmosphere
Determine aerosols’ characteristics
Simulants of radiologically relevant fission products for a late phase of the severe accident: stable Sr, Ba, Ce, La, Mo, Ru
Objectives
Verification of models describing FPR into the atmosphere of the primary circuit/containment
Analysis of phenomena, which set conditions for source term

## Slide 3: Methodology
Main tests:
- medium-scale tests with chemically prototypic molten corium (~2 kg),
- power deposited in the melt is simulated by the melt induction heating in a cold crucible (IMCC),
- flow method for release rate determination
Illustration of an analytical system used in the LPP project
1. Shielded box. 2. Metallic bottom. 3. Molten corium. 4. Inductor. 5. Cold crucible. 6. Quartz tube. 7. Cooled cover. 8. Start-up medium area filter (MAF). 9. Side port of the cover. 10. Vacuum pump. 11, 19, 20, 37. Regulating valves. 13. Analytical line rotameter. 12,25. Roll-blade flow meter. 14. Pressurized gas tanks (air, nitrogen). 15,16,24,34. Pressure sensors. 17,26,27,31,35. L thermocouples. 21. Analytical filters F1 (AFA). 22. Medium-area filters F2 (MAF). 23. Three-way cock. 28. Vibrator. 29. Analytical line. 30. Main line. 32. Cyclone. 33. Large-area filter F3 (LAF). 38. Disposable specimen holder. 39. Disposable module.

## Slide 4: View of IMCC furnace with connected sampling line

## Slide 5: Methodology (2)
Supportive analytical tests performed at the ISC RAS:
Determination of the FP partial pressures above the corium microspecimens in vacuum
Differential mass-spectrometry – a version of the Knudsen method
Coupled Knudsen chamber of isothermal effusion
1 - covers with effusion ports
2 - molybdenum crucible
3 - cathodes 4 - holders
5 - pyrometric port
6 - plate

## Slide 6: Methodology (3)
Weight analysis is used for determining the mass of aerosols collected on the analytical filters installed in the gas-aerosol sampling system, and aerosol transport losses in furnace components and lines
Elemental and phase composition of aerosols is determined by the ICP MS, XRF, SEM/EDX, XRD and various methods of chemical analysis
Particle size distrtibution is measured using the method of the small-angle light scattering, optical and electron microscopy of filters and substrates
Methods of aerosol posttest analysis:

## Slide 7: Experimental matrix for Task 2 of EVAN Project (Phase 1)
Start-up mode – melting and homogenization of C-32 molten corium pool in argon, with the surface temperature Tliq+(50÷100)C. Melt sampling
Switching from the start-up aerosol line to the one of working regime
Aerosol sampling mode for 30 min during evaporation of molten C-32
Feeding of the argon-oxygen mixture into the furnace at a constant flow rate. Sampling regime for approximately 60 min during the melt C-32 to C-100 transition
Melt sampling
Aerosol sampling mode for 30 min during evaporation of molten C-100
HF heating disconnection
Installation disassembly, preparation of aerosol and ingot samples for analytical tests and posttest analysis
Test procedure

## Slide 8: Questions for discussion
Content of FPS in the charge It is proposed to use the same content as in MASCA (mass %: La2O3 - 0.59, CeO2 - 0.61, BaO - 0.56, SrO - 0.59, Mo - 0.5, Ru - 0.5) for the comparison of the results
Forms of the FPS put in the charge
It is proposed to introduce Mo and Ru in the form of metals, and other FP as oxides (SrO and BaO will be sintered with ZrO2 )