## Slide 1: Results on the UO2 – SiO2 system
ISTC PRECOS Project
#3813
A.P. Alexandrov Research Institute of Technology
1st PRECOS Meeting
Presented by Larisa Mezentseva
ISC RAS
Saint-Petersburg

## Slide 2: Previously obtained data on the system
Phase diagrams available in literature
UO2–SiO2 phase diagram with a eutectic by S.M. Lang et al., Nat. Bur. Stand., Circular 568. 1956
Eutectic composition (15-10) UO2 – (85-90) SiO2, mol %
Eutectic temperature 1650±10 °С
1650±10
SiO2
80
60
40
20
UO2
1800
mol % SiO2
UO2 + SiO2
1400
1600
2000
2200
UO2 + L
L
SiO2
+
L
T, C

## Slide 3: Previously obtained data on the system
Phase diagram available in literature
Fusion diagram with the miscibility gap by S. Lungu, Romanian J. of Physics. 1962. V. 7. N 4. P. 419
Eutectics composition: 2 UO2 – 98 SiO2, mol %
Eutectic temperature 1719±10 °С
Monotectic temperature 2070±10 °С
mol % SiO2
2600
1719±10
SiO2
80
60
40
20
UO2
2000
UO2 + SiO2
1600
1800
2200
2400
UO2 + L
T, C
2800
L
L1 + L2
2070±10

## Slide 4: Experimental CORPHAD results
Red lines – Lungu’ diagram
Blue lines and blue points –
results of our previous work
within the CORPHAD project
The miscibility gap was found to exist
The miscibility region position was roughly outlined
The monotectic temperature was determine to be in the temperature range of 2000–2080C

## Slide 5: Research objectives of PRECOS project
  To define the monotectic temperature and the boundary curve of the miscibility gap in vicinity of the monotectic temperature
  To determine the critical point of the boundary curve
  To determine eutectic, solidus and liquidus temperatures, tie-lines in the miscibility gap

## Slide 6: Methods of analysis
Solidus – liquidus temperatures determination by
visual polythermal analysis (Galakhov microfurnace and IMCC)
Heat treatment, exposure and quenching
SEM/EDX analysis

## Slide 7: Experiment technique
  1 – pyrometer;
  2 – video cameras;
  3 – W heating tube;
  4 – Mo crucible
  Atmosphere – Ar + H2(4 vol. %)
  Total gas pressure – 3 atm
  Mass of the samples – 50–150 mg
  Stepwise heating
  Heating rate – 1–8C/min
  Exposure time – 5 and 10 min
  Quenching
The error of pyrometer temperature
measurements is ±1 relative %
Scheme of the modernized Galakhov microfurnace:

## Slide 8: Characteristics of the tests on the UO2–SiO2 system
UO2 of >99.0 % purity
SiO2 of 99.99% purity
Total mass of the charge – 150 mg (Galakhov microfurnace)
– about 1 kg (IMCC)

## Slide 9: Experimental results of Galakhov microfurnace
Longitudinal sections of the crucibles
GPRS 1
2050C 5 min.
below monotectic
GPRS 2
2080C 5 min.
GPRS 3
2080C 10 min.
just above monotectic
Mo crucible
Heavy liquid
Light liquid
0.5 mm
0.7 mm
0.8 mm
Heavy liquid
Light liquid

## Slide 10: Experimental results of Galakhov microfurnace
Longitudinal section
of the crucible
GPRS 1
2050C 5 min.
below monotectic
Fragment of the cooled specimen
Bright UO2 unfused crystals are observed
80 m
0.5 mm

## Slide 11: Experimental results of Galakhov microfurnace
Longitudinal section
of the crucible
GPRS 2
2080C 5 min
just above monotectic
Fragment of the cooled specimen
Cooled heavy liquid
Cooled light liquid
Mo crucible
50 m
60 m
0.7 mm

## Slide 12: Experimental results of Galakhov microfurnace
Longitudinal section
of the crucible
GPRS 3
2080C 10 min
just above monotectic
Fragment of the cooled specimen
Cooled heavy liquid
Cooled light liquid
Mo crucible
30 m
0.8 mm
100 m

## Slide 13: Experimental results of Galakhov microfurnace
GPRS 2
2080C 5 min
A drop of heavy liquid in light liquid near the phase boundary after cooling
30 m

## Slide 14: Experimental results
GPRS 2 and 3
EDX analysis of the domains in heavy liquid layer
Examined region | Composition, mol % | 
 | UO2 | SiO2
SQ1 | 26.7 | 73.3
SQ2 | 27.34 | 72.66
SQ3 | 27.96 | 72.04
SQ4 | 30.28 | 69.72
Overage value | 28.07±1.56 | 71.93±1.56
Examined region | Composition, mol % | 
 | UO2 | SiO2
SQ1 | 28.09 | 71.91
SQ2 | 31.78 | 68.22
SQ3 | 29.97 | 70.03
SQ4 | 28.26 | 71.74
Overage value | 29.53±1.73 | 70.47±1.73
2080C 5 min
2080C 10 min

## Slide 15: Experimental results
GPRS 2 and 3
EDX analysis of the domains in light liquid layer
Examined region | Composition, mol % | 
 | UO2 | SiO2
SQ1 | 12.64 | 87.36
SQ2 | 11.69 | 88.31
SQ3 | 11.66 | 88.34
Overage value | 12.00±0.56 | 88.00±0.56
Examined region | Composition, mol % | 
 | UO2 | SiO2
SQ1 | 11.51 | 88.49
SQ2 | 11.62 | 88.38
SQ3 | 12.74 | 87.26
Overage value | 11.96±0.68 | 88.04±0.68
2080C 5 min
2080C 10 min

## Slide 16: Experimental results of IMCC
The thermogram of PRS1 test
sampling 1 2 3
Tliq measurement

## Slide 17: Experimental results of IMCC
Fragment of thermogram of PRS1 test
Tliq measurement

## Slide 18: Experimental results of IMCC
Optical microscopy
Longitudinal section
of the crystallized melt
(PRS1 test)

## Slide 19: Experimental results
PRS 1
Chemical analysis of the sampling
Sampling number | Composition, mol % | 
 | UO2 | SiO2
1 | 37.68 | 62.32
2 | 47.40 | 52.60
3 | 48.36 | 51.64
Overage value | 44.48±5.91 | 55.52±5.91
Tliq measurement
Measure number | Tliq, C
1 | 2444
2 | 2404
3 | 2427
Overage value | 2425±20

## Slide 20: Experimental PRECOS results
Red lines – Lungu’ diagram
Blue lines and blue points –
results of our previous work
within the CORPHAD project
Yellow points – results of the
present work

## Slide 21: Summary
The monotectic temperature was determine to be in vicinity of 2080C
The liquidus temperature of the 44.5 UO2 – 55.5 SiO2 mol% composition is 2425±20C

## Slide 22: Conclusions
5- and 10 minute exposure at high temperatures is enough to determine correctly a composition of the coexisting liquid phases in the system under investigation, but it is difficult to get reliable results due to the SiO release
To prevent a composition changing during heat treatment use of cover in Galakhov microfurnace could be possibly helpful

## Slide 23: Conclusions
Further experiments required:
To define miscibility gap region
T=2450C, 30 sec exposure (with cover)
T=2500C, 30 sec exposure (with cover)
To define the eutectic temperature
DTA analysis of a series of compositions (mol%)
05UO2 – 95SiO2
04UO2 – 96SiO2
03UO2 – 97SiO2
02UO2 – 98SiO2