## Slide 1
INVESTIGATION OF FISSION PRODUCT RELEASE FROM HIGH BURN-UP FUEL ANNEALED UNDER OXIDIZING AND REDUCTION CONDITION
12th CEG-SAM Meeting
Saint Petersburg, Russia
SPAEP (Atomenergoproekt)
September 11-13, 2007
VERONIKA
(VVER Experiments on Release due to Over-heating: Normalization and Knowledge Augmentation).
Project Proposal
RIAR (Dimitrovgrad), IBRAE (Moscow)
International Science and Technology Center

## Slide 2: Objectives of VERONIKA Project
Receiving the experimental data on fission products release from highly irradiated VVER fuel along with fuel microstructure evolution under severe accident conditions
Physical fission products release models and numerical codes development on the base of results obtained

## Slide 3: MFPR Basic Models
Intragranular gas atoms
-
diffusion towards grain boundary (
С
concentration)
-
bubble nucleation & capture by bubbles
-
capture by dislocations
-
directio
nal diffusion by
С
T
-
grain
-
boundary sweeping, dislocation creep
Intragranular bubbles
-
nucleation and coalescence
-
capture of gas atoms
-
loss of gas atoms by re
-
solution (thermal & recoil)
-
di
ffusion towards grain boundaries (face bubbles):
directional diffusion by
С
T, grain
-
boundary sweeping,
dislocation creep, vacancy gradient.
-
Face bubbles
-
fed by gas atoms, intragranular bubbles
& vaporizati
on of condensed
-
phase species
-
growth & interconnection leading to release
into edge bubbles
Intergranular
zone
Edge bubbles
-
supplied by face bubbles
-
swelling until a critical threshold
-
release into open porosities
Intragranular
zone
Precipitates
-
fed by intragranular diffusion of non
-
gas FPs
-
formation of 3 condensed phases at grain boundary:
ternary (e.g.
Cs
2
MoO
4
),
CsI
& metallic (
Ru
,
Mo, Sb
)
-
equilibrium between precipitates, face bubbles,
UO
2+x
Dislo
cations
-
creep towards grain boundaries
-
trapping of intragranular gases
(atoms & bubbles)
Grain
-
growth & boundary sweeping

## Slide 4: Transport of Fission Gases
Diffusion of gas atoms (Cg)
Intragranular bubbles (Cb, Nb) nucleation, growth and resolution (thermal and irradiation-induced)
Intragranular bubbles diffusion (also biased in temperature gradient) and coalescence
Interactions with dislocations (d), sintering pores (Cp), vacancies (Cv) and interstitials (Ci)
Intergranular bubbles formation, coalescence and interconnection...
X = {Cg, Cb, Vb, d, Cd, Vp, Cp, Cv, Ci}
System of equations:

## Slide 5: Scope of VERONIKA Project Tests
Investigation of fission products release from fuel with burnup of 60 MW*d/kgU in oxidizing and reducing environments in the temperature range of 1400 - 2300oC
Investigation of the release of a wide list of fission products including short living isotopes: 85Kr, 133Xe, 131I, 137Cs, 134Cs, 106Ru, 103Ru, 144Ce, 99Mo, 140Ba, 95Zr and other. That will be provided by pre-irradiation of the specimens in the research reactor

## Slide 6: Revised test matrix part 1
(a): the samples are fuel fragments and the test consists of simple ramp (1K/s) up to 1400°C maintained one hour.
(b): the test consists of the test (a) followed by a ramp (1K/s) up to 1700°C maintained 30 minutes.
(c): the same as (b) but the second ramp ends at T3>2000°C maintained 30 minutes.
(d): in this case samples are fuel pellets in their original cladding ant the test is identical to (b)
(d’): idem (d) but with air.

## Slide 7: Revised test matrix part 2
(a1, b1, c1) : the scenario of tests is identical to a, b and c respectively but in this case the gas phase composition is mixed, for example 25mg/s for H2O and 0,3 mg/s for H2)
(a2, b2): idem than tests a1, b1 but with bare fuel
(e): idem (a) but with fuel rod segments
(f): idem ( c) but with fuel rod segments
(e’): idem (e) but with air
(f’): idem (f) but with air

## Slide 8: Main Test Procedures
Manufacturing of the experimental rig
Initial fuel rod examinations
Refabricated fuel rods manufacturing
Refabricated fuel rods irradiation
Preparation and certification of fuel specimens (fuel pellets and fragments of fuel rods)
FP release tests
Post-test examination of fuel specimens

## Slide 9: Initial fuel rod examination
Objectives:
Selection of the typical spent fuel rod
Avoid the cladding defects – debris, nodules etc
Initial fuel and cladding certification
Test procedures
Eddy-current defectoscopy
Y-scanning
Profilometry
Plenum gas analysis
Fuel and cladding structure characterization
Metallography – Pellet crack pattern, fuel-cladding interaction/gap, fuel porosity, fuel grain size measurement.
SEM - (polished surface and fractography) porosity, intra- and intergranular bubbles pattern.
EPMA – Fission product distribution, precipitates composition.

## Slide 10: Refabricated fuel rods manufacturing
Manufacturing of the short fuel rods (200 mm long) sealed by the welded end plugs and filled with He at 2-2.5 MPa from the fragments of initial fuel rod.
Refabricated fuel rods irradiation
Low power (30-50 Wt/cm)
Low temperature (to be defined)
Objective: accumulation of the short-lived isotopes in the solid solution; prevent any fuel structure transformation

## Slide 11: The main irradiation test parameters of fuel samples

## Slide 12: The interesting fission products

## Slide 13: Specimen preparation
Radial and contraction cracks in the fuel
Pellet-clad separation by heating
the pressurised rods up to 700oC
Bare fuel pellet extraction

## Slide 14: Test Rig
Steam overheater
(800°С)
Heater(150°С)
Condenser
Filter-
dehydrator
Water collector
Additional filter
Flow meter
Ceramic tubes
(ZrO2, Al2O3, Al2O3)
HF coil
Pyrometer
Inlet gas line
Main channel
(ZrO2)
Main filter
Carrier gas line
(in the case
of pure steam
environment)
Gamma-spectrometer
(FP measurement
in the filter)
Gamma-spectrometer
(FP measurement
in the specimen)
Protective gas line
Specimen
holder
Specimen
Pressure
transducer
Hot cell
Gamma-spectrometer
(GFP measurement)
Intel steam line
H2
He
Mass spectrometer

## Slide 15: Crucible materials
Specimen UO2(Zr-UO2 )
Crucible ZrO2
Channel tube (ZrO2 )
Insulating plate (Y2O3 )

## Slide 16: Test Regime
Test temperature
heating in the inert atmosphere up to the temperature of 600 °C
heating from 600 up to 1400 °C with a rate of 1 K/s
annealing at 1400 °C during 1 hour
heating with a rate of ~ 1 K/s up to the specified temperature (1700 or 2300 °C)
annealing during 30 minutes
end of heating

## Slide 17: Test Performance
Parameters to be measured during the test
  intensity of GFP in the delay coil
  intensity of FP in a fuel specimen
  intensity of FP on the main filter
  hydrogen concentration in the carrier-gas after passing through the heater
Results to be obtained
  relative FP release
  hydrogen generation

## Slide 18: Post-Test Examinations
Optical metallography
  grain size
  porosity
  gas swelling
EPMA and SEM analysis
  local content and radial distribution of fission products
  composition of precipitates in the fuel

## Slide 19
MFPR Tasks in VERONIKA Project
Pre-test calculations for determination of the test parameters and conditions
Processing and analysis of the test results
Development and improvement of the physical models on fission products release and high burnup VVER fuel behaviour under severe accident conditions
Implementation of the developed and improved models to the MFPR code
Verification of the MFPR code against the new experimental database and other new available data at the end or during the program

## Slide 20: Project Costs
The first stage
(3 years duration, 800 000 $) :
Т10 – beginning of the work under the project;
Т10+1 year – manufacturing and testing of the experimental rig
Т10+1 year - adaptation of the MFPR code to the new experimental rig, pre-test calculations
Т10+2,5 years – first series of tests (10 tests)
Т10+3,0 years – theoretical analysis of the obtained experimental data, development of models and codes
The second stage
(2.5 years duration, 500 000 $):
  Т20 – beginning of the second stage work;
  Т20+1 year – second series of tests (10 tests)
  Т20+2.5 years –post-test specimen examinations; theoretical analysis of the obtained experimental data, development of models and codes
The estimated total cost of the Project (2 stages) – 1 300 000 $