## Slide 1: Proposals on the ZrO2–FeOy system study
ISTC PRECOS Project
#3813
A.P. Alexandrov Research Institute of Technology
Presented by Oksana Almjasheva
1st PRECOS Meeting
ISC RAS
Saint-Petersburg

## Slide 2: Research objectives
ZrO2–FeOy
ZrO2
Т, C
mol %
60
40
20
FeO1.5
10-7
10-5
10-3
10-1
101
103
air
Fe0.938O
500
700
900
1100
1300
1500
1700
FeO
80
10-1
101
10-7
10-5
10-3
10-1
103
10-3
105
105
air
Darken L.S. Gurry R.W.
(1945, 1946)
FeO
Fe2O3
Fe3O4
?
ss
CORPHAD
FeO mol %
1300
1700
2100
2500
80
60
40
20
T, C
FeO
ZrO2
(1332±5)C
2900
Published
?
1597
?
Jones T.S.
Kimura Sh.
Muan A.
(1967)
FeO1.5
FeO1.5, mol. %
1300
1500
1700
1900
80
60
40
20
Т, C
2100
2300
2500
2700
2710
1525
1434
?
ZrO2
Petrov Yu.B.
Udalov Yu.P.
Slovak J.
Morozov Yu.G.
(2002)
FeO1.33, mol. %
1300
1500
1700
1900
80
60
40
20
Т, C
2100
2500
2300
~FeO1.3
2700
ZrO2
?
?
~FeO1.33

## Slide 3: Research objectives
 | Zr 4+ | Fe | 
 |  | 2+ | 3+
R, Å | 0.98 | 1.07 | 0.95
(ΔR/R)2 | 0 | 1.6·10-3 | 1.8·10-4
– Zr
– O
b
a
c
FeO mol %
1300
1700
2100
2500
80
60
40
20
T, C
~FeO
ZrO2
(1332±5)C
2900
500
1000
1500
2000
Т, C
2500
1172
m-ZrO2
2347
2710
t-ZrO2
c-ZrO2
Zr1-x-yFe2+xFe3+y⁪x+0.5yO2-x-0.5y
(y/x)
– Fe
?
Petrov Yu.B.
Udalov Yu.P.
Slovak J.
Morozov Yu.G.
(2002)
FeO1.33, mol. %
1300
1500
1700
1900
80
60
40
20
Т, C
2100
2500
2300
~FeO1.3
2700
~FeO1.33
ZrO2
Jones T.S.
Kimura Sh.
Muan A.
(1967)
~FeO1.5
FeO1.5, mol. %
1300
1500
1700
1900
80
60
40
20
Т, C
2100
2300
2500
2700
2710
1525
1434
?
ZrO2
?
Zr
Fe
O2-
⁪
⁪

## Slide 4: Methods of synthesis
Initial compositions
mechanical mixing of powders
Hydrothermal synthesis
conventional technique
sol-gel technique
oxidizing medium => iron state – mainly Fe3+
solid solution ZrO2(FeOy) formation
mixing of components at the molecular level =>
=> the Increasing of the processes rate

## Slide 5: Methods of synthesis and investigation
annealing and quenching in neutral atmosphere or in oxygen flow
Heat treatment and analysis
visual-thermal analysis with assigned and controlled partial oxygen pressure
IMCC (air)
Minimum deviation from initial composition due to high heating rate
Tliq ; Tsol
DTA(DSC)/TG/MS analysis with assigned and controlled partial oxygen pressure
the evaluation of changing O2 content during heating
Tliq, stratification

## Slide 6: Investigation methods
SEM/EDX/WDS analysis
POST-TEST analysis
chemical composition of a system, crystallizing phases including light elements
X-ray powder diffraction analysis
XRF analysis
chemical composition of a system
Mössbauer spectroscopy
Structure and type-structure of crystallizing phases in a system
Chemical analysis
chemical composition of a system
oxidation state of elements
charge state of iron
quantitative evaluation of Fe2+/Fe3+ ratio
quantity of iron in ZrO2 and as of separate phase
localization of iron ions in ZrO2 structure

## Slide 7: Conclusions
Really analyzing the ZrO2–FeOy, it is necessary to study the ZrO2–FeO–Fe2O3 system (because y depends on T and pO2)
To obtain the reliable data complex study of the system is needed, in particular solid solutions and liquidus character
Complex method of sample preparation and analysis is necessary
Experiments are to be carry out in the gas atmosphere with controlled pO2
Following matrix of the compositions and conditions of the experiment are proposed

## Slide 8: Conclusions
ZrO2
FeO
Fe2O3
Fe3O4
ss
Pt | FeO1.5, mol % | Atm | Objectives
1 | 95 | air | eutectic
2 |  | O2 | 
3 | 90 | air | 
 |  | O2 | 
4 |  |  | 
5 | 20 | air | solid solutions
 |  | O2 | 
6 |  |  | 
7 | 10 | air | 
8 |  | O2 | 
9 | 60 | air | miscibility gap
10 |  | O2 | 
11 | 50 | air | 
 |  | O2 | 
12 |  |  | 
13 | 40 | air | 
 |  | O2 | 
14 |  |  |