## Slide 1: O-U-Zr phase diagram : state of the art after the CORPHAD project
M. Barrachin
11th July 2008 St Petersburg, ISTC PRECOS Kick-off Meeting

## Slide 2
Outline
CORPHAD objectives
Past data on the miscibility gap in the U-O-Zr phase diagram
NUCLEA actual modelling
Experimental data (CORPHAD)
Possible revision of the U-O-Zr phase diagram modelling
ITU experimental data
Conclusions

## Slide 3
CORPHAD objectives related to the U-O-Zr phase diagram investigation
To determine more accurately the shape of the miscibility gap (MG) in the U-O-Zr phase diagram (hypostoichiometric region)
The shape of the miscibility gap as well as the orientation of the tie lines inside this MG have an impact on the composition of the non miscible phases in the bottom of the RPV at high temperature (stratification process).
Few quantitative thermodynamic experimental data related to the MG before the CORPHAD Project :
  at very high temperature : Guéneau et al. (1998), tie-line in the liquid state, measured at 3223 ±100 K
  at lower temperature : apparently contradictory and imprecise data

## Slide 4
Past data on the MG in U-O-Zr (1)

## Slide 5
Past data on the MG in U-O-Zr (2)

## Slide 6
Past data on the MG in U-O-Zr (3)

## Slide 7
NUCLEA actual modelling: 2173 K (1)
Reproduces the small oxygen solubility in U-Zr alloys measured by Maurizi (1996)
Maurizi’s data consistent with a small oxygen solubility in U (Guéneau 1998, CORPHAD 2006)
Leads to a rather large MG at higher temperature

## Slide 8
NUCLEA actual modelling : 2573 K (2)
Allows to reconcile the different data apparently contradictory about the existence of a large miscibility gap

## Slide 9
NUCLEA actual modelling 3073 K (3)
Reproduces Guéneau’s data at very high temperature
Large MG

## Slide 10
NUCLEA actual modelling (4)
Comparison with experimental liquidus for (U,Zr)O2+x

## Slide 11
NUCLEA actual modelling (5)
Main conclusions and main uncertainties (as stated in 2003)
Below 2073 K, good agreement between NUCLEA and the available experimental data
At T > 2073 K and high zirconium content, it seems that the extent of the miscibility gap is limited by the UO2-Zr0.7O0.3 line (to be confirmed in CORPHAD)
UO2-Zr0.7O0.3

## Slide 12
NUCLEA actual modelling (6)
Main conclusions and main uncertainties (as stated in 2003)
The diphasic field L + (U,Zr)O2-x is not precisely determined between 2273 and 2573 K (to be determined in CORPHAD)
Orientation of the tie lines in the diphasic field L1 + L2 at a temperature lower than that of the Guéneau’s test (to be determined in CORPHAD)
L + (U,Zr)O2-x
L1 + L2

## Slide 13
Liquidus and solidus temperatures in the UO2-ZrO2-Zr region in order to determine the limits of the diphasic field L + (U,Zr)O2-x
For compositions for which liquidus and solidus are determined, detection of MG
Experimental data related to the extent of the miscibility gap and measurement of the tie lines
CORPHAD experimental data
3 « types »

## Slide 14
Test | U | Zr | O | Tliq (K) | Calculation | D
CORD 28-I | 7.7 | 53.7 | 38.6 | 2358 | 2238 | -120
CD4 | 8.0 | 52.0 | 40.0 | 2373 | 2231 | -142
CORD 28-II | 12.9 | 43.9 | 43.2 | 2443 | 2357 | -86
CD3 | 13.0 | 43.0 | 44.0 | 2408 | 2362 | -46
CD5 | 16.0 | 36.0 | 48.0 | 2498 | 2426 | -72
CORD 34 | 21.5 | 34.7 | 43.8 | 2578 | 2470 | -92
ITU | 22.0 | 33.0 | 44.0 | 2550 | 2486 | -64
CORD 37 | 32.5 | 29.2 | 38.3 | 2601 | 2570 | -31
CORD 42 | 40.5 | 27.0 | 32.5 | 2663 | 2595 | -68
CORD 41 | 56.0 | 3.1 | 40.9 | 2788 | 2690 | -98
CORD 29 | 19.8 | 17.2 | 63.0 | 2734 | 2803 | +69
CORPHAD experimental data (2)
Significant disagreement at low liquidus temperatures (i.e high Zr content) up to 2573 K
Consistent disagreement : calculated liquidus temperatures too low

## Slide 15
CORPHAD experimental data (3)
CORPHAD tests (42, 37) in agreement with NUCLEA
CORPHAD test (34) in disagreement with NUCLEA
(??) at this temperature, no MG in O-U

## Slide 16
Tie lines in the miscibility gap
 |  | U0.325Zr0.292 O0.383 (2643 K) | U0.405Zr0.270O0.325 (2753 K) | U0.560Zr0.031O0.409 (2948 K)
L2 (oxide) | U | 25.2 | 27.7 | 43.7
 | Zr | 26.7 | 23.2 | 1.4
 | O | 48.2 | 49.2 | 54.9
L1 (metal) | U | 40.8 | 53.2 | 88.8
 | Zr | 32.2 | 29.3 | 2.7
 | O | 27.2 | 17.6 | 8.5
CORPHAD experimental data (4)

## Slide 17
U0.325Zr0.292 O0.383 (2643 K)
Not compatible with the Guéneau’s data
CORPHAD experimental data (5)

## Slide 18
U0.405Zr0.270 O0.325 (2753 K)
CORPHAD experimental data (6)

## Slide 19
U0.560Zr0.031 O0.409 (2958 K)
CORPHAD experimental data (7)

## Slide 20
CORPHAD experimental data (8)
Significant disagreement at low liquidus temperatures (i.e high Zr content) up to 2573 K
Experimental data related to the extent of the miscibility gap and measurement of the tie lines indicate that MG does not reach the UO2-Zr section
Main conclusions

## Slide 21
Possible revision of the O-U-Zr phase diagram (1)
2373 K
NUCLEA
Revised

## Slide 22
Possible revision of the O-U-Zr phase diagram (2)
2473 K
NUCLEA
Revised

## Slide 23
Possible revision of the O-U-Zr phase diagram (3)
Miscibility gap at 2573 K
At temperature slightly higher than in NUCLEA
2573 K
NUCLEA
Revised

## Slide 24
2573 K (revised)
Possible revision of the O-U-Zr phase diagram (4)
Global agreement with the CORPHAD observations about presence of MG
Comparison with the detections of the MG for the CORPHAD compositions in the U-O-Zr

## Slide 25
ITU experimental data (1)
From M. Sheindlin et al. (2006)

## Slide 26
ITU experimental data (2)
ITU liq
 Seems to confirm the presence of MG on the UO2-Zr section.
ITU sol
CORPHAD liq (no MG)

## Slide 27
Conclusions
At T > 2073 K and high zirconium content, it seems that the extent of the miscibility gap is limited by the UO2-Zr0.7O0.3 line (to be confirmed in CORPHAD)
 it is confirmed by the CORPHAD results
The diphasic field L + (U,Zr)O2-x was not precisely determined between 2273 and 2573 K (to be determined in CORPHAD)
 the CORPHAD results confirm that the liquidus line modelling should be revised
Orientation of the tie lines in the diphasic field L1 + L2 at a temperature lower than that of the Guéneau’s test (to be determined in CORPHAD)
     the CORPHAD results indicate a smaller MG than that determined by Guéneau et al. (disagreement with ITU results)

## Slide 28
CORPHAD results
ITU results
NUCLEA
PRECOS matrix ?
Thank you for your attention