## Slide 1: Eutectic in the FeO1.5-UO2-ZrO2 system
ISTC PRECOS Project
#3813
A.P. Alexandrov Research Institute of Technology
Presented by Vyacheslav Almjashev
1st PRECOS Meeting
ISC RAS
Saint-Petersburg

## Slide 2: Experimental objectives
To specify the ternary eutectics temperature and composition in the inert atmosphere
To determine solubility limits of components in the solid solutions

## Slide 3: Known data in the system
Riley B.
(1969)
Evans W.D.J.
White J.
(1964)
UFeO4
Jones T.S.
Kimura Sh.
Muan A.
(1967)
~FeO1.5
FeO1.5, mol. %
1300
1500
1700
1900
80
60
40
20
Т, C
2100
2300
2500
2700
2710
1525
1434
?
ZrO2
Petrov Yu.B.
Udalov Yu.P.
Slovak J.
Morozov Yu.G.
(2002)
FeO1.33, mol. %
1300
1500
1700
1900
80
60
40
20
Т, C
2100
2500
2300
~FeO1.3
2700
~FeO1.33
ZrO2
1300
1350
1400
80
60
40
20
Т, C
UO2.67
FeO1.5
FeO1.5, mol %
1450
0.210105 Pa
?
1200
1400
1600
1800
80
60
40
20
Т, C
UO2+x
2000
FeO1.5
FeO1.5, mol %

## Slide 4
Fusion diagram near eutectic point
20
80
UO2+x
80
UFeO4
20
mol %
FeO1.5
60
ZrO2
UO2 ss
1323
1525
<1200
1240
1348
60
1323
1348
1240

## Slide 5
Paper
Almjashev V.I., Barrachin M., Bechta S.V., Bottomley D., Defoort F., Fischer M., Gusarov V.V., Hellmann S., Khabensky V.B., Krushinov E.V., Lopukh D.B., Mezentseva L.P., Miassoedov A., Petrov Yu.B., Vitol S.A. Eutectic crystallization in the FeO1.5–UO2+x–ZrO2 system // J. Nucl. Mater (Prepared for press)

## Slide 6
Conclusions
Existence range of UFeO4 compound is unknown
Several eutectics are possible in the system
More detailed consideration of this system is required
FeO1.5
UFeO4
ZrO2
?
UO2+x
UFeO4
ZrO2
?